| Submitted by the expert from OICA | Informal document No. GRSG-102-19 (102nd GRSG, 16-20 April 2012 agenda item 8) |
| --- | --- |

Proposal for amendments to Regulation No. 67
(Equipment for liquefied petroleum gas (LPG))

The modifications to the proposal ECE/TRANS/WP.29/GRSG/2012/8 are marked in blue.

Annex 8, insert new paragraphs 4.4.2.1. to 4.4.2.3., to read:

"4.4.2.1.	The test shall be performed in compliance with standard

ISO 1431/1 -1:2004/Amd 1:2009.

4.4.2.2.	The test-pieces, which have to be stretched to an elongation of 20 per cent shall be exposed to air of 40 °C and a relative humidity of 50 per cent ± 10 per cent with an ozone concentration of 50 parts per hundred million during 120 hours.

4.4.2.3.	Cracking of the test pieces is not allowed."

Paragraphs 4.4.3.3.1., 4.4.3.3.2. and 4.4.3.3.3., should be deleted.

__________