#### UNITED

# NATIONS

Distr.

# GENERAL

# ST/SG/AC.10/C.3/2001/52

17 September 2001

# ORIGINAL : ENGLISH

# COMMITTEE OF EXPERTS ON THE TRANSPORT OF

# DANGEROUS GOODS AND ON THE GLOBALLY

# HARMONIZED SYSTEM OF CLASSIFICATION

# AND LABELLING OF CHEMICALS

# Sub-Committee of Experts on the

# Transport of Dangerous Goods

# (Twentieth session, 3-12 December 2001,

# agenda item 5 (b))

# PACKAGINGS

# Miscellaneous proposals

# Transmitted by the European Secretariat of Manufacturers

# of Light Metal Packaging (SEFEL)

# Background

# In their informal document UN/SCETDG/19/INF.10 for the July 2001 meeting of the Sub-Committee of Experts on the Transport of Dangerous Goods, SEFEL already proposed to base the general requirements of steel quality in connection with para. 6.1.4.1.1 on concrete international standards. SEFEL also outlined the reasons for that proposal.

# A similar proposal was made by the International Conferederation of Drum Manufacturers (ICDM) and the International Confederation of Container Reconditioners (ICCR) in their document ST/SG/A.C10/C.3/2001/17 for drums greater than 100 litres. The July 2001 Sub-Committee meeting adopted the ICDM/ICCR proposal putting the contents of it into a note to para. 6.1.4.1.1.

# The Sub-Committee further decided to come back to the SEFEL proposal contained in their INF.10 at the next session on the basis of a new document which SEFEL was invited to prepare.

# GE.01-

# Proposal

# In this connection, SEFEL proposes to complement the Note to para. 6.1.4.1.1 for smaller drums by the following:

# "In the case of carbon steel drums of a capacity not greater than 40 litres, "suitable" steels below a thickness of 0.5 mm are identified in ISO 11949: Cold-reduced electrolytic tinplate, ISO 11950: Cold-reduced electrolytic chromium/chromium oxide-coated steed and ISO 11951: Cold-reduced blackplate in coil form for the production of tinplate or electrolytic chromium/chromium oxide-coated steel".

# _______

# Text boxes

STSTE

Secretariat