| UNITED NATIONS |  | ST |
| --- | --- | --- |
|  | Secretariat | Distr. GENERAL ST/SG/AC.10/C.3/2009/39 7 September 2009 Original: ENGLISH |

COMMITTEE OF EXPERTS ON THE TRANSPORT OF

# DANGEROUS GOODS AND ON THE GLOBALLY

# HARMONIZED SYSTEM OF CLASSIFICATION

# AND LABELLING OF CHEMICALS

Sub-Committee of Experts on the 
Transport of Dangerous Goods

Thirty-sixth session
Geneva, 30 November – 9 December 2009
Item 5 of the provisional agenda

MISCELLANEOUS PROPOSALS OF AMENDMENTS TO THE MODEL REGULATIONS ON THE TRANSPORT OF DANGEROUS GOODS

6.1.4 Requirements for  packagings

4.1.4.1 Packing instructions concerning the use of packagings

Transmitted by the expert from Italy

Introduction

1.	The requirements for the manufacturing of packagings mentioned in Chapter 6.1 do not give the opportunity to build the boxes with metals other than steel or aluminum (code 4N).

2.	In 4.1.4.1, in the packing instructions for explosives (P 110a to P144) 1N2 removable head drums are not listed.

3. 	Titanium is a metal that has mechanical properties equal if not superior to those of other metals that are explicitly provided for in Chapter 6.1 as steel and aluminum, in terms of hardness and mechanical resistance to traction. Moreover, unlike steel, titanium is non-magnetic, a feature essential for its use on board military vehicles, such as minesweepers.

4. 	Testing explosive articles, such as ELECTRICAL or NON-ELECTRICAL DETONATORS for blasting, UN 0030 and 0029 respectively, contained in combination packagings with a titanium box or drum as the outer packaging, in compliance with Test Series 6 in the Manual of Tests and Criteria, have confirmed the excellent properties of this metal, even superior to similar steel external packagings. The titanium boxes/drums were also tested for the contemporary explosion of the articles placed inside the containers.

5.	The tests results show that the outer packagings such as boxes made of titanium (Mod VAS/3 bis) to provide the desired resistance to the simultaneous explosion of all the detonators contained therein, were built with a wall thickness of the body and the fund of only 3 mm, instead of those made of steel – on a previous prototype subjected to the same series of tests – constructed with a wall thickness of 5 mm.

6. 	From the tests it can be said:

4N boxes, and drums 1N2 removable head (where N is titanium) are, in relation to the weight, certainly more robust than their analogues produced in steel (4A) and (1A2) or aluminum (4B) and (1B2 )

Proposal:

7.	In Chapter 6.1, Table 6.1.2.7, 4. Boxes, after H. Plastics the following line should be added:

N.  Metal, other than steel or aluminium                                   4N             6.1.4.14

In 6.1.4.14 Steel or aluminium boxes the following lines should be modified to read as follows:

Steel or aluminium or other metal boxes

4A Steel boxes

4B Aluminium boxes

4N Metal, other than steel or aluminium boxes

8.	In 4.1.4.1

4N should be added after 4A and 4B in the following instructions:

P001, P002, P110a), P110b), P111, P112a), P112b), P112c), P113, P114, P114b), P115, P116, P130, P131, P132a), P132b), P133, P134, P135, P136, P137, P138, P139, P140, P141, P142, P143, P144, P400, P403, P404, P405, P406, P410, P501, P502, P503, P504, P520, P600, P601, P602, P800, P802, P803, P804.

9.	In 4.1.4.1

1N2 should be added after 1A2 and/or 1B2 in the following packing instructions (Packing instructions for Class 1 explosives):

P110a), P110b), P111, P112a), P112b), P112c), P113, P114, P114b), P115, P116, P130, P131, P132a), P132b), P133, P134, P135, P136, P137, P138, P139, P140, P141, P142, P143, P144.

10.	If necessary, in the Packing Instructions for explosives, the code N can be assigned exclusively to Titanium by adding a note as follows:

4N(a)

1N2(a)

where N stands for Titanium.

Examples:

| P001 PACKING INSTRUCTION (LIQUIDS) P001 |
| --- |
| The following packagings are authorized provided that the general provisions of 4.1.1 and 4.1.3 are met: |
|  | Maximum capacity/Net mass (see 4.1.3.3) |
|  | Packing group I | Packing group II | Packing group III |
| Combination packagings |
| Inner packagings | Outer packagings |  |  |  |
| Glass 10 l Plastics 30 l Metal 40 l | Drums steel (1A2) aluminium (1B2) other metal(1N2) plastics (1H2) plywood (1D) fibre (1G) Boxes steel (4A) aluminium (4B) other metal(4N) natural wood (4C1, 4C2) plywood (4D) reconstituted wood (4F) fibreboard (4G) expanded plastics (4H1) solid plastics (4H2) Jerricans ... ... | 250 kg 250 kg 250 kg 250 kg 150 kg 75 kg 250 kg 250 kg 250 kg 150 kg 150 kg 75 kg 75 kg 60 kg 150 kg .... .... | 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 60 kg 400 kg ... ... | 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 400 kg 60 kg 400 kg ... ... |
| Single packagings |
| ... | ... | ... | ... |

| P131 PACKING INSTRUCTION P131 |
| --- |
| The following packagings are authorized, provided that the general packing provisions of 4.1.1, 4.1.3 and special packing provisions of 4.1.5 are met: |
| Inner packagings | Intermediate packagings | Outer packagings |
| Bags paper plastics Receptacles fibreboard metal plastics wood Reels | Not necessary | Boxes steel (4A) aluminium (4B) other metal (4N)(a) natural wood, ordinary (4C1) natural wood, sift-proof walls (4C2) plywood (4D) reconstituted wood (4F) fibreboard (4G) Drums steel, removable head (1A2) aluminium, removable head (1B2) other metal, removable head (1N2)(a) fibre (1G) plastics, removable head (1H2) plywood (1D) |
| Special packing provision: PP68 For UN Nos. 0029, 0267 and 0455, bags and reels shall not be used as inner packagings. |

(a) Only titanium

_______________

# Footnotes

In accordance with the programme of work of the Sub-Committee for 2009-2010 approved by the Committee at its fourth session (refer to ST/SG/AC.10/C.3/68, para. 118 (d) and ST/SG/AC.10/36, para. 14).