|  | United Nations | ECE/TRANS/WP.29/GRSP/2019/25 |
| --- | --- | --- |
|  | Economic and Social Council | Distr.: General 18 September 2019 Original: English |

Economic Commission for Europe

Inland Transport Committee

World Forum for Harmonization of Vehicle Regulations

Working Party on Passive Safety

Sixty-sixth session

Geneva, 10-13 December 2019

Item 10 of the provisional agenda

UN Regulation No. 22 (Protective helmets)

Proposal for the 06 series of amendments of UN Regulation No. 22 (Protective helmets)

Submitted by the experts from the Informal Working Group on UN Regulation No. 22*

The text reproduced below was prepared by the experts from the Informal Working Group on UN Regulation No. 22. It is based on ECE/TRANS/WP.29/GRSP/2019/11 distributed at the sixty-fifth session of the Working Party on Passive Safety (GRSP). The modifications to the current text of UN Regulation No. 22 are marked in bold for new characters and strikethrough for deleted characters.

I.	Proposal

"UN Regulation No. 22

Uniform provisions concerning the approval of protective helmets and of their visors for drivers and passengers of motor cycles and mopeds

Contents

Page

Regulation

1.	Scope			4

2.	Definitions		4

3.	Application for approval		6

4.	Markings		7

5.	Approval		7

6.	General specifications		10

7.	Tests				18

8.	Tests report		38

9.	Production qualification		38

10.	Conformity of production and routine tests		40

11.	Modification and extension of approval of a helmet or a visor type		46

12.	Penalties for non-conformity of production		47

13.	Production definitely discontinued		47

14.	Information for wearers		47

15.	Transitional provisions		48

16.	Names and addresses of the Technical Services responsible for conducting approval tests and 
of the Type Approval Authorities		49

Annexes

1	Communication concerning approval or extension or refusal or withdrawal of approval or production definitely discontinued of a protective helmet and visor type pursuant to Regulation No. 22		51

2	Examples of arrangements of approval marks		53

3	Diagram of protective helmets		56

4	Headforms		57

5	Positioning of the helmet on the headform		63

6	Reference headforms (shape, dimensions)		64

7	Oblique impact test method of measuring rotational acceleration		89

8	Test machines		94

9	Testing of the angle of opening of the visor		101

10	Abrasion test procedure		102

11	Methods of measuring light diffusion and light transmission coefficient		104

12	Type approval scheme (Flow chart)		110

13	Definitions		111

14	Product of the spectral distribution of radiation of the signal light 
and standard illuminant D65		112

15	Test of refractive powers		119

16	Test for mist-retardant visors		122

17	High speed particle Test for visors		124

18	Test for photochromic, liquid crystal visors		126

1.		Scope

This Regulation applies to protective helmets for drivers and passengers of mopeds and of motor cycles with or without side-car  and to the visors fitted to such helmets or intended to be added to them.

2.		Definitions

For the purposes of this Regulation,

2.1.	"protective helmet" means a helmet primarily intended to protect the wearer's head against impact. Some helmets may provide additional protection;

2.2.	"shell" means the hard part of the protective helmet, which gives it its general shape;

2.3.	"protective padding" means a material used to absorb impact energy;

2.4.	"comfort padding" means a material provided for the wearer's comfort;

2.5.	"retention system" means the complete assembly by means of which the helmet is maintained in position on the head, including any devices for adjustment of the system or to enhance the wearer's comfort;

2.5.1.	"chin-strap" means a part of the retention system consisting of a strap that passes under the wearer's jaws to keep the helmet in position;

2.5.2.	"chin-cup" means an accessory of the chin-strap that fits round the point of the wearer's chin;

2.6.	"peak" means an extension of the shell above the eyes;

2.7.	"lower face cover" means a detachable, movable or integral (permanently fixed) part of the helmet covering the lower part of the face;

2.7.1.	"protective lower face cover" means a detachable, movable or integral (permanently fixed) part of the helmet covering the lower part of the face and intended to protect the chin of the user against impacts;

2.7.2.	"non protective lower face cover" means a detachable or movable part of the helmet covering the lower part of the face that does not protect the chin of the user against impacts;

2.7.3.	Helmet types

(J) Jet: helmet without any part to cover the lower part of the face. Open face.

(NP) Jet: helmet with a detachable or movable part of that cover the lower part of the face that does not protect the chin

(P) Full face, helmet with a detachable, movable or integral (permanently fixed) part of the helmet covering the lower part of the face and intended to protect the chin

(P/J) Modular helmet, means a helmet, equipped with a movable or detachable protective lower face cover, that meets the requirements for both conditions of use with or without chin guard in position. Chin protection is only guaranteed with the lower face cover in position.

2.8.	"visor" means a transparent protective screen extending over the eyes and covering all or part of the face;

2.8.1.	"sun shield" means an additional tinted screen in combination with clear visor, as define at § 6.16.3.4., that covers the eyes.

2.9.	"goggles" mean transparent protectors that enclose the eyes;

2.10.		Disposable protective film

2.10.1.	A removable plastic film may be applied to protect the visor prior to use. In this case the film has to be opaque or printed, so that it must be removed before use.

2.10.2.	A protective film (tear-off) may be used for racing for example to reduce the level of luminous transmission. Such tear-off- films are not for use on the road and are not covered by this Regulation.

2.11.	"ocular areas" mean two circles of minimum diameter 52 mm spaced symmetrically about the vertical centre line of the visor, the distance between the centres of the circles being 64 mm measured in the horizontal front plane of the visor as worn.

2.12.	"luminous transmittance τv" is defined in Annex 13.

2.13.	"relative visual attenuation quotient" means the relative visual quotient (Q) and is defined in Annex 13.

2.14.	"basic plane of the human head" means a plane at the level of the opening of the external auditory meatus (external ear opening) and the lower edge of the orbits (lower edge of the eye sockets);

2.15.	"basic plane of the headform" means a plane which corresponds to the basic plane of the human head;

2.16.	"reference plane" means a construction plane parallel to the basic plane of the headform at a distance from it which is a function of the size of the headform;

2.17.	"protective helmet type" a category of protective helmets displaying differences from one another, with special regard to:

2.17.1.	the trade name or mark, or "manufacturer"
It is possible to have different trade marks, provided that a trade mark stated in the approval certificate is also present in an easily accessible position.

2.17.2.	the materials or dimensions of the shell, of the retention system or of the protective padding. shell or protective padding materials. However, a protective helmet type may include a range of sizes, provided that the thickness and density of the protective padding of each size in the range is at least equal to that of the protective helmet that has passed the tests.

A type of helmet may include different shell sizes (provided that the shell design must stay the same) and different retaining systems provided that they all meet the requirements of this UN Regulation

2.18.	"visor type" means a category of visors which do not differ substantially in such essential characteristics as:

2.18.1.	the trade name or mark, or "manufacturer"

However, it is possible to have different trade marks, provided that a trade mark stated in the approval certificate is also present in an easily accessible position.

2.18.2.	the materials, dimensions, manufacturing processes (such as extrusion of moulding), colour, surface treatment, system of attachment to the helmet;

2.19.	"approval test" means a test to determine the extent to which a protective helmet type and/or a visor type submitted for approval is capable of satisfying the requirements;

2.20.	"production quality test" means a test to determine whether the manufacturer is able to produce helmets and/or visors in conforming with the helmets and/or visors submitted for type approval.

2.21.	"routine testing" means the testing of a number of helmets and/or visors selected from a single batch to verify the extent to which they satisfy the requirements.

2.22.	"accessory" means any object intended to integrate the secondary functionalities of the helmet (e.g. tear off inner visor, electronic devices and their support).

2.23.	"trade mark" means the trade name which is used by the manufacturer and declared on the approval certificate to mark the helmet or the visor.

2.24.	"HPI Head Position Index" means the distances on the headform measured from the basic plane along the intersection with the longitudinal plane to the lower front edge of the helmet.

3.		Application for approval

3.1.	Application for approval of a protective helmet type

3.1.1.	The application for approval of a protective helmet type, without or with one or more visor types, shall be submitted by the helmet manufacturer or by the holder of the manufacturer's name or trade mark or by his duly accredited representative, and for each type the application shall be accompanied by the following:

3.1.1.1.	Drawings in triplicate to a scale of 1:1, in scale with sufficient detail to permit identification of the helmet type, including the methods of assembly. The drawings shall show the position intended for the approval mark as set out in paragraph 5.1.4.1.,

3.1.1.2.	A brief technical specification stating the materials used and a test report of the photometric and colorimetric performance of the retroreflective material.

3.1.1.3.	If the helmet is fitted with one or more visors:

3.1.1.3.1.	Drawings in triplicate to a scale of 1:1, in scale with sufficient detail to permit identification of the visor type and of its means of attachment to the helmet. The drawings shall show the position intended for the approval mark as set out in paragraph 5.1.4.1.,

3.1.1.3.2.	A technical description of the visor stating the materials used, the manufacturing processes and, where appropriate, the surface treatment,

3.1.1.4.	A number of helmets, with or without visors, out of [20] samples of different sizes, sufficient to enable all the tests specified in paragraph 7.1. to be conducted and one helmet additionally to be retained by the technical service responsible for conducting the approval test.

3.1.1.5.	For each visor type, if any, 7 (+3 if optional test for mist retardant visor is carried out) visors taken from a sample of not less than 14 (+ 6 if optional test) specimens. 6 (+ 3 if optional test) visors shall be subjected to the tests and the seventh (or tenth if optional test) shall be retained by the technical service responsible for conducting the approval test.

3.2.	Application for approval of a visor type

3.2.1.	The application for approval of a visor type shall be submitted by the visor manufacturer or by the holder of the manufacturer's name or trade mark or by his duly accredited representative, and for each type the application shall be accompanied by the following:

3.2.1.1.		Drawings in triplicate to a scale of 1:1, scale with sufficient detail to permit identification of the visor type and of its means of attachment to the helmet. The drawings shall show the position intended for the approval mark as set out in paragraph 5.2.4.1.,

3.2.1.2.	A technical description of the visor stating materials used, the manufacturing processes and, where appropriate, the surface treatment,

3.2.1.3.	List of approved helmet types to which the visor may be fitted,

3.2.1.4.	For each visor type, if any, 7 (+3 if optional test for mist retardant visor is carried out) visors taken from a sample of not less than 14 (+ 6 if optional test) specimens and the helmets to which the visors are intended to be fitted.

6 (+ 3 if optional test) visors shall be subjected to the tests and the seventh (or tenth if optional test) shall be retained by the technical service responsible for conducting the approval test.

3.3.	The competent authority shall verify the existence of satisfactory arrangements in order to ensure effective control of the conformity of production in accordance with the provisions of paragraph 10. and annex 12 before type approval is granted.

4.		Markings

4.1.	The protective helmets submitted for approval in conformity with paragraph 3.1. above shall bear:

4.1.1.	On the helmet, the applicant's trade name or mark, an indication of the size (in letter and cm), the year of production and, if appropriate, an indication of the unsuitability of the lower face cover to offer any protection against impacts to the chin.

4.1.2.	On the visor, the applicant’s trade name or mark and, if appropriate, an indication of the unsuitability of the visor for use during the hours of darkness or in conditions of poor visibility.

4.2.	The visors submitted for approval in conformity with paragraph 3.2. above shall bear the applicant's trade name or mark and, if appropriate, an indication of the unsuitability of the visor for use during the hours of darkness or in conditions of poor visibility.

4.3.	The marking shall not be placed within the main visibility area.

4.4.	The marking shall be indelible, clearly legible and in readily accessible place.

5.		Approval

5.1.	Approval of a protective helmet type, without or with one or more visor types

5.1.1	If the protective helmets and the visors, if any, submitted in pursuance of paragraph 3.1.1.4. above meet the requirements of this Regulation, approval shall be granted.

5.1.2.	An approval number shall be assigned to each type approved. Its first two digits (at present 05 06) shall indicate the series of amendments incorporating the most recent major technical amendments made to the Regulation at the time of issue of the approval. The same Contracting Party shall not assign the same number to another helmet type covered by this Regulation.

5.1.3.	Notice of approval or of extension or refusal or withdrawal of approval or production definitely discontinued of a protective helmet type, without or with one or more visor types pursuant to this Regulation shall be communicated to the Parties to the 1958 Agreement applying this Regulation, by means of a form conforming to the model in annex 1 A to this Regulation.

5.1.4.	In addition to the marks described in paragraph 4.1.1. above, the following particulars shall be indicated on every protective helmet conforming to a type approved under this Regulation by means of the labels referred to in paragraph 5.1.9. below:

5.1.4.1.	An international approval mark consisting of:

5.1.4.1.1.	A circle surrounding the letter "E" followed by the distinguishing number of the country which has granted approval, :

5.1.4.1.2.	The approval number followed by:

5.1.4.1.2.1.	a slash and symbol:

"J" if the helmet does not have a lower face cover

"P" if the helmet has a protective lower face cover,

"NP" if the helmet has a non protective lower face cover

"P/J" if the helmet has a detachable or movable protective lower face cover as a combination of two codes of protection.

5.1.4.1.2.2.	a dash followed by a production serial number. The production serial numbers shall be continuous for all protective helmets of the same type approved, and each authority shall keep a register from which it can check that the type and production serial numbers correspond.

5.1.4.1.3.	The marking and/or symbol denoting the unsuitability of the lower face cover, if appropriate.

5.1.4.1.4.	The marking on the helmet and, if appropriate, lower face cover shall be clearly legible, indelible and resistant to wear.

5.1.4.1.5.		The label can also include, not in alternative, a bar or QR code for digital reading.

5.1.5.	In addition to the marks described in paragraph 4.1.2. above, the following particulars shall be affixed visibly and in a readily accessible place to every visor, if any, conforming to a type approved with a helmet under this UN Regulation:

5.1.5.1.	An international approval mark consisting of:

5.1.5.1.1.	A circle surrounding the letter "E" followed by the distinguishing number of the country which has granted approval,

5.1.5.1.2.	The approval number followed by:

5.1.5.1.2.1.	a dash followed by a production serial number. The production serial numbers shall be continuous for all protective helmets of the same type approved, and each authority shall keep a register from which it can verify that the type and production serial numbers correspond.

5.1.5.1.3.	The symbol denoting daytime use only, if appropriate.

5.1.6.	The marking on the visor shall be clearly legible, indelible and resistant to wear.

Note: A ultradistructive label can also be an acceptable marking on the visors.

5.1.7.	The marking on the visor shall not be placed within the main visibility area.

5.1.8.	The approval marks prescribed in paragraphs 5.1.4., 5.1.5. and 5.2.4. above may not be replaced by a Unique Identifier (UI) as referred to in Schedule 5 of the 1958 Agreement.

5.1.9.	Annex 2 A to this Regulation gives examples of the arrangements of the approval marks for protective helmets and visors.

5.1.10.	In order to be considered as approved under this Regulation, subject to the provisions of paragraph 9. below, every protective helmet shall bear, sewn to its retention system, one of the labels referred to in paragraph 5.1.4. above. A different method of securing the label is authorized if it complies with the above provisions.

5.1.11.	The labels referred to in paragraph 5.1.9. above may be issued either by the authority which has granted the approval or, subject to that authority's authorization, by the manufacturer.

5.1.12.	The label referred to in paragraph 5.1.9. above shall be clearly legible and resistant to wear.

5.1.13.	Approval of helmets of size 48/49 shall be granted without additional tests if such helmets belong to a type already approved which comprises size 50 in its range of sizes.

5.1.14.	Approval of helmets larger than size 62 shall be granted without additional tests if such helmets belong to a type already approved which comprises size 62 in its range of sizes.

5.2.	Approval of a visor type

5.2.1.	Where the visors submitted in accordance with paragraph 3.2.1.4. above meet the requirements of paragraphs 6.15. and 7.8. of this UN Regulation, approval shall be granted.

5.2.2.	An approval number shall be assigned to each type approved. Its first two digits (at present 06) shall indicate the series of amendments incorporating the most recent major technical amendments made to the Regulation at the time of issue of the approval. The same Contracting Party shall not assign the same number to another visor type covered by this Regulation.

5.2.3.	Notice of approval or of extension or refusal or withdrawal of approval or production definitely discontinued of a visor type pursuant to this Regulation shall be communicated to the Parties to the 1958 Agreement applying this Regulation, by means of a form conforming to the model in annex 1 B to this Regulation.

5.2.4.	In addition to the marks prescribed in paragraph 4.2. above, the following particulars shall be affixed visibly and in a readily accessible place to every visor conforming to a type approved under this UN Regulation:

5.2.4.1.	An international approval mark consisting of:

5.2.4.1.1.	the approval symbol described in paragraph 5.1.4.1.1.,

5.2.4.1.2.	the approval number,

5.2.4.1.3.	a production serial number. The production serial numbers shall be continuous for all visors of the same type approved, and each authority shall keep a register from which it can check that the type and production serial numbers correspond.

5.2.4.1.4.	the symbol denoting daytime use only, if appropriate.

5.2.5.	The approval mark shall be clearly legible, indelible and resistant to wear.

Note: A ultradistructive label can also be an acceptable marking on the visors.

5.2.6.	The marking shall not be placed within the main visibility area.

5.2.7.	Annex 2 B to this Regulation gives an example of the arrangement of approval mark for a visor.

6.		General specifications

6.1.	The basic construction of the helmet shall be in the form of a hard outer shell, containing additional means of absorbing impact energy, and a retention system.

6.2.	The protective helmet may be fitted with ear flaps and a neck curtain.

6.2.1.	It may also have a detachable peak, a visor and an additional sun shield and, if is the case, electronic equipment or accessories.

6.2.2.	The protective helmet may be fitted with ear flaps and a neck curtain. It may also have a fixed, detachable or movable lower face cover. If fitted with a not protective lower face cover the outer surface of the cover shall be marked "Does not protect chin from impacts" and/or with the symbol shown in figure 1 below indicating the unsuitability of the lower face cover to offer any protection against impacts to the chin.

Figure 1
Symbol "Does not protect chin from impacts"

Note: this symbol or indication must visible and extend over at least 2 cm2

6.3.	No component or device may be fitted to or incorporated in the protective helmet unless it is designed in such a way that it will not cause injury and that, when it is fitted to or incorporated in the protective helmet, the helmet still complies with the requirements of this Regulation.

6.4.	The extent of the protection provided shall be as follows:

6.4.1.	The shell shall cover all areas above plane AA' and shall extend downwards at least as far as the lines CDEF on both sides of the headform (see annex 4, fig. 1 A).

6.4.2 	At the rear, the rigid parts and, in particular, the shell shall not be within a cylinder defined as follows (see annex 4, fig. 1 B):

(a)	Diameter 100 mm;

(b)	Axis, situated at the intersection of the medium plane of symmetry of the headform and of a plane parallel to and 110 mm below the reference plane.

6.4.3. 	The protective padding shall cover all the areas defined in paragraph 6.4.1., account being taken of the requirements of paragraph 6.5.

6.5.	The helmet shall not dangerously affect the wearer's ability to hear.	The temperature in the space between the head and the shell shall not rise inordinately; to prevent this, ventilation holes may be provided in the shell.

Where means for attaching a visor are not provided, the profile at the front edge shall not prevent the wearing of goggles.

6.6.	All projections from or irregularities in the outer surface of the shell greater than 2 mm shall be tested for shear assessment according to paragraphs 7.4.1. or 7.4.2. The outer surface of the helmet shall be tested for friction assessment according to paragraphs 7.4.1. or 7.4.2.  This applies in particular to a movable lower face cover in all positions intended by the manufacturer.

6.7.	All external projections shall be radiused and any external projections other than press-fasteners shall be smooth and adequately faired.

6.7.1.	All external projections not more than 2 mm above the outer surface of the shell (e.g. rivet heads) shall have a radius of a minimum of 1 mm.

6.7.2.	All external projections more than 2 mm above the outer surface of the shell shall have a radius of a minimum of 2 mm.

The latter specific requirements shall not apply if a projection satisfies the requirements in paragraphs 7.4.1. or 7.4.2. below.

6.8.		There shall be no inward-facing sharp edges on the inside of the helmet; rigid, projecting internal parts shall be covered with padding so that any stresses transmitted to the head are not highly concentrated.

6.9.	The various components of the protective helmet, shall be so assembled that they are not liable to become easily detached as a result of an impact.

In the case of visor and movable or detachable lower face cover, only when in not protective position, the detachment is acceptable provided that it is complete and not to cause possible injuries to the user.

6.10.	Retention systems shall be protected from abrasion.

6.11.	The helmet shall be held in place on the wearer's head by means of a retention system which is secured under the lower jaw. All parts of the retention system shall be permanently attached to the system or to the helmet.

6.11.1.	If the retention system includes a chin-strap, the strap shall be not less than 20 mm wide under a load of 150 N ± 5 N applied under the condition prescribed in paragraph 7.6.2.

6.11.2.	The chin strap shall not include a chin-cup.

6.11.3.	Chin straps shall be fitted with a device to adjust and maintain tension in the strap.

6.11.4.		Chin strap fastening and tensioning devices shall be positioned on the straps either so that there are no rigid parts extending more than 130 mm vertically below the headform reference plane with the helmet mounted on the appropriate sized headform, or so that the whole of the device is between the bony projections of the underside of the lower jaw.

6.11.5.	If the retention system includes either a double-D ring or sliding bar fastening device then means shall be provided to prevent the retention system being completely undone and also to retain the free end of the strap when the retention system is adjusted.

Retaining systems using closing rings ("double D") or a "roller buckle" shall be conceived to prevent the total opening of the system and to maintain the strap in the desired position once the retaining system has been adjusted.

If the retaining system can be opened completely, it must be possible only with voluntary action. To prevent any possible misuse the helmet must be provided with detailed instructions on the use of the buckle.

6.11.6.	Sliding bar and double-D ring fastening devices shall be fitted with a pulling flap to be used for releasing the retention system. Its color must be red and its minimum dimensions must be 10 x 20 mm.

6.11.7 	If a retention system includes a quick-release mechanism, then the method of release of this mechanism shall be self-evident. Any levers, tabs, buttons or other components which need to be operated to release the mechanism shall be colored red, those parts of the rest of the system which are visible when closed shall not be similarly colored, and the mode of operation shall be permanently indicated.

6.11.8.	The retention system shall remain closed when the tests described in paragraphs 7.3., 7.6. and 7.7. are carried out.

6.11.9.	The buckle of the retention system shall be designed so as to preclude any possibility of incorrect manipulation.	This means, inter alia, that it must not be possible for the buckle to be left in a partially closed position.

Note: in the case of a buckle that allows multiple hooking positions, it shall be tested in the worst-case configuration.

6.12.	If the lower face cover is detachable or movable, the lower face cover shall be fitted with a device that maintains the intended position even during the complete series of impacts and retention (detaching) test. The device must be such that incorrect handling is impossible. The control/actuating device must be of red colour. The helmet must comply with the requirements for helmet categories "J","P" or both.

6.13.	The characteristics of the materials used in the manufacture of helmets shall be known not to undergo appreciable alteration under the influence of ageing, or of the circumstances of use to which the helmet is normally subjected, such as exposure to sun, extremes of temperature and rain. For those parts of the helmet coming into contact with the skin, the materials used shall be known not to undergo appreciable alteration through the effect of perspiration or of toilet preparations. The manufacturer shall not use materials known to cause skin troubles. The suitability of a proposed new material shall be established by the manufacturer.

6.14.	After the performance of one of the prescribed tests, the protective helmet shall not exhibit any breakage or deformation dangerous to the wearer.

Note: As example visor sunshield and shell significant cracks or any part partially detached (spoiler, lower face cover, accessories) that can hurt the user while he’s rolling on the road.

6.15.	Peripheral vision

6.15.1.	To carry out the test, the technical service shall select from among the existing sizes of a helmet type the size it considers likely to yield the least favorable result;

6.15.2.	The helmet shall be placed on the headform corresponding to its size by the procedure set out in annex 5 to this Regulation;

6.15.3.	In the above conditions there shall be no occultation in the field of vision bounded by: (see annex 4, figs. 2A,2B,2C and 2D)

6.15.3.1.	Horizontally:	two segments of dihedral angles symmetrical in relation to the median longitudinal vertical plane of the headform and situated between the reference and the basic planes.

Each of these dihedral angles is defined by the median longitudinal vertical plane of the headform and the vertical plane forming an angle of not less than 105° with the median longitudinal vertical plane and whose edge is the straight line LK;

6.15.3.2.	Upwards:	a dihedral angle defined by the reference plane of the headform and a plane forming an angle of not less than 7° with the reference plane and whose edge is the straight line L1 L2, the points L1 and L2 representing the eyes;

6.15.3.3.	Downwards:	a dihedral angle defined by the basic plane of the headform and a plane forming an angle of not less than 45° with the basic plane and whose edge is the straight line K1 K2.

However, this downward clearance makes specific allowance for breath deflectors.

The breath deflector allowance is shown in Annex 4 fig. 2D. It includes the region that is within 31 mm to the right and left of the longitudinal plane and that lies below the two planes that form 45º angles with the longitudinal plane and that intersect it at the level of the 6 mm below the basic plane.

6.16.	Visors

6.16.1.	The systems of attachment of a visor to a helmet shall be such that the visor is removable. It must be possible to manoeuvre the visor out of the field of vision with a simple movement of one hand. However, the latter prescription may not be required for helmets which do not provide chin protection provided that a label is attached to the helmet to the effect of warning the purchaser that the visor cannot be manoeuvred.

6.16.2.	Angle opening (see annex 9)

6.16.3.	Field of vision

6.16.3.1. 	The visor shall not comprise any part liable to impair the user's peripheral vision as defined in paragraph 6.14. when the visor is in the totally opened position. Furthermore, the lower edge of the visor shall not be situated in the downward field of vision of the user as defined in paragraph 6.14. when the visor is in closed position. The surface of the visor in the peripheral field of vision of the helmet may however include:

(i)	The lower edge of the visor, provided that it is made of a material with at least the same transmittance as the rest of the visor,

(ii)	A device to allow the visor to be manoeuvred or locked in close position. However, if this device is situated within the field of vision of the visor defined in paragraph 6.16.3.2. below it shall be at the lower edge and present a maximum height (h) of 10 mm and its width (l) shall be such that the product (h x l) at the most is equal to [1.5 cm2 ], moreover if bigger it must be made of a material with at least the same transmittance as the visor and it must be free of any engraving, paint or other covering feature,

(iii)	Fixings and devices to allow the visor to be manoeuvred if they are situated outside of the field of vision of the visor and if the total surface of these parts, including devices, if any, to allow the visor to be manoeuvred does not exceed 2 cm2, possibly distributed on each side of the field of vision.

6.16.3.2.	The field of vision of the visor is defined by:

(a)	A dihedron defined by the reference plane of the headform and a plane forming an angle of at least 7° upwards, its edge being the straight line L1 L2, with points L1 and L2 representing the eyes,

(b)	Two segments of dihedral angles symmetrical to the median vertical longitudinal plane of the headform. Each of these dihedral angles is defined by the median vertical longitudinal plane of the headform and the vertical plane forming with this plane an angle of 90°, its edge being the straight line LK,

(c)	and the lower edge of the visor.

6.16.3.3.	To determine the field of vision as defined in paragraph 6.16.3.2. above, the helmet fitted with the visor being tested shall be placed on a test headform of suitable size in accordance with the provisions of paragraph 7.3.1.3.1., with the helmet tipped towards the rear as specified in paragraph 7.3.1.3.1. and the visor placed in the closed position.

6.16.3.4.	Visors shall have a luminous transmittance τv   ≥ 80per cent , relative to the standard illuminant D65. A luminous transmittance 80per cent  > τv   ≥ 35 per cent , measured by the method given in paragraph 7.8.3.2.1.1., is also permissible if the visor is marked with the symbol shown in figure 2 and/or with the English words "DAYTIME USE ONLY".

When describing the transmittance properties of photochromic, liquid crystal or equivalent visors, two values as to be considered: one corresponds to the faded state, the other to the darkened state. The visor shall be classified according to the darkened state. The luminous transmittance shall be measured before the abrasion test.

Figure 2
Symbol "Daytime use only"

Note: this symbol or indication must visible and extend over at least 1 cm2

6.16.3.5.	Visors shall be free from any significant defects likely to impair the vision, such as bubbles, scratches, inclusions, dull spots, holes, mould marks, scratches or other defects originating from the manufacturing process in the field of vision. The light diffusion shall not exceed the limit in accordance with paragraph 7.8.3.2.1.2. when measured in accordance with one of the methods specified in annex 11.

If different results arise when this is assessed, the requirements on scattered light shall be measured and assessed over an area 5 mm in diameter which includes the presumed error. In addition, the regular transmittance shall not deviate by more than ± [5] per cent from the reference value, measured in one of two sight points specified in paragraph 6.16.3.8., at any point within the field of vision of the visor.

6.16.3.6. 	Visors shall in addition be sufficiently transparent, shall not cause any noticeable distortion of object as seen through the visor, shall be resistant to abrasion, resistant to impact and shall not give rise to any confusion between the color used in road traffic sign and signals. The relative visual attenuation quotient (Q) shall not be less than:

0.80 for red signal light;

0.60 for yellow signal lights;

0.60 for green signal light;

0.40 0.60 for blue signal light.

The relative attenuation quotient shall be measured by the method given in paragraph 7.8.3.2.1.1., before the abrasion test.

Note:	When calculating the value of Q from the spectral measurements, the value in annex 14 shall be used. Linear interpolation of these values for steps smaller than 10 nm is permissible.

6.16.3.7.	In the range 500 475 nm to 650 nm, the spectral transmittance, measured by the method given in paragraph 7.8.3.2.1.1., of the visor shall not be less than 0.2 τv. The spectral transmittance shall be measured before the abrasion test.

6.16.3.8. 	The table contains the permissible refractive powers at the sight points. The sight points are located in the reference plane 32 mm to the right and the left of the longitudinal median plane (see fig. 2B).

Permissible refractive power values for visors

| Spherical effect | Astigmatic effect |  |  | Prismatic effect difference |
| --- | --- | --- | --- | --- |
| (D1 + D2)/2 m-1 | ¦ D1 - D2 ¦ m-1 | Horizontal |  | Vertical cm/m |
|  |  | Base Out cm/m | Base In cm/m |  |
| ± 0.12 | 0.12 | 1.00 | 0.25 | 0.25 |

# D1, D2:	Refractive effect in two main sectors

The requirements for the prismatic effect apply to the difference between the values at the two sight points.

The refractive powers shall be measured according to method

specified in Annex 15.

6.16.3.9.	Mist retardant visor (Optional requirements)

The internal face of the visor is regarded as having a mist retardant facility if the square of the specular transmittance has not fallen below 80 per cent of the initial value without misting within 20 s when tested as described in annex 16. Such facility may be indicated by the English words "MIST RETARDANT".

6.17. 	Sun shield

6.17.1. 	Sun shield shall not restrain or prevent the movement of the visor. On opening the visor, the sun shield can pivot in the working position.

By means of a simple movement the sun shield shall be able to be moved separately from the visor out of the visual field.

6.17.2.	Field of vision

6.17.2.1.	Sun shield shall not restrict the field of vision given in paragraph 6.15. in the working or parking position. If the sun shield is fixed outside of the visor, the surface may include fixings or devices to make movement possible. The total surface of the fixings or devices shall not exceed 2cm²; they can be distributed on both sides of the field of vision.

6.17.2.2.	Sun shield shall have a luminous transmittance τv >20 per cent, relative to the standard illuminant D65.

6.17.2.3.	Sun shield shall be free from any significant defects likely to impair the vision, such as bubbles, scratches, inclusions, dull spots, holes, mould marks, scratches or other defects originating from the manufacturing process in the field of vision.

6.17.2.4.	Sun shield shall not cause any noticeable distortion of object as seen through the visor, resistant to impact and shall not give rise to any confusion between the colour used in road traffic sign and signals. The relative visual attenuation quotient (Q) shall not be less than:

0.80 for red signal light;

0.60 for yellow signal lights;

0.60 for green signal light;

0.60 for blue signal light.

The relative attenuation quotient shall be measured by the method given in paragraph 7.8.3.2.1.1.

6.17.2.5.	In the range 475 nm to 650 nm, the spectral transmittance, measured by the method given in paragraph 7.8.3.2.1.1., of the visor shall not be less than 0.2 τv

6.17.2.6.	The table contains the permissible refractive powers at the sight points. The sight points are located in the reference plane 32 mm to the right and the left of the longitudinal median plane (see fig. 2B).

Permissible refractive power values for sun shields; measured without a combination with the visor.

| Spherical effect | Astigmatic effect | Prismatic effect difference |  |  |
| --- | --- | --- | --- | --- |
| (D1 + D2)/2 m-1 | ¦ D1 - D2 ¦ m-1 | Horizontal |  | Vertical cm/m |
|  |  | Base Out cm/m | Base In cm/m |  |
| ± 0.12 | 0.12 | 1.00 | 0.25 | 0.25 |

D1, D2:	Refractive effect in two main sectors

The requirements for the prismatic effect apply to the difference between the values at the two sight points.

The refractive powers shall be measured according to method specified in Annex 15.

6.18.		Conspicuity marking

6.18.1.	General

In order to comply with national requirements for use, the helmet may be required by individual Contracting Parties to contribute to the conspicuity of the user both during the daytime and at night:

from the front;

from the rear;

from the right;

from the left

by means of parts made of reflective materials which conform to

the specifications laid down in paragraphs 6.16.2. to 6.16.6. of

this Regulation.

It is allowed that the helmet is equipped with reflective materials on the box, with proper indications to the user on where and how to apply them on the helmet.

Note:	The mandating of conspicuity marks is left to the discretion of individual Contracting Parties.	Article 3 of the Agreement to which this Regulation is annexed shall not prevent the Contracting Parties from prohibiting the use of helmets not meeting the conspicuity requirements.

6.18.2.	Reflective parts

6.18.2.1.	Geometry

The total surface area and shape of the reflective part used shall be such that in each direction, corresponding to one of the areas defined in the figure below, visibility is ensured by a surface area of at least 18 cm2 of simple shape and measured by application on a plane.

In each surface area of minimum 18 cm2 it shall be possible to mark:

either a circle of 40 mm diameter;

or, a rectangle at least 12.5 cm2 in surface area and at least

20 mm in width.

Each of these surfaces shall be situated as near as possible to the point of contact with the shell of a vertical plane parallel to the longitudinal vertical plane of symmetry, to the right and to the left, and as near as possible to the point of contact with the shell of a vertical plane perpendicular to the longitudinal plane of symmetry, to the front and to the rear.

6.18.3.	Colorimetric test

Each of the retroreflective areas shall emit white light when it is illuminated with a standard illuminant A, with an observation angle of 1/3° and an illumination angle β1 = β2 = 0°  (or β1 = ± 5°, β2 = 0°); in other words: the color value chart "x" and "y" of the reflected light shall lie within the zone specified below:

White:

limit towards blue	x ≥  0.310

limit towards yellow	x ≤  0.500

limit towards green	y ≤  0.150 + 0.640x

limit towards green	y ≤  0.440

limit towards purple	y ≥  0.050 + 0.750x

limit towards red	y ≥  0.382

6.18.4.	Photometric test

The minimum value of the luminous intensity coefficient of a surface area of 18 cm2 of material when revolved shall not be less than the values specified in the table below, expressed in millicandelas per lux.

| Angle of Divergence | Angle of Illumination |  |  |
| --- | --- | --- | --- |
|  | 0° | 20° | 40° |
| 20' | 100 | 60 | 25 |

6.18.5.	Resistance to external agent

After each conditioning as described in paragraph 7.2., the helmet shall be visually inspected.	There shall be no signs of cracking or appreciable distortion of the retroreflective material.

6.18.6.	Compatibility of materials

Neither the adhesive nor the retroreflective material shall affect the mechanical performance of the helmet according to the related tests in the present Regulation.

7.		Tests

7.1.	Each helmet type, fitted with its visor if placed on the market with a visor, shall be conditioned as shown below.

| Test | Number of helmets to be conditioned |  |  |  | Total |
| --- | --- | --- | --- | --- | --- |
|  | ambient-temperature and hygrometry conditioning | Heat conditioning | low-temperature conditioning | ultra-violet radiation conditioning and moisture conditioning |  |
| Impact absorption | 2 | 1 | 1 | 1 | 5 |
| Imp. Abs. extra point | 2 |  |  |  | 2 |
| Hi/Low energy impact | 2 |  |  |  | 2 |
| Rotational | 2 |  |  |  | 2 |
| Projection and surface friction | 1 |  |  |  | 1 |
| Rigidity | 2 |  |  |  | 2 |
| Retention system | 1 |  |  |  | 1 |
|  |  |  |  |  | 15 |

**The largest size of each helmet type The largest size of each combination shell size and protective padding of each helmet type shall be tested for impact absorption, rotational and rigidity. For impact absorption on extra point, Hi and Low energy impacts and tests of the retention system, helmet sizes shall be chosen such that the helmet to be tested shall be that offering the likely least favorable conditions (such as thickest padding, etc).

All the types of retention systems available for the helmet must be tested. Supplementary samples could be necessary.

Additionally, for each smaller headform size within the size range of the helmet type two helmets shall undergo the impact absorption test. One helmet shall be heat conditioned, and the other low temperature conditioned. The conditioned helmets shall be impacted against either anvil, in equal numbers if possible, at the choice of the laboratory.

7.2.	Types of conditioning

Prior to any type of further conditioning for mechanical tests, as specified in paragraph 7.1., each helmet shall be subject:

7.2.1. 		Solvent conditioning

Take a cotton cloth approximately 150 mm square and a quantity approximately 25 ml of a solvent consisting of test liquid B in accordance with ISO 1817:1985 4/. Using the cloth soaked in the solvent, apply the solvent to all those regions of the outside surface of the helmet within 50 mm of the chin strap fixings, and keep these regions wet with the solvent for (7.5 ± 2.5) s. Repeat the procedure on the remainder of the external surface including any chin guard, keeping these regions wet for (12.5 ± 2.5) s. Do not carry out any further conditioning or testing during the following 30 min.

7.2.1.	Ambient-temperature and hygrometry conditioning

The helmet shall be exposed to a temperature of 25 °C ± 5 °C and a relative humidity of 50 per cent ± 10 per cent for at least 4 hours.

7.2.2.	Heat conditioning

The helmet shall be exposed to a temperature of 50 °C ± 2 °C for not less than 4 hours and not more than 6 8 hours.

7.2.3.	Low-temperature conditioning

The helmet shall be exposed to a temperature of – 20 -10 °C ± 2 °C for not less than 4 hours and not more than 6 hours.

7.2.4.	Ultraviolet-radiation conditioning and moisture conditioning. The outer surface of the protective helmet shall be exposed successively to:

7.2.4.1.		ultraviolet irradiation by a 125 150-watt xenon-filled quartz lamp for 48 hours at a range of 25 cm;

7.2.4.2.	spraying for 4 to 6 8 hours with water at ambient temperature at the rate of 1 litre per minute.

7.3.	Linear Impact – energy absorption tests

7.3.1.	Description of test

7.3.1.1.	Principle

Impact absorption capacity is determined by recording against time the acceleration imparted to a headform fitted with the helmet, when dropped in guided free fall at a specific impact velocity upon a fixed steel anvil.

7.3.1.2.	Marking of points and areas of impact

Before conditioning, the points and areas of impact are marked as indicated in paragraph 7.3.4.2. and annex 4 (fig. 3) and the helmet is positioned in accordance to annex 5.

7.3.1.3.	Positioning of the helmet

After conditioning:

7.3.1.3.1.	The helmet shall be positioned in accordance with the requirements of annex 5 on a headform of appropriate size selected from among those listed in paragraph 7.3.3.1.  When testing impact points B, X, P and R the helmet is tipped towards the rear so that the front edge of the helmet in the median plane is displaced by 25 mm; the retention system is then adjusted under the chin of the headform; if the system includes an adjustable chin strap, the strap is tightened as for "normal use".

"Tightened as for normal use" means that the helmet must be tighten after having applied below the chin a rigid cylinder 10 mm diameter at least 30 mm long that will be removed before the test.

7.3.1.3.1.1.	When testing impact point S on a helmet with a protective lower face cover, the helmeted headform is tipped forwards so that the central vertical axis of the headform is inclined at an angle of 65 ± 3° to the vertical with the vertical longitudinal plane of symmetry of the helmeted headform in the vertical position. If the impact point would be within 15 mm of the rim, the helmeted headform shall be re-positioned so that the impact point is not less than 15 mm from the rim.

7.3.1.3.2.	The test headform shall be so positioned that the designated point on the helmet is vertically above the centre of the anvil. The plane tangential to the point of impact shall be horizontal. This prescription does not apply for the S impact point.

7.3.1.3.3.	Helmets placed on the market with a visor shall be tested with the visor in the closed position.

7.3.1.3.4.	Helmets placed on the market with a sun shield shall be tested with the sun shield in working position.

7.3.1.3.5.	Helmets placed on the market with accessories shall be examined to assess that the supplementary equipment has no adverse effect and that in any case the protective helmet and/or visor still complies with all the requirements.

Note: The evaluation shall be done with and without the accessory and their support with particular attention, as example, to energy absorption, sharp edges and field of vision.

No helmet shall be modified from its original specification as manufactured. Accessories must be fitted in accordance with the helmet manufacturer’s instructions. Only accessories approved by the Authority shall be used. In case of any other modification or addition of non-approved accessories (helmet cameras, visors, communication devices, etc.) the helmet homologation becomes invalid.

7.3.1.4.	Test

The test shall be completed in not more than five minutes after the helmet is taken from the conditioning chamber.

Tests at point S shall be carried out after tests at points B, X, P and R. For the extra point the sequence is up to the technical service.

The drop height impact speed shall be equal to:

7.5 (+ 0.15/- 0.0) m/s for both anvils specified in paragraphs 7.3.2.3.1. and 7.3.2.3.2.

5.5 6.0 (+ 0.15/ -0.0) m/s for tests at point S.

8.2 (+ 0.15/- 0.0) m/s for linear high energy, only flat anvil shall be used

6.0 (+ 0.15/ -0.0) m/s for linear low energy, both anvils may be used.

7.3.1.5.	Measurements

The velocity of the moving mass is measured between 1 cm and 6 cm before impact, to an accuracy of 1 per cent. The acceleration against time at the centre of gravity of the headform is measured and recorded and the Head Injury Criterion (HIC) calculated as prescribed in paragraph 7.3.2.5.

7.3.2.	Apparatus (see annex 8, fig. 1)

7.3.2.1.	Description

The test apparatus shall comprise:

(a)	An anvil rigidly fixed to a base;

(b)	A free fall guidance system;

(c)	A mobile system supporting the helmeted headform;

(d)	A metal headform fitted with a tridirectional accelerometer and a measuring assembly;

(e)	A system by which the point of impact can be brought into correspondence with the centre of the anvil.

7.3.2.2.	Base

The base shall be made of steel or concrete or a combination of these materials and have a mass of at least 500 kg.

It shall be so constructed that there is no significant deformation of the surface under the test load.

No part of the base or anvil shall have a resonance frequency liable to affect the measurements.

7.3.2.3.	Anvils

7.3.2.3.1.	The flat steel anvil shall have a circular impact face of diameter 130 mm ± 3 mm.

7.3.2.3.2.	The kerbstone anvil shall have two sides forming an angle of 105 ± 5°, each of them with a slope of 52.5 ± 2.5° towards the vertical and meeting along a striking edge with a radius of 15 mm ± 0.5 mm. The height must be at least 50 mm and the length not less than 125 mm.

The orientation is 45° to the longitudinal vertical plane at points B, P, R, and extra points, 45° to the base plane at point X (front low, back up).

7.3.2.4.	Mobile system and guides

The mobile system supporting the headform shall be such that its characteristics do not affect the measurement of acceleration at the centre of gravity of the headform. It shall also be such that any point in the area ACDEF can be positioned vertically above the centre of the anvil.

The guides shall be such that the impact velocity is not less than 95 per cent of the theoretical velocity.

7.3.2.5.	Accelerometer and measuring assembly

The accelerometer shall be capable of withstanding a maximum acceleration of 2,000 g without damage.	Its maximum mass shall be 50 grammes. The measuring system, including the drop assembly, shall have a frequency response in accordance with channel frequency class (CFC) 1000 of the International Standard ISO "Road vehicles - Techniques of measurement in impact tests - Instrumentation" (Ref. No. ISO 6487:2015 and updated versions).

The HIC shall be calculated as the maximum (depending from t1 and t2) of the equation:

where 'a' is the resultant acceleration as a multiple of 'g' and t1 and t2 are any two points in time (sec) during the impact. The acceleration data has to be sampled at a frequency of at least 8,000 Hz and filtered in accordance with the latest edition of ISO 6487 (CFC 1000).

7.3.3.	Headforms

7.3.3.1.	The headforms used for the impact-absorption test shall be made of metal and, together with any means for their support, shall exhibit no resonance below a frequency of 3,000 2,000 Hz.

Full headforms shall have the following characteristics:

(a)	the centre of gravity shall be located within a 10 mm radius of point G on the central vertical axis;

(b)	a facility for attaching an accelerometer shall be incorporated such that, with the headform in any angular orientation, the respective sensitive axes of the accelerometer shall pass within 10 mm of point G;

the appropriate mass, as specified in Table below.

7.3.3.2.	The general characteristics of the test headforms to be used shall be as follows:

| Symbols | Circumference (in mm) | Mass (in Kg) |
| --- | --- | --- |
| A | 495 | 3.1 (±0.10) |
| C | 515 | 3.6 (±0.10) |
| E | 535 | 4.1 (±0.12) |
| J | 575 | 4.7 (±0.14) |
| M | 605 | 5.6 (±0.16) |
| O | 625 | 6.1 (±0.18) |

7.3.3.3.	The shape of the test headforms shall be in conformity with the detailed dimensions of the reference headforms shown in annex 6;

7.3.3.4. 	The centre of gravity of the headform shall be near the point G on the central vertical axis at "l" mm below the reference plane, as defined in annex 7. The headform shall contain, near its centre of gravity, a housing for a tridirectional accelerometer.

7.3.3.4.	For tests other than those of impact-absorption, appropriate full headforms complying only with the geometrical provisions of paragraph 7.3.3.3. above, may be used.

Table 1
Correspondence between test headforms and Helmet Sizes.

| Largest Size specified (cm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Smallest Size specified (cm) |  | 50 | 51 | 52 | 53 | 54 | 55 | 56 | 57 | 58 | 59 | 60 | 61 | 62 |
|  | 50 | A | A | C |  |  |  |  |  |  |  |  |  |  |
|  | 51 |  | C | C | C |  |  |  |  |  |  |  |  |  |
|  | 52 |  |  | C | C | E |  |  |  |  |  |  |  |  |
|  | 53 |  |  |  | E | E | E |  |  |  |  |  |  |  |
|  | 54 |  |  |  |  | E | E | E |  |  |  |  |  |  |
|  | 55 |  |  |  |  |  | E | E | J |  |  |  |  |  |
|  | 56 |  |  |  |  |  |  | J | J | J |  |  |  |  |
|  | 57 |  |  |  |  |  |  |  | J | J | J |  |  |  |
|  | 58 |  |  |  |  |  |  |  |  | J | J | M |  |  |
|  | 59 |  |  |  |  |  |  |  |  |  | J | M | M |  |
|  | 60 |  |  |  |  |  |  |  |  |  |  | M | M | M |
|  | 61 |  |  |  |  |  |  |  |  |  |  |  | M | O |
|  | 62 |  |  |  |  |  |  |  |  |  |  |  |  | O |

7.3.4.	Selection of points of impact

7.3.4.1.	Each test shall be carried out with 4 impacts on one helmet on the points B, X, P and R, in this sequence.

When a helmet with a protective lower face cover is being tested then an additional point S shall be impacted after the four other points, but only against the anvil specified in paragraph 7.3.2.3.1.

Other test samples can be used for additional linear impact on extra point.

7.3.4.1.1.	After each impact the helmet shall be re-positioned correctly on the headform prior to the next impact, without interfering with the adjustment of the retention system. Before each impact on the point S the helmet shall be re-positioned correctly on the headform and the retention system adjusted under the chin of the headform; if the system includes an adjustable chin strap, the strap is tightened as much as possible.

7.3.4.2.	The points of impact are defined for each helmet:

B,	in the frontal area, situated in the vertical longitudinal plane of symmetry of the helmet and at an angle of 20° measured from Z above the AA' plane.

X,	in either the left or right lateral area, situated in the central transverse vertical plane and 12.7 mm below the AA' plane.

R,	in the rear area, situated in the vertical longitudinal plane of symmetry of the helmet and at an angle of 20° measured from Z above the AA' plane.

P,	in the centre at the intersection of the central vertical axis and the outer surface of the helmet shell.

S,	in the lower face cover area, situated within an area bounded by a sector of 20° divided symmetrically by the vertical longitudinal plane of symmetry of the helmet.

7.3.4.2.1.	Extra point

At least three further impact tests shall be performed on a helmet sample.

The impact points shall be selected among the 12 points as listed below and depicted in figure.

Impact sites shall be spaced at least 130 mm for A and C headforms, 140 mm for E and J headforms, and 150 mm for M and O headforms.

BP - in the front-superior area, situated in the vertical longitudinal plane of symmetry of the helmet (0º) situated in the vertical plane and at an angle of 45°measured from Z above the AA' plane.

BXL - in the left (315º) front-lateral area, situated in the vertical plane and at an angle of 20°measured from Z above the AA' plane.

BXR - in the right (45º) front-lateral area, situated in the vertical plane and at an angle of 20°measured from Z above the AA' plane.

BXPL - in the left (315º) front-lateral-superior area, situated in the vertical plane and at an angle of 45°measured from Z above the AA' plane.

BXPR - in the right (45º) front-lateral-superior area, situated in the vertical plane and at an angle of 45°measured from Z above the AA' plane.

XPL - in the left (270º) lateral-superior area, situated in the central transverse vertical plane and at an angle of 45°measured from Z above the AA' plane.

XPR - in the right (90º) lateral-superior area, situated in the central transverse vertical plane and at an angle of 45°measured from Z above the AA' plane.

RXL - in the left (225º) rear-lateral area, situated in the vertical plane and at an angle of 20°measured from Z above the AA' plane.

RXR - in the right (135º) rear-lateral area, situated in the vertical plane and at an angle of 20°measured from Z above the AA' plane.

RXPL - in the left (225º) rear-lateral-superior area, situated in the vertical plane and at an angle of 45°measured from Z above the AA' plane.

RXPR - in the right (135º) rear-lateral-superior area, situated in the vertical plane and at an angle of 45°measured from Z above the AA' plane.

RP - in the rear-superior area, situated in the vertical longitudinal plane of symmetry of the helmet (180º) and at an angle of 45°measured from Z above the AA' plane.

Impacts points should be within 10 mm radius of the defined point.

Any other point inside the extent of protection [paragraph 6.4.1.] as particular ventilation holes and/or special features on helmet should be considered.

Impacts at points B, X and R should be within 10 mm radius of the defined point.

7.3.5.	Combination of conditioning and anvils

| Conditioning: | Anvils a/ |
| --- | --- |
| Ambient | Flat and kerbstone |
| Heat | Kerbstone b/ |
| Low temperature c/ | Flat b/ |
| Ultraviolet radiation and moisture | Flat or kerbstone w(to be selected by the laboratory) |

a/ Point S shall only be impacted against the flat anvil.

b/ Only for the largest helmet size. For smaller headforms in the size range of the helmet type either anvil may be used. See paragraph 7.1.

c/ Only each helmet size subjected to low-temperature conditioning shall undergo the impact test at point S.

7.3.6.	The absorption efficiency shall be considered sufficient where the resultant acceleration measured at the centre of gravity of the headform at no time exceeds:

| Type of test | Acceleration | HIC |
| --- | --- | --- |
| Std Linear Impact Std | ≤ 275 g | ≤2 400 |
| Linear Extra Point | ≤ 275 g | ≤2 400 |
| Linear Hi Energy | ≤ 275 g | ≤2 880 |
| Linear Low Energy | ≤180 g | ≤1 300 |

The helmet shall not become detached from the headform.

7.4	Test for projections and surface friction

An appropriate size of helmet shall be subjected to the test described in paragraph 7.4.1. or to the test described in paragraph 7.4.2.

7.4.1.	Test for projections and surface friction (method A)

7.4.1.1.	Description of test

7.4.1.1.1.	Principle

The rotation-inducing forces caused by projections on the helmet and friction against the outer surface of the helmet which occur when a helmeted headform is dropped vertically on to an inclined anvil are measured in the longitudinal axis of the anvil. The peak force and its integral with respect to time over the duration of the positive impulse are used as performance criteria.

7.4.1.1.2.	Selection and positioning of the helmet

7.4.1.1.2.1.	An appropriate size helmet shall be selected to fit the headform referred to in paragraph 7.4.1.2.6. The horizontal axis of the helmet shall be determined by placing the helmet on a headform, of a type referred to in paragraph 7.3.3., according to the requirements of annex 5. The helmet shall then be removed from that headform and placed on a headform of a type referred to in paragraph 7.4.1.2.6. A load of 50 N is applied to the crown of the helmet in order to adjust the helmet on the headform such that there is contact between the crown of the headform and the inner surface of the helmet.

The horizontal plane of the helmet shall then be adjusted to be within 90° ± 5° of the vertical axis of the headform.

The retention system is then adjusted under the chin of the headform; if the system includes an adjustable chin strap, the strap is tightened as much as possible.

7.4.1.1.2.2.	The test headform shall be so positioned that the chosen impact point on the helmet is vertically above the upper part of the face of the anvil.

7.4.1.1.2.3.	The helmet shall be tested in any condition in which it may be placed on the market, that is both with and without accessories if they are supplied as original equipment. Helmets placed on the market with a visor shall be tested with the visor in the closed position.

Helmets of the category "P/J" shall be tested in all the configurations provided by the manufacturer.

7.4.1.1.3.	Test

The drop height shall be such that the unit constituted by the headform and helmet falls on the test anvil at a velocity which, immediately before impact, is equal to 8.5 (-0.0/+0.15) m/s.

7.4.1.2.	Apparatus (see annex 8, fig. 1b)

7.4.1.2.1.	Description

The test apparatus shall comprise:

(a)	An anvil rigidly fixed to a base;

(b)	A free fall guidance system;

(c)	A mobile system supporting the helmeted headform;

(d)	A headform conforming to that referred to in paragraph 7.4.1.2.6., and

(e)	A system which may be adjusted such that the point of impact can be brought into correspondence with the upper part of the face of the anvil.

(f)	A means of recording the continuously changing transmitted anvil force during the impact.

(g)	A suitable energy-absorbing base and catch net to prevent damage to the helmet after the impact.

7.4.1.2.2.	Base

This shall conform to the requirements specified in paragraph 7.3.2.2.

7.4.1.2.3.	Anvil

7.4.1.2.3.1.	The anvil is mounted securely at an angle of 15° to the vertical with provision for fore-and-aft adjustment. The anvil has a minimum width of 200 mm and is adaptable to carry either of two different impact surfaces as follows:

7.4.1.2.3.1.1.	The bar anvil consists of a series of at least 5 horizontal bars at 40 mm centres. Each bar is made from a steel strip of height 6 mm and width 25 mm with its uppermost edge machined to a 1 mm radius and the lower 15 mm of its face chamfered at an angle of 15° so that, as mounted, the upper edge of each bar is fully exposed from vertically above. The bars are

case-hardened to a depth of approximately 0.5 mm.

The bar anvil should be used to assess the tangential forces and their integrals with time caused by projections on the helmet, e.g. visor fittings, screws, press studs and steps in the shell surface, etc.

7.4.1.2.3.1.2.	The abrasive anvil is a sheet of grade 80 closed-coat aluminium oxide abrasive paper with a minimum supported length of 225 mm and is securely clamped to the base of the anvil to prevent slippage.

The abrasive anvil should be used to assess the tangential forces and their integrals with time caused by friction against the outer surface of the helmet. This is particularly applicable to selected areas of helmets, the outer surface of which either have significant variations of curvature or are made of more than one material.

7.4.1.2.3.2.	The anvil is fitted with force transducer(s) connected to recording apparatus so that the transmitted longitudinal force component can be measured and continuously recorded with an accuracy of ± 5 per cent during a glancing blow to any part of its exposed surface.

7.4.1.2.4.	Mobile system and guides

The mobile system supporting the headform shall be such that its characteristics do not affect the measurement of force in the anvil. It shall also be such that any point on the helmet can be positioned vertically above the anvil. The guides shall be such that the impact velocity is not less than 95 per cent of the theoretical velocity.

7.4.1.2.5.	Force and measuring assembly

The force transducers fitted to the anvil shall be capable of withstanding a maximum force of 20,000 N without damage.	The measuring system including the anvil assembly shall have a frequency response in accordance with channel frequency class (CFC) 1000 of the International Standard ISO "Road vehicles - Techniques of measurement in impact tests - Instrumentation".

7.4.1.2.6.	Headform

The headform shall be that referred to in paragraph 7.3.3. characterized by the symbol J.

7.4.1.3.	Selection of impact points

Any point on the helmet may be selected. The impact point should be selected with regard to the anvil against which the helmet is to be tested, taking into account the function of the anvils given in paragraphs 7.4.1.2.3.1.1. and 7.4.1.2.3.1.2. The helmet shall be tested as many times as necessary to ensure that all notable features are evaluated.

When the abrasive anvil is used, evaluate the front, rear, sides and crown areas of the helmet, selecting within these general areas, sites on the outer surface which are likely to produce the greatest force and/or the greatest impulse where impulse is the integral of force with respect to time over the duration of the impact. Examples of such areas are those having the greatest radius of curvature (i.e. the flattest surface) or areas having more than one type of surface, for example a visor fixing cover plate or a painted shell partially overlaid by a fabric cover.

Note: The primary impact site on any projection is likely to be opposite to the site where the projection receives maximum support. For example, the primary impact site on a visor cover plate assembly is opposite to the area where the visor and cover plate locates in a recess in the shell.

When the abrasive anvil is used, evaluate the front, rear sides and crown areas of the helmet, selecting within the general areas, sites on the outer surface which are likely to produce the greatest force and/or the greatest impulse where impulse is the integral of force with respect to time over the duration of the impact. Examples of such areas are those having least curvature or areas having more than one type of surface finish, for example a painted shell partially overlaid by a fabric cover.

The rim of the shell and the upper and lower edge of the visor situated within an area bounded by a sector of 120° divided symmetrically by the vertical longitudinal plane of symmetry of the helmet do not constitute a projection for the purpose of this test.

7.4.1.4.	Requirements

7.4.1.4.1.	When tested against the bar anvil the helmet shall satisfy the following requirements:

7.4.1.4.1.1.	the peak longitudinal force measured on the anvil shall not exceed 2,500 N, nor shall its integral with respect to time over the duration of the impact exceed 12.5 Ns for any of the selected impact points.

7.4.1.4.2.	When tested against the abrasive anvil, a second helmet shall satisfy the following requirements:

7.4.1.4.2.1.	the peak longitudinal force measured on the anvil shall not exceed 3,500 N, nor shall its integral with respect to time over the duration of the impact exceed 25 Ns for any of the selected impact points.

7.4.2.	Test for projections and surface friction (method B)

7.4.2.1.	Description of test

7.4.2.1.1.	Principle

The rotation-inducing forces caused by projections on the helmets and friction against the outer surface of the helmets are assessed firstly by a shear impact on the projections using a shear edge against which the projections shall

shear away, be detached, or permit the shear edge to slide past the projections. The friction is assessed by the displacement of a carriage abrading the outer surface of the helmet. The shear impact and abrading carriage displacement are generated by a drop weight device.

7.4.2.1.2.	Positioning of the helmets

7.4.2.1.2.1.	The helmet is placed on a headform of appropriate size in accordance with the requirements of annex 5. The helmet is tipped towards the rear so that the front edge of the helmet in the median plane is displaced by 25 mm; if the helmet includes an adjustable chin strap, the strap shall be tightened as much as possible. The headform shall be so positioned that the chosen location on the helmet can be positioned in contact with the upper surface of the horizontal carriage.

7.4.2.1.2.2.	The helmet shall be tested in any condition in which it may be placed on the market, that is both with and without accessories if they are supplied as original equipment. Helmets placed on the market with a visor shall be tested with the visor in the closed position.

Helmets of the category "P/J" shall be tested in all the configurations provided by the manufacturer.

7.4.2.1.3.	Test

7.4.2.1.3.1.	Test of projection

The headform is adjusted in order to have the chosen projection on the carriage so that the shear edge is positioned 50 mm from the projection and makes lateral contact with the projection after the drop weight is released from its upper position.

7.4.2.1.3.2.	Test of outer surface

The abrasive paper is mounted on the carriage in the position specified in paragraph 7.4.2.2.2.	The chosen outer surface of the helmet is lowered on to the abrading carriage at the centre of the

flat surface without abrasive paper. A loading mass is applied in accordance with paragraph 7.4.2.2.8. The drop weight is released from its upper position in accordance with paragraph 7.4.2.2.5. The abrasive paper shall be changed after every test.

7.4.2.2.	Apparatus (a suitable apparatus is illustrated in annex 8, figure 1c)

7.4.2.2.1.	Description

The test apparatus shall comprise:

(a)	A horizontal guided carriage with interchangeable attachments for abrasive paper or a shear edge;

(b)	A horizontal guide and support for this carriage;

(c)	A roller with a wire rope or a strap or a similar flexible connection;

(d)	A lever connecting the headform to the test apparatus with a hinge;

(e)	An adjustable system supporting the headform;

(f)	A drop weight to load the lower end support of the wire rope, or a strap, after the weight is released;

(g)	A system to support a headform and to apply a force to the helmet normal to the carriage.

7.4.2.2.2.	Carriage

For friction assessment the carriage bears a sheet of grade 80 closed-coat aluminium oxide abrasive paper with a supported length of 300.0 (- 0.0/+ 3.0) mm and securely clamped to the carriage to prevent slippage. At its end towards the drop weight and in this direction the carriage has a 80 mm ± 1 mm long smooth steel area not being covered by the abrasive paper and higher than the rest of the carriage by the thickness of the abrasive paper plus 0.5 ± 0.1 mm.

For shear assessment the carriage is provided in the middle, with a bar made from a steel strip of height 6 mm and width

25 mm with its uppermost edges machined to a 1 mm radius. The bar is case-hardened to a depth of approximately 0.5 mm.

The carriage and either attachment shall have a total mass of 5.0 (- 0.2/+ 0.0) kg.

7.4.2.2.3.	Horizontal guide

The horizontal guide which guides and supports the carriage may consist of two cylindrical bars on which the ball bearings of the carriage may freely travel.

7.4.2.2.4.	Roller with a wire rope or strap

The rollers shall have a diameter of at least 60 mm and lead the wire rope or strap from the horizontal into the vertical direction. The horizontal end of the wire rope or strap is fixed to the carriage, the vertical end is fixed to the drop weight.

7.4.2.2.5.	Drop weight

The drop weight shall have a mass of 15.0 (- 0.0/+ 0.5) kg. For shear assessment the free drop height shall be

500.0 (- 0.0/ + 5.0) mm with provision for further possible

travel of at least 400 mm. For testing the friction assessment, the free drop height shall be 500.0 (- 0.0/+ 5.0) mm with provision for further possible travel of at least 400 mm.

7.4.2.2.6.	Headform support

The system supporting the headform shall be such that any point on the helmet can be positioned in contact with the upper surface of the carriage.

7.4.2.2.7.	Lever and hinge

A rigid lever shall connect the headform support to the test apparatus with a hinge. The height of the hinge pivot above the upper surface of the carriage shall not be greater than 150 mm.

7.4.2.2.8.	Loading mass

A loading system is used to generate a force

of 400.0 (- 0.0/+ 10.0) N on the helmet normal to the surface of the carriage. This force shall be measured before each test.

7.4.2.2.9.	Verification of the test apparatus

With the unloaded carriage and a drop height of up to 450 mm, the velocity	of the carriage after 250 mm of travel shall be 4.0 ± 0.1 m/sec. This requirement shall be verified after every 500 helmet tests or once every 3 months whichever is sooner.

7.4.2.3.	Selection of test points

Any point on the helmet may be selected for friction and/or shear assessment. A helmet shall be tested as many times as necessary to ensure that all notable features are evaluated with one test only per feature. Re-orientate the helmet as necessary to allow every feature to be tested. For shear assessment evaluate all different external projections greater than 2 mm above the outer surface of the shell.

For friction assessment evaluate areas of the outer surface that are likely to produce the greatest friction.

The rim of the shell and the upper and lower edge of the visor situated within an area bounded by a sector of 120° divided symmetrically by the vertical longitudinal plane of symmetry of the helmet do not constitute a projection for the purpose of this test.

7.4.2.4.	Requirements

7.4.2.4.1.	For shear assessment the tested projection shall shear away, be detached or alternatively shall not prevent the assessment bar from sliding past the projection. In all cases the bar on the horizontal carriage shall travel past the projection.

7.4.2.4.2.	For friction assessment the abrasive carriage shall not be brought to rest by the helmet.

7.4.3.	Test for projections of the category P/J with movable lower face cover

7.4.3.1.	For strength assessment of the movable face cover in the position "J", the helmet shall be placed on the appropriate test head form selected from annex 4 in compliance with paragraph 7.3.1.3.1.

7.4.3.2.	A device to guide and release a falling mass of 4 kg ± 0.01 kg shall then be released and shall drop in a guided free fall from a height of 600 ± 5 mm hooked on to the front part of the chin section in the position "J" in the median vertical plane of the helmet

7.4.3.3.	The test apparatus shall be used to apply a shock load to a helmet secured to the headform by its own retention system. The headform shall be secured in a test ﬁxture with its vertical axis pointing upward at 45° to the direction of gravity.

This equipment shall allow a drop weight to slide in a guided free fall to impact a rigid stop anvil. The mass of the guide shall be 1.0 -0.0 +0.2 kg.     The guiding devices shall be such as to ensure that the impact speed is not less than 95 per cent of the theoretical speed.

7.4.3.4.	the movement must be such to avoid any possible interference of the chin guard with 100 mm cylinder as defined in paragraph 6.4.2. Partial detachment is not acceptable.

7.5.	Rigidity tests

7.5.1.	The helmet, after undergoing ambient-temperature and hygrometry conditioning, shall be placed between two parallel plates by means of which a known load can be applied along the longitudinal axis  (line LL in the figure) or the transverse axis (line TT in the figure). The surface of the plates shall be large enough to contain a circle of at least 65 mm in diameter.

An initial load of 30 N shall be applied, at a minimum plates speed of 20 mm/min, and after two minutes at least 30s the distance between the two plates shall be measured. The load shall then be increased by 100 N, at a minimum plates speed of 20 mm/min, and then wait for two minutes. This procedure shall be repeated until the application of a load of 630 N.

7.5.2.	The load applied to the plates shall be reduced to 30 N, at a minimum plates speed of 20 mm/min; the distance between the plates shall then be measured.

7.5.3.	The helmet used for the test along the longitudinal axis shall be a new helmet, and another new helmet shall be used for the test along the transverse axis.

7.5.4.	In the test along each axis, the deformation measured under the 630 N load shall not exceed that measured under the initial 30 N load by more than 40 mm.

7.5.5.	After restoration of the 30 N load, the deformation measured shall not exceed that measured under the initial 30 N load by more than 15 mm.

7.5.6.	In the event of cracks or breakage of the shell during the impact tests, the rigidity test may be repeated on the damaged helmets to evaluate the residual mechanical characteristics.

In this case the maximum deformation measured shall not exceed 50 mm.

7.6.	Dynamic test of the retention system (see annex 8, figure 2)

7.6.1.	The helmet shall be positioned as prescribed in paragraph 7.3.1.3.1. above.

7.6.2.	In this position the helmet is held by the shell at a point traversed by the vertical axis passing through the centre of gravity of the headform. The headform is equipped with a load-bearing device aligned with the vertical axis passing through the centre of gravity of the headform and with a device to measure the vertical displacement of the point of application of the force. A guide and arrest device for a falling mass shall then be attached below the headform. The mass of the headform so equipped shall be 15 kg ± 0.5 kg, which shall be the pre-loading on the retention system for determining the position from which the vertical displacement of the point of application of the force shall be measured.

7.6.3.	The falling mass of 10 kg ± 0.1 kg shall then be released and shall drop in a guided free fall from a height of 750 ± 5 mm.

7.6.4.	During the test, the dynamic displacement of the point of application of the force shall not exceed 35 mm.

7.6.5.	After two minutes, the residual displacement of the point of application of the force, as measured under a mass of 15 kg ± 0.5 kg, shall not exceed 25 mm.

7.6.6.	Damage to the retention system shall be accepted provided that it is still possible to remove the helmet easily from the headform. In the case of retention systems fitted with quick release mechanisms it must be possible to release the mechanism in accordance with paragraphs 7.12.2. to 7.12.2.2. The specifications set out in paragraphs 7.6.4. and 7.6.5. shall be met.

7.7.	Retention (detaching) test

7.7.1.	The helmet, previously conditioned at ambient temperature and hygrometry, is attached to the appropriate headform, selected from those listed in annex 4, in accordance with the requirements of paragraph 7.3.1.3.1. of this Regulation.

7.7.2.	Before the test, the retention system must be capable to maintain the helmet on the headform. When a preload of 3 kg ± 0.1 kg is hooked to the front border of the shell in the median vertical plane of the helmet, in reverse position, the angle between the reference line situated on the shell of the helmet and the reference plane of the headform shall not exceed 30°.

7.7.3.	A device to guide and release a falling mass (the total mass being 3 kg ± 0.1 kg) is hooked on to the rear part of the shell in the median vertical plane of the helmet, as shown in annex 8, figure 3.

7.7.4.	The falling mass of 10 kg ± 0.01 kg is then released and drops in a guided free fall from a height of 0.50 m ± 0.01 m. The guiding devices shall be such as to ensure that the impact speed is not less than 95 per cent of the theoretical speed.

7.7.5.	After the test the angle between the reference line situated on the shell of the helmet and the reference plane of the headform shall not exceed 30°.

7.7.6.	In modular helmets the test must be done in J and P configuration.

7.8.	Visor tests

7.8.1.	Sampling and use of samples

The 7 (+3 if optional test) visors are used as follows:

| Paragraph | Test | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11-14 | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | If optional test |  |  |  |  |
| 6.16.3. | Field of vision of the visor | X |  |  |  |  |  | R E T A I N E D |  |  |  | X | 1 |
| 6.16.3.4. 6.16.3.5. 6.16.3.6. 6.16.3.7. | Luminous transmittance Light diffusion Recognition signal lights Spectral transmittance | X | X | X |  |  |  |  |  |  |  |  | 3 |
| 6.16.3.8. | Refractive powers |  |  |  | X | X | X |  |  |  |  |  | 3 |
| 6.16.3.9. | Mist retardant visor (opt.) |  |  |  |  |  |  |  | X | X | X |  | 3 |
| 7.8.2. | Mechanical character. |  |  |  | X | X | X |  |  |  |  |  | 7 |
| 7.8.3. | Optical quality and scratch res. | X | X | X |  |  |  |  |  |  |  |  | 3 |

Note:	The test for recognition of signal lights may be dispensed with in the case of visors with luminous transmittance τv ≥ 80 per cent.

7.8.1.1.	Prior to any type of further conditioning for mechanical or optical test, as specified in paragraph 7.8.1., each visor shall be subject to the ultraviolet conditioning in accordance with the provision of paragraph 7.2.4.1.

7.8.2.	Mechanical characteristics

7.8.2.1.	The helmet, fitted with its visor and previously conditioned in accordance with the provisions of paragraph 7.2.3., shall be placed in accordance with the provisions of paragraph 7.3.1.3.1. on a test headform of suitable size. The test headform selected from among those shown in annex 4 shall be so placed that the basic plane is vertical.

7.8.2.2.	The test apparatus used shall be as described in paragraph 7.8.2.2.1., the metal punch being placed in contact with the visor in the vertical symmetrical plane of the headform to the right of point K. The apparatus shall be designed in such a way that the punch is stopped not less than 5 mm above the headform.

7.8.2.2.1.	The testing device mentioned in paragraph 7.8.2.2. above shall have the following characteristics:

Mass of punch 0.3 kg ± 10g Angle of cone forming punch head 60° ± 1° Radius of rounded top of punch head	0.5 mm

Mass of the drop hammer	3 kg ± 25 g

7.8.2.2.2	when the drop-hammer falls from a height of 1 + 0.005 m, measured between the top face of the punch and the lower face of the hammer, it shall be ascertained that:

7.8.2.2.3	no sharp splinters are produced if the visor is shattered. Any segment having an angle less than 60° shall be considered as a sharp splinter.

7.8.2.3.	High Speed particle test

7.8.2.3.1.	Visors shall be tested in accordance with the method specified in Annex 17

7.8.2.3.2.	After testing, the following defects shall not occur:

(a)	Visor fracture: a visor shall be considered to have fractured if it cracks through its entire thickness into two or more pieces, or visor material becomes detached from the surface away from the one struck by the ball, or if the ball passes through the visor;

(b)	Visor deformation: a visor shall be considered to have been deformed if a mark appears on the white paper on the opposite side to that struck by the ball;

(c)	Visor housing failure: a visor housing shall be considered to have failed if it separates into two or more pieces, or if it is no longer capable of holding a visor in position.

7.8.3.	Optical qualities and scratch resistance

7.8.3.1.	Test procedure

7.8.3.1.1.	The test piece shall be taken from the flattest part of the visor in the area specified in paragraph 6.16.3.2. and its minimum dimensions shall be 50 mm x 50 mm. The test shall be carried out on the face corresponding to the outside of the visor.

7.8.3.1.2.	The test piece shall undergo ambient-temperature and hygrometry conditioning in accordance with paragraph 7.2.2.

7.8.3.1.3.	The test shall comprise the following sequence of operations:

7.8.3.1.3.1.	The surface of the test piece shall be washed in water containing l per cent detergent and rinsed with distilled or demineralized water, then carefully dried with a grease-free and dust-free linen cloth.

7.8.3.1.3.2.	Immediately after drying and before abrasion, the luminous transmittance shall be measured using the method given in paragraph 7.8.3.2.1.1., and the light diffusion shall be measured according to one of the methods specified in annex 11.

7.8.3.1.3.3.	The test piece shall then be subjected to the abrasion test described in annex 10, during which 3 kg ± 0,01 kg of abrasive material shall be projected at the sample.

7.8.3.1.3.4.	Following the test, the test piece shall again be cleaned in accordance with paragraph 7.8.3.1.3.1.

7.8.3.1.3.5.	Immediately after drying the light diffusion after abrasion shall be measured by using again the same method used in accordance with paragraph 7.8.3.1.3.2. above.

7.8.3.2.	Requirements

7.8.3.2.1.	Three similar test pieces, each from a different visor and taken from the area specified in paragraph 6.16.3.2., shall meet the requirements of paragraphs 7.8.3.2.1.1. and 7.8.3.2.1.2.

7.8.3.2.1.1.	In a parallel beam, with the test specimens being irradiated vertically, determine the spectral transmittance values between 380 nm and 780 nm and then the transmittance and the visual attenuation quotient in accordance with the equations given in annex 13.

To calculate the luminous transmittance, the spectral distribution of standard illuminant D65 and the spectral values of the colorimetric 2° standard observer CIE 1931 according to ISO/CIE 10526 shall be used. The product of the spectral distribution of standard illuminant D65 and the spectral values of the colorimetric 2° standard observer CIE 1931 according to ISO/CIE 10526 is given in annex 14. Linear interpolation of these values for steps smaller than 10 nm is permissible.

7.8.3.2.1.2.	The light diffusion shall not exceed the following values for each method:

| Before abrasion |  |  | After abrasion |  |  |
| --- | --- | --- | --- | --- | --- |
| 0.65 cd/m2/l | a/ | c/ | 5.0 cd/m2/l | a/ | c/ |
| 2.5per cent | b/ |  | 10 per cent | b/ |  |

a/ measured according to annex 11, method (a);

b/ measured according to annex 11, method (b);

c/ measured according to annex 11, method (c).

7.9.	Sun shield tests

7.9.1.	Sampling and use of samples

The seven sun shield are used as follows:

| Paragraph | Test | 1 | 2 | 3 | 4 | 5 | 6 | 7 | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6.17.2 | Field of vision of the sun shield | X |  |  |  |  |  |  | 1 |
| 6.17.2.2 6.17.2.4 6.17.2.5 | Luminous transmittance Recognition of signal lights Spectral transmittance | X | X | X |  |  |  |  | 3 |
| 6.17.2.6 | Refractive powers |  |  |  | X | X | X |  | 3 |

7.9.1.1.	Prior to any type of further conditioning for mechanical or optical test, as specified in paragraph 7.9.1., each sun shield shall be subject to the ultraviolet conditioning in accordance with the provision of paragraph 7.2.4.1.

7.10.	Micro-slip test of the chin strap (see annex 8, Figure 4)

7.10.1.	The test rig consists of a flat horizontal robust base, a weight for applying a load, a freely rotatable horizontal roller of diameter not less than 20 mm, and in the same horizontal plane as the top of the roller a clamp capable of reciprocating horizontal motion at right angles to the axis of the roller with a total amplitude of 50 ± 5 mm at a frequency between 0.5 Hz and 2 Hz.

7.10.2.	Take a sample of the strap at least 300 mm long, including the tensioning and adjusting device and any additional strap fastening. Fix the upper end of the strap to the reciprocating clamp level with the top of the roller and drape the strap over the roller. Attach a weight to the lower end of the strap so that when the weight is lifted by the strap it imposes a tensile force of 20 ± 1 N. Adjust the apparatus so that when the reciprocating clamp is at the centre of its motion the weight is just resting on the base with the strap barely in tension and the strap buckle is between the clamp and roller and will not touch the roller during reciprocation.

7.10.3.	Operate the reciprocating clamp for 20 cycles. Note the position of the components on the strap. Operate the reciprocating clamp for 500 cycles then record the distance through which the components have slipped along the strap.

7.10.4.	The total slippage through the grip shall not exceed 10 mm.

7.11.	Test for resistance to abrasion of the chin strap (see Annex 8, Figure 5)

The test shall be performed on every device in which the strap slides through a rigid part of the retention system, with the following exceptions:

(a)	where the micro-slip test, paragraph 7.10., shows that the strap slips less than half the prescribed value; or,

(b)	where the composition of the material used, or the information already available, renders the test superfluous in the judgement of the technical service.

7.11.1.	The test rig is similar to that described in paragraph 7.10.1. except that the amplitude of motion is 100 ± 10 mm and the strap passes over a representative surface of the associated adjuster or other strap fitting through an appropriate angle.

7.11.2.	Select an arrangement of the apparatus appropriate for the particular design of both the strap and the fitting likely to cause abrasion. Grip one end of the strap in the oscillating clamp, arrange the strap to be threaded through the fitting as designed and hang a weight on the end to tension the strap with a force of 20 ± 1 N. Mount or otherwise steady the fitting in such a position that movement of the oscillating clamp slides the strap through the fitting, in a manner simulating slippage of the fitting on the strap when the helmet is on the head.

7.11.3.	Oscillate the clamp for a total of 5,000 cycles at a frequency between 0.5 and 2 Hz.

7.11.4.	Mount the abraded strap in a tensile testing machine using clamps which avoid local breakage of the strap, and so that there is a length of 150 ± 15 mm of strap, including the abraded portion, between the clamps. Operate the machine to stretch the strap at a speed of 100 ± 20 mm per minute.

7.11.5.	The strap shall withstand a tension of 3 kN without breaking.

7.12.	Tests for retention systems relying on quick-release mechanisms

7.12.1.	Inadvertent release by pressure

7.12.1.1.	If the retention system is designed to be released by pressure on a certain part, the system shall not release when a rigid sphere of diameter 100 mm is pressed with a force of 100 ± 5 N directly in the line of movement of that part.

7.12.1.2.	If such a system incorporates more than one quick-release mechanism, or one such mechanism requiring more than one operation to release it, the system shall be deemed not to comply with this requirement if sufficient opening of the system is caused by the pressure of the sphere on only one quick-release mechanism or for only one operation, whichever is appropriate, to allow the release of the appropriate headform.

7.12.2.	Ease of release

7.12.2.1.	The helmet shall be mounted on the apparatus described in paragraph 7.6. such that a static force of 150 ± 5 N is applied to the retention system. An additional static force of 350 ± 5 N shall be applied to the retention system for at least 30 seconds and then removed. After the additional force has been removed, the opening system shall be capable of being operated by a force not exceeding 30 N. However, if the quick release mechanism is incorporated in the helmet shell, the opening system shall be capable of being operated by a force not exceeding 60 N.

7.12.2.2.	The buckle opening force shall be applied using a dynamometer or similar device in the manner and direction of normal use. In the case of a push button the contact end shall be a polished metal hemisphere with radius 2.5 ± 0.1 mm. The opening force shall be applied on the geometric centre of the push button or respective application areas.

7.12.3.	Durability of quick-release mechanisms

7.12.3.1.	Subject the quick-release mechanism to the following procedures in the order given.

7.12.3.2.	Using apparatus appropriate to the particular design of mechanism carry out the following procedure. Close and lock the mechanism. Apply a loading force of 20 ± 1 N in the direction in which the mechanism is designed to bear load, then unlock and disengage the mechanism under load. Complete this cycle in not less than 2 s. Repeat for a total of 5,000 cycles.

7.11.3.3.	If the quick-release mechanism incorporates metal components carry out the following procedure:

7.12.3.3.	Place the complete mechanism in a closed cabinet so that the mechanism can be continuously wetted by a spray while still allowing free access of air to all parts of the mechanism. Subject the mechanism to a spray of a solution consisting of 5 ±1 per cent (m/m) of reagent grade sodium chloride in distilled or deionized water for a period of 48 ± 1 h at a temperature of 35 ± 5 °C. Rinse the mechanism thoroughly in clean running water to remove salt deposits and allow it to dry for 24 ± 1 h.

Repeat the procedure in paragraph 7.12.3.2.

7.12.3.4.	The quick release mechanism shall not fracture nor disengage when a tensile force of 2.0 kN ± 50 N is progressively applied to the retention system in the direction in which the mechanism is designed to bear load. Following the application and removal of the force, the quick release mechanism shall still be capable of operation.

7.13.	Oblique impact test method of measuring rotational acceleration

7.13.1 		Acceptance criteria

The peak of the resultant rotational acceleration (𝑃𝑅𝐴) shall be calculated. The 𝑃𝑅𝐴 shall not exceed 10,400 rad/s2 in all impact sites on helmets.

The injury predictor so called as Brain Injury Criterion (𝐵𝑟𝐼𝐶) shall be also calculated as follows:

where

ωx, ωy and ωz are maximum angular rates on X, Y, and Z-axis respectively

ωxC, ωyC and ωzC are the critical angular velocities in their respective directions:

o ωxC = 66.25 rad/s

o ωyC = 56.45 rad/s

o ωzC = 42.87 rad/s

The final time of the impact is calculated as the time where the resultant linear acceleration decreases at 5 g after its maximum peak.

The resultant value of 𝐵𝑟𝐼𝐶 must have at no time a value exceeding 0.78 during the defined impact time, in all impact sites on the samples one and two.

7.13.2.	Helmets shall be tested in accordance with the method specified in Annex 7.

7.14.	Test of photochromic visors, liquid crystal or equivalent visors

7.14.1	Acceptance criteria

The photochromic visor is characterized by its luminous transmittance that shall be determined in faded state τvo and in darkened state τv1 achieved after 15 min irradiation according with the method specified in Annex 18.

In both states, the requirements specified in 6.16.3.6. (recognition of signal lights) shall be met.

For photochromic visors, τvo /τv1 shall be ≥ 1.25.

7.14.2.	Visors shall be tested in accordance with the method specified in Annex 18.

8.		Test reports

8.1.	Each technical service shall prepare reports on the results of the approval tests and keep such reports for 10 years. In the case of the impact absorption test the report shall indicate, in addition to the results of the tests, the type of conditioning and the anvil used when these are at the discretion of the technical service, and the results of the impact on the fifth site.

9.		Production qualification

9.1.	In order to make sure that the manufacturer's production system is satisfactory, the technical service which conducted the approval tests must carry out tests to qualify production in accordance with paragraphs 9.2. and 9.3.

9.2.	Qualifying the production of helmets

The production of each new approved type of helmet must be subjected to production qualification tests.

For this purpose, a random sample from the first batch will be taken of 40 helmets of the largest size (50 helmets if the test on the S point is involved) and 10 helmets of the smallest size.

For this purpose, a random sample of helmets will be taken from the first batch, to be divided into homogenous lots of 10, choosing the biggest helmet sizes for each shell size. At least two lots among those subjected to the shock-absorption test shall consist of maximum size helmets.

The first batch is considered to be the production of the first tranche containing a minimum of 200 helmets and a maximum of 3,200 helmets.

9.2.1.	Test on the system of retention

9.2.1.1.	The 10 helmets of the smallest size of each shell are subjected to the test of the retention system described in paragraph 7.6.

All the types of retention system available for the helmet must be checked.

9.2.2.	Shock absorption test

9.2.2.1.	From the 40 helmets (50 if the S test point is involved) take 4 (5 if the S point test is involved) groups each with 10 helmets.

From every shell size of helmet type take two groups each with 10 helmets of the largest size.

9.2.2.2.	All of the helmets in a group must first be subjected to the same conditioning treatment and then subjected to the shock absorption test described in paragraph 7.3. at the same point of impact. The first group of 10 helmets will be subjected to the shock absorption test at point B, the second at point x, the third at point P the fourth at point R (and the fifth at oint S if it is involved). The conditioning and the anvil for each group are chosen by the technical service which conducted the approval tests. The helmets of the same batch can be submitted to test up to three different impact point. The location of the points must be the same for all the helmets of the same batch.

9.2.2.3.	All the shell sizes of a type of helmet must be submitted to std linear impact test on the BXPR and S points if present.

The results of the tests described in paragraphs 9.2.1. and 9.2.2. must comply with the following two conditions:

no value shall exceed 1.1 L, and

 + 2.4 S shall not exceed L

where:

L =	the limit value prescribed for each approval test

 = the mean of the values

S =	the standard deviation of the values

The value of 2.4 specified above is only valid for a series of tests applied to at least 10 helmets, tested under the same conditions.

9.2.2.3.1.	No Contracting Party applying this Regulation shall apply the criterion

 + 2.4 S shall not exceed L

as contained in paragraph 9.2.2.3., to the HIC value as measured in accordance with paragraph 7.3.

9.3.	Production qualification of the visors

The production of each new approved type of visor (approved as such or as forming part of the helmet) must be subjected to production qualification tests.

For this purpose, a random sample of 20 visors (30 if the mist- retardant test is involved) will be taken from the first batch.

The first batch is considered to be the production of the first tranche containing a minimum of 200 visors and a maximum of 3,200 visors.

9.3.1.	Test group A

light transmission 	- paragraph 6.16.3.4.

recognition of light signals 	- paragraph 6.16.3.6.

spectral transmission 	- paragraph 6.16.3.7.

light diffusion 	- paragraph 6.16.3.5.

optical qualities and 
resistance to scratches 	- paragraph 7.8.3.

Test group B

refractivity 	- paragraph 6.16.3.8.

mechanical characteristics 	- paragraph 7.8.2.

Test group C (optional)

mist-retardant 	- paragraph 6.16.3.9.

9.3.2.	From the 20 visors (30 if the mist-retardant test is involved) take two (or three if the mist-retardant test is involved) groups each of 10 visors.

9.3.3.	The first group of 10 visors will be subjected to each of the tests in group A, the second group to each of the tests in group B (and the third group to the test in group C if the mist-retardant test is involved).

9.3.4.	The results of the tests described in paragraph 9.3.3. must comply with the values prescribed for each approval test.

9.4.	Product qualification test of sun shield

9.4.1.	Test group A

light transmission			- paragraph 6.15.3.4.

recognition of light signals	- paragraph 6.15.3.6

spectral transmission		- paragraph 6.15.3.7.

Test group B

Refractive power         		- paragraph 6.15.3.8.

9.4.2.	From the 20 sun shields take two groups each of 10 sun shields.

9.4.3.	The first group of 10 sun shields will be subjected to each of the tests in group A, the second group to each of the tests in group B.

9.4.4.	The results of the tests described in paragraph 9.4.3 must comply with the values prescribed for each approval test

10.		Conformity of production and routine tests

The conformity of production procedures shall comply with those set out in the Agreement, Schedule 1 (E/ECE/TRANS/505/Rev.3), with the following requirements:

10.1.	The helmet or visor approved under this Regulation (whether the visor is approved as such or as forming part of the helmet), having satisfied the acceptability conditions of production qualification, shall be so manufactured as to conform to the type approved by complying with the requirements set out in paragraphs 6. and 7.

10.2.	In order to verify that the conditions stated in paragraph 10.1. have been met, appropriate control of the production must be performed.

10.3.	The holder of the approval is responsible for the conformity of production procedures and he must in particular:

10.3.1.	Ensure the existence of effective procedures so that the quality of the products can be inspected;

10.3.2.	Have access to the testing equipment needed to inspect the conformity of each approved type;

10.3.3.	Ensure that the test results are recorded and that the annexed documents remain available for a time period of 10 years after test;

10.3.4.	Analyze the results of each type of test in order to verify and ensure the stability of the helmet or visor characteristics, making allowances for the variations of industrial production;

10.3.5.	Ensure that for each type of helmet or visor at least those tests prescribed in paragraphs 10.5. and 10.6. of the present Regulation are carried out;

10.3.6.	Ensure that when any samples or test pieces show non-conformity with the standard test concerned, further samples are taken and tested.  All the necessary steps must be taken to restore conformity of the corresponding production.

10.4.	The authority which has granted the approval may at any time verify the conformity control methods applied in each production facility.

10.4.1.	At every inspection, the test records and production progress records must be available to the visiting inspector.

10.4.2.	The inspector may select samples at random to be tested in the manufacturer's test laboratory (in the case where the manufacturer has such a laboratory). The minimum number of samples may be determined according to the results of the manufacturer's own verification.

10.4.3.	When the level of control appears unsatisfactory, or when it seems necessary to check the validity of the tests carried out in application of paragraph 10.4.2., the inspector must select samples which will be sent to the technical service which conducted the approval tests.

10.4.4.	The relevant authorities may carry out all of the tests prescribed in the present Regulation.

10.4.5.	The relevant authorities must conduct inspections in accordance with annex 12. In cases where unsatisfactory results  are found during an inspection, the approval authority must ensure that all necessary steps are taken to restore conformity of production as rapidly as possible.

10.5.	Minimum conditions for the control of conformity of helmets

In agreement with the relevant authorities, the holder of an approval will undertake the control of conformity following the method of batch control (paragraph 10.5.1.) or following the method of continuous control (paragraph 10.5.2.).

10.5.1.	Batch control

10.5.1.1.	The holder of an approval must divide the helmets into batches which are as uniform as possible in regard to raw materials or intermediate products involved in their manufacture, and in regard to production conditions. The numbers in a batch must not exceed 3,200 units.

In agreement with the relevant authorities the tests can be carried out by the technical service or by the holder of an approval.

10.5.1.2.	For each batch, a sample must be taken in accordance with the provisions of paragraph 10.5.1.4. The sample may be taken before the batch is complete provided the sample is taken from a larger sample consisting of not less than 20 per cent of the final batch quantity.

10.5.1.3.	The size of the helmets and the tests to be conducted are given in paragraph 10.5.1.4.

10.5.1.4.	In order to be accepted, a batch of helmets must satisfy the following conditions:

|  |  |  | TESTS TO BE CONDUCTED |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Numbers in the batch | Number of samples/ helmet size | Combined number of samples | Shock absorption (para. 7.3.) | Detaching test (para. 7.7.) Retention system (para. 7.6.) | Acceptance criteria | Rejection criteria | Degree of control rigour |
| 0 < N # 500 | 1st = 1LS+1SS+2MS | 8 | 1 LS + 2 MS | 1 on SS* | 0 | 2 | Normal |
|  | 2nd = 1LS+1SS+2MS |  | 1 LS + 2 MS | 1 on SS * | 1 | 2 |  |
| 500 < N # 3200 | 1st = 2LS+1SS+2MS | 10 | 2 LS + 2 MS | 1 on SS * | 0 | 2 | Normal |
|  | 2nd = 2LS+1SS+2MS |  | 2 LS + 2 MS | 1 on SS * | 1 | 2 |  |
| 0 < N # 1200 | 1st = 3LS+2SS+3MS | 16 | 3 LS + 3 MS | 2 on SS * | 0 | 2 | Strengthened |
|  | 2nd = 3LS+2SS+3MS |  | 3 LS + 3 MS | 2 on SS * | 1 | 2 |  |
| 1200<N # 3200 | 1st = 5LS+3SS+5MS | 26 | 5 LS + 5 MS | 3 on SS * | 0 | 3 | Strengthened |
|  | 2nd = 5LS+3SS+5MS |  | 5 LS + 5 MS | 3 on SS * | 3 | 4 |  |
| Note: LS signifies = largest size (max. 62) MS signifies = medium size SS signifies = smallest size (min. 50) * = Both tests (para. 7.7. before para. 7.6.) are carried out on the same helmet. The absorption of the shocks is arranged on B, X, P, R, S for the same helmet |  |  |  |  |  |  |  |

The conditioning and the anvil in the case of the shock absorption tests are chosen by the technical service which carried out the approval tests.

This dual sampling plan functions as follows:

For a normal control, if the first sample does not contain any defective units the batch is accepted without testing a second sample. If it contains two defective units the batch is rejected.

Finally, if it contains one defective unit a second sample is extracted and it is the cumulative number which must satisfy the condition of column 7 of the table above.

There is a change from normal control to strengthened control if, out of 5 consecutive batches, two are rejected. Normal control is resumed if 5 consecutive batches are accepted.

If 2 consecutive batches subjected to the strengthened control are rejected, the provisions of paragraph 12. are applied.

10.5.1.5.	The remainder of the tests, not specified in the table above but which have to be conducted in order to obtain approval, must be conducted at least once per year.

10.5.1.6.	The control of helmet conformity is undertaken starting with the batch manufactured after the first batch which was subjected to production qualification.

10.5.1.7.	The test results described in paragraph 10.5.1.4. must not exceed L, where L is the limit value prescribed for each approval test.

10.5.2.	Continuous control

10.5.2.1.	The holder of an approval shall be obliged to carry continuous quality control on a statistical basis and by sampling. In agreement with the relevant authorities, the tests can be carried out by the technical service or by the holder of an approval.

10.5.2.2.	The samples must be taken in accordance with the provisions of paragraph 10.5.2.4.

10.5.2.3.	The helmets size is taken at random and the tests to carry out are described in paragraph 10.5.2.4.

10.5.2.4.	For the production to be considered conform, the tests of continuous control shall meet the following requirements.

|  | TESTS TO BE CONDUCTED |  |  |  |
| --- | --- | --- | --- | --- |
| Helmets Taken | Shock absorption kerbstone anvil, heat (para. 7.3.) | Shock absorption flat anvil, low temperature (para. 7.3.) | Detaching (para. 7.7.) Retention system (para. 7.6.) | Degree of control rigour |
| 0.8% means one helmet taken from every 125 manufactured | Helmet No. 1 | Helmet No. 2 | Helmet No. 3* | Normal |
| 1.5% means one helmet taken from every 66 manufactured | Helmet No. 1 | Helmet No. 2 | Helmet No. 3* | Strengthened |
| Note: * = Both tests (para. 7.7. before para. 7.6.) are carried out on the same helmet. The absorption of the shocks is arranged on B, X, P, R, S for the same helmet. |  |  |  |  |

This dual sampling plan functions as follows: Normal control:

If the helmet tested is considered to conform, the production

conforms.

If the helmet does not meet the requirements, a second helmet shall be taken.

If the second helmet tested is considered to conform, the production conforms.

If both helmets do not meet the requirements, the production does not conform and helmets which are likely to present the same failure shall be withdrawn.

Strengthened control:

Strengthened control shall replace normal control if, out of

22 helmets tested consecutively, the production has had to be withdrawn twice.

Normal control is resumed if 40 helmets taken consecutively are considered to conform,

If production subjected to the strengthened control has been withdrawn on two consecutive occasions, the provisions of paragraph 12. are applied.

10.5.2.5.	The remainder of the tests, not set out in the table above but which have to be conducted in order to obtain approval, must be conducted at least once per year.

10.5.2.6.	The continuous control of helmets is undertaken starting after the production qualification.

10.5.2.7.	The test results described in paragraph 10.5.2.4. must not exceed L, where L is the limit value prescribed for each approval test.

10.6.	Minimum conditions for the control of conformity of visors

In agreement with the relevant authorities, the holder of

an approval will undertake the control of conformity following the method of batch control (paragraph 10.6.1.) or following the method of continuous control (paragraph 10.6.2.).

10.6.1.	Batch control

10.6.1.1.	The holder of an approval must divide the visors into batches which are as uniform as possible in regard to raw materials or intermediate products involved in their manufacture, and in regard to production conditions. The numbers in a batch must not exceed 3,200 units. In agreement with the relevant authorities the tests can be carried out by the technical service or by the holder of an approval.

10.6.1.2.	For each batch, a sample must be taken in accordance with the provisions of paragraph 10.6.1.3. The sample may be taken before the batch is complete provided the sample is taken from a larger sample consisting of not less than 20 per cent of the final batch quantity.

10.6.1.3.	In order to be accepted, a batch of visors must satisfy the following conditions:

|  |  |  | TESTS TO BE CONDUCTED |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Numbers in the batch | Number of samples | Combined number of samples | Group A | Group B | Group C* | Acceptance criteria | Rejection criteria | Stringency of inspection |
| 0 < N # 500 | 1st = 4 (5*) | 8 | 3 | 1 | 1 | 0 | 2 | Normal |
|  | 2nd = 4 (5*) |  | 3 | 1 | 1 | 1 | 2 |  |
| 500 < N # 3200 | 1st = 5 (6*) | 10 | 4 | 1 | 1 | 0 | 2 | Normal |
|  | 2nd = 5 (6*) |  | 4 | 1 | 1 | 1 | 2 |  |
| 0 < N # 1200 | 1st = 8 (10*) | 16 | 6 | 2 | 2 | 0 | 2 | Strengthened |
|  | 2nd = 8 (10*) |  | 6 | 2 | 2 | 1 | 2 |  |
| 1200< N # 3200 | 1st = 13 (16*) | 26 | 10 | 3 | 3 | 0 | 3 | Strengthened |
|  | 2nd = 13 (16*) |  | 10 | 3 | 3 | 3 | 4 |  |
| * Additional visor (s) in the case where the visor (s) have been tested in accordance with mist retardant for approval |  |  |  |  |  |  |  |  |

Test group A

Light transmission 			- para.6.16.3.4.

Recognition of light signals	- para.6.16.3.6.

Spectral transmission		- para.6.16.3.7.

Light diffusion			- para.6.16.3.5.

Optical qualities and 
resistance to scratches		- para. 7.8.3.

Test group B

Refractivity	- para.6.16.3.8. 
Mechanical characteristics		- para. 7.8.2.

Test group C

Mist retardant               		 - para.6.16.3.9.

This dual sampling plan functions as follows:

For a normal control, if the first sample does not contain any defective units the batch is accepted without testing a second sample. If it contains two defective units the batch is rejected.

Finally, if it contains one defective unit a second sample is extracted and it is the cumulative number which must satisfy the condition of column 7 of the table above.

There is a change from normal control to strengthened control if, out of 5 consecutive batches, two are rejected. Normal control is resumed if 5 consecutive batches are accepted.

If 2 consecutive batches subjected to the strengthened control are rejected, the provisions of paragraph 12. are applied.

10.6.1.4.	The control of visor conformity is undertaken starting with the batch manufactured after the first batch which was subjected to production qualification.

10.6.1.5.	The test results described in paragraph 10.6.1.3. must not exceed L, where L is the limit value prescribed for each approval test.

10.6.2.	Continuous control

10.6.2.1.	The holder of an approval shall be obliged to carry continuous quality control on a statistical basis and by sampling. In agreement with the relevant authorities, the tests can be carried out by the technical service or by the holder of an  approval.

10.6.2.2.	The samples must be taken in accordance with the provisions of paragraph 10.6.2.3.

10.6.2.3.			For the production to be considered conform, the tests of continuous control shall meet the following requirements:

|  | TESTS TO BE CONDUCTED |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Visors Taken |  | Group A | Group B | Group C |  | Stringency of inspection |
| 0.8% means one visor every 125 manufactured |  | Visor Nos. 1, 2, 3 | Visor No. 4 | Visor No. 5* |  | Normal |
| 1.5% means one visor taken every 66 manufactured |  | Visor Nos. 1, 2, 3 | Visor No. 4 | Visor No. 5* |  | Strengthened |
| Note: Additional visor(s) in the case where the visor(s) have been tested in accordance with mist retardant for approval. |  |  |  |  |  |  |

Test group A

Light transmission	- para. 6.15.3.4. Recognition of light signals	- para.6.15.3.6. Spectral transmission	- para. 6.15.3.7.

Light diffusion	- para. 6.15.3.5.

Optical qualities and

resistance to scratches	- para. 7.8.3.

Test group B

Refractivity	- para. 6.15.3.8. Mechanical characteristics	- para. 7.8.2.

Test group C

Mist retardant	- para. 6.15.3.9.

This dual sampling plan functions as follows: Normal control:

If the visor tested is considered to conform, the production conforms. If the visor does not meet the requirements, a second visor shall be taken.

If the second visor tested is considered to conform, the production conforms.

If both visors do not meet the requirements, the production does not conform and visors which are likely to present the same failure shall be withdrawn.

Strengthened control:

Strengthened control shall replace normal control if, out of 22 visors tested consecutively, the production has had to be withdrawn twice. Normal control is resumed if 40 visors taken consecutively are considered to conform. If production subjected to the strengthened control has been withdrawn on two consecutive occasions, the provisions of paragraph 12. are applied.

10.6.2.4.	The continuous control of visors is undertaken starting after the production qualification.

10.6.2.5.	The test results described in paragraph 10.6.2.3. must not

exceed L, where L is the limit value prescribed for each approval test.

11.	Modification and extension of approval of a helmet or a visor type

11.1.	Every modification of the helmet and/or the visor type shall be notified to the administrative department which approved the helmet and/or the visor type.	The department may then either:

11.1.1.	Consider that the modifications made are unlikely to have an appreciable adverse effect and that in any case the protective helmet and/or visor still complies with the requirements; or

11.1.2.	Require a further test report from the technical service responsible for conducting the tests.

11.2.	Confirmation or refusal of approval, specifying the alterations shall be communicated by the procedure specified in paragraphs 5.1.3. and 5.2.3. above to the Parties to the Agreement applying this Regulation.

11.3.	The competent authority issuing the extension of approval shall assign a series number for such an extension and inform thereof the other Parties to the 1958 Agreement applying this Regulation by means of a communication form conforming to the model in annex 1A or annex 1B to this Regulation.

12.		Penalties for non-conformity of production

12.1.	The approval granted in respect of a helmet or a visor type pursuant to this Regulation may be withdrawn if the requirements set forth above are not met.

12.2.	If a Contracting Party to the Agreement applying this Regulation withdraws an approval it has previously granted, it shall forthwith so notify the other Contracting Parties applying this Regulation by means of a communication form conforming to the model in annex 1A or annex 1B to this Regulation.

13.		Production definitely discontinued

If the holder of the approval completely ceases to manufacture a helmet or a visor type approved in accordance with this Regulation, he shall so inform the authority which granted the approval.

Upon receiving the relevant communication that authority shall inform thereof the other Parties to the 1958 Agreement applying this Regulation by means of a communication form conforming to the model in annex 1A or annex 1B to this Regulation.

14.		Information for wearers

14.1.	Every protective helmet placed on the market shall bear a clearly visible label with the following inscription in the national language, or at least one of the national languages of the country of destination.

This information shall contain:

"For adequate protection, this helmet must fit closely and be securely attached.	Any helmet that has sustained a violent impact should be replaced"

and, if fitted with a non protective lower face cover:

"Does not protect chin from impacts" together with the symbol indicating the unsuitability of the lower face cover to offer any protection against impacts to the chin.

14.2.	Additionally where hydrocarbons, cleaning fluids, paints, transfers or other extraneous additions affect the shell material adversely a separate and specific warning shall be emphasized in the above-mentioned label and worded as follows:

"'Warning' -	Do not apply paint, stickers, petrol or other solvents to this helmet".

14.3.	Every protective helmet shall be clearly marked with its size and its maximum weight, to the nearest 50 grams, as placed on the market. The maximum weight quoted should include all the accessories that are supplied with the helmets, within the packaging, as it is placed on the market, whether or not those accessories have actually been fitted to the helmet.

14.4.	Every protective helmet offered for sale shall bear a label showing the type or types of visor that have been approved at the manufacturer's request.

14.5.	Every visor offered for sale shall bear a label showing the types of protective helmet for which it has been approved.

14.6.	Every visor placed on the market with a protective helmet shall be accompanied by information in the national language, or in at least one of the national languages, of the country of destination. This information shall contain:

14.6.1.	General instruction for storage and care.

14.6.2.	Specific instructions for cleaning and their notice of use. These instructions shall include a warning regarding the dangers of using unsuitable agents for cleaning (such as solvents), especially if abrasion resistant coatings are to be preserved.

14.6.3.	Advice as to the suitability of the visor for use in conditions of poor visibility and during the hours of darkness. The following warning shall be included:

14.6.3.1.	Visors with the marking indicating "daytime use only" are not suitable for use during the hours of darkness or in conditions of poor visibility.

14.6.4.	If appropriate, the following warning shall also be included:

14.6.4.1.	The fastening of this visor is such that it will not be possible to remove it instantly from the line of sight with one hand should an emergency (such as headlamp glare or misting) occur.

14.6.5.	If the visor is MIST RETARDANT approved it may be indicated.

14.6.6.	Instructions regarding the detection of obsolescence.

14.7.	Every visor placed on the market as a separate technical unit shall be accompanied by information in the national language, or in at least one of the national languages, of the country of destination. This information shall contain advice on the protective helmets for which the visor is suitable and information on those aspects specified in paragraphs 14.6.1. to 14.6.6. where such information is different to that which

accompanied the visor that was placed on the market with the protective helmets for which the visor is stated to be suitable.

15.		Transitional provisions

15.1.	Helmets and visors

15.1.1.	As from the official date of entry into force of the 06 series of amendments, no Contracting Party applying this Regulation shall refuse to grant ECE approval under this Regulation as amended by the 06 series of amendments.

15.1.2.	As from 18 months after the official date of entry into force of the 06 series of amendments, no Contracting Party applying this Regulation shall grant ECE approvals and extension unless the helmet or visor type to be approved meets the requirements of this Regulation as amended by the 06 series of amendments.

15.1.3.	As from 30 months after the official date of entry into force of the 06 series of amendments, all the Contracting Parties applying this Regulation shall prohibit the application of approval marks on helmets and visors if they refer to type approvals granted under the preceding series of amendments to this Regulation.

15.1.4.	As from 36 months after the official date of entry into force of the 06 series of amendments, Contracting Parties applying this Regulation may prohibit the sale of helmets and visors which do not meet the requirements of the 06 series of amendments to this Regulation.

15.1.5.	From the day of entry into force of this Regulation for the United Kingdom,

(a)	by way of derogation to the obligations of Contracting Parties during the transitional period set out in paragraphs 15.1.1. to 15.1.4., and

(b)	based on the declaration made by the European Community at the time of its accession to the 1958 Agreement (Depositary Notification C.N.60.1998.TREATIES-28),

the United Kingdom may prohibit the placing on the market of helmets and visors which do not meet the requirements of the 05 series of amendments to this Regulation.

16.		Names and addresses of technical services responsible for conducting approval tests, and of administrative departments

The Parties to the 1958 Agreement applying this Regulation shall communicate to the United Nations Secretariat the names and addresses of the technical services responsible for conducting approval tests and of the administrative departments which grant approval and to which forms certifying approval or extension or refusal or withdrawal of approval, or production definitely discontinued, issued in other countries, are to be sent.

Annex 1 A

Communication

(Maximum format: A4 (210 x 297 mm)

issued by:		Name of administration:

......................................

......................................

......................................

Concerning: 2	Approval granted

Approval extended

Approval refused

Approval withdrawn

Production definitively discontinued

of a type of protective helmet without/with 2 one/more 2 visor type(s) pursuant to UN Regulation No. 22

Approval No.: ............................................	Extension No.: ..........................................

1.	Trade mark:

2.	Type:

3.	Sizes:

4.	Manufacturer's name:

5.	Address:

6.	If applicable, name of manufacturer's representative:

7.	Address:

8.	Brief description of helmet:

9. 	Helmet without lower face cover (J) / with protective lower face cover

(P) / with non protective lower face cover (NP)/ with detachable or movable lower

face cover (P/J) 2

10.	Type of visor or visors:

11.	Brief description of visor or visors:

12.	Submitted for approval on:

13.	Technical service responsible for conducting approval tests:

14.	Date of report issued by that service:

15.	Number of report issued by that service:

16.	Comments:

17. 	Approval granted/extended/refused/withdrawn 2

18.	Place:

19.	Date:

20.	Signature:

21.	The following documents, bearing the approval number shown above, are available on request

Annex 1 B

Communication

(Maximum format: A4 (210 x 297 mm)

issued by:		Name of administration:

......................................

......................................

......................................

Concerning:2	Approval granted

Approval extended

Approval refused

Approval withdrawn

Production definitively discontinued

of a type of helmet visor type pursuant to UN Regulation No. 22

Approval No.: ............................................	Extension No.: ..........................................

1.	Trade mark:

2.	Type:

3.	Manufacturer's name:

4.	Address:

5.	If applicable, name of manufacturer's representative:

6.	Address:

7.	Brief description of visor:

8.	Types of helmet to which the visor may be fitted:

9.	Submitted for approval on:

10.	Technical service responsible for conducting approval tests:

12.	Number of report issued by that service:

13.	Remarks:

14.	Approval granted/extended/refused/withdrawn 2/

15.	Place:

16.	Date:

17.	Signature:

18.	The following documents, bearing the approval number shown above,

are available on request

Annex 2 A

I.	Protective helmet

Example of the arrangement of approval mark for a protective helmet without or with one or more types of visor

(See paragraph 5.1. of this Regulation)

The above approval mark affixed to a protective helmet shows that the helmet type concerned has been approved in the Netherlands (E4) under approval number 061406/J.	The approval number shows that this approval concerns a helmet which does not have a lower face cover (J) and was granted in accordance with the requirements of Regulation No. 22 already incorporating the 06 series of amendments at the time of approval, and that its production serial number is 1952.

Note:	The approval number and the production serial number shall be placed close to the circle and either above or below the letter "E" or to the left or right of that letter. The digits of the approval number and of the production serial number shall be on the same side of the letter "E" and face the same direction. The use of Roman numerals as approval numbers should be avoided so as to prevent any confusion with other symbols.

II.	Visor

Example of the arrangement of approval mark for a visor fitted to a protective helmet

(See paragraph 5.1. of this Regulation)

The above approval mark affixed to a visor shows that the visor concerned has been approved in the Netherlands (E4) under reference FX2, and that it forms an integral part of an approved helmet and that its production serial number is 1952.

Note:	The approval number and the production serial number shall be placed close to the circle and either above or below the letter "E" or to the left or right of that letter. The digits of the approval number and of the production serial number shall be on the same side of the letter "E" and face the same direction. The use of Roman numerals as approval numbers should be avoided so as to prevent any confusion with other symbols.

Annex 2 B

Example of the arrangement of the approval mark for a helmet visor

(See paragraph 5.2.7. of this Regulation)

The above approval mark affixed to a visor shows that the visor type concerned has been approved in the Netherlands (E4) under approval number 065413. The approval number shows that approval was granted in accordance with the requirements of the Regulation incorporating the 05 series of amendments at the time of approval and that its production serial number is 1952.

Note:	The approval number and the production serial number shall be placed close to the circle and either above or below the letter "E" or to the left or right of that letter. The digits of the approval number and of the production serial number shall be on the same side of the letter "E" and face the same direction. The use of Roman numerals as approval numbers should be avoided so as to prevent any confusion with other symbols.

Annex 3

Diagram of protective helmet

Annex 4

Headforms

Figure 1
Minimum extent of protection

Figure 2A
Peripheral vision

Figure 2B

Peripheral vision - vertical field

Figure 2C 
Peripheral vision - horizontal field

Figure 2D 
Peripheral vision – breath deflector

Figure 3 
Identification of points of impact

Annex 5

Positioning of the helmet on the headform

1.	The helmet is placed on a headform of appropriate size. A load of 50 N is applied on the crown of the helmet in order to adjust the helmet on the headform. It is ascertained that the vertical median plane of the helmet coincides with the median vertical plane of the headform.

2.	The front edge of the helmet is placed against a gauge to check the minimum angle for the upward field of vision. The following points are then checked:

2.1.	that the line AC and the ACDEF zone are covered by the shell (annex 4, fig. 1);

2.2.	that the requirements for the minimum downward angle and the horizontal field of vision are satisfied;

2.3.	Requirements of paragraph 6.4.2. of this Regulation relating to the rear projection should be respected.

3.	If one of these conditions is not met, the helmet is moved slightly from front to rear to seek a position where all the requirements are met. Once such a position is determined, a horizontal line is drawn on the shell at the level of the AA' plane.	This horizontal line shall determine the reference plane for the positioning of the helmet during the tests.

Annex 6

Reference headforms (shape, dimensions)

Figure 1

Principal planes and reference points of a headform

Section on a vertical longitudinal plane

Key

1	AA' plane
2	reference plane
3 	basic plane
4	point A
5	point R
	point G
6	central vertical axis

Table 1
Dimensions for Figure 1 and headform masses

| Size designation | h (mm) | x(mm) | y(mm) | z(mm) | Mass (g) |
| --- | --- | --- | --- | --- | --- |
| 445 | 108,5 | 21,0 | 81,7 | 9,9 |  |
| 455 | 110,6 | 21,5 | 83,3 | 10,1 | 1 970 ± 75 |
| 465 | 112,7 | 22,0 | 84,8 | 10,4 |  |
| 475 | 114,8 | 22,5 | 86,4 | 10,6 |  |
| 485 | 116,9 | 23,0 | 88,0 | 10.8 |  |
| 495 | 119,0 | 23,5 | 89,7 | 11,1 | 3 100 ± 100 |
| 505 | 121,1 | 24,0 | 91,2 | 11,3 |  |
| 515 | 123,2 | 24,5 | 92,7 | 11,5 |  |
| 525 | 125,3 | 25,0 | 94,5 | 11,7 |  |
| 535 | 127,4 | 25,5 | 96,0 | 11,9 | 4 100 ± 120 |
| 545 | 129,5 | 26,0 | 97,5 | 12,1 |  |
| 555 | 131,6 | 26,5 | 99,1 | 12,3 |  |
| 565 | 133,7 | 27,0 | 100,8 | 12,5 |  |
| 575 | 135,8 | 27,5 | 102,4 | 12,7 | 4 700± 140 |
| 585 | 137,9 | 28,0 | 103,9 | 12,9 |  |
| 595 | 140,0 | 28,5 | 105,4 | 13,1 |  |
| 605 | 142,1 | 29,0 | 107,2 | 13,3 | 5 600 ± 160 |
| 615 | 144,2 | 29,5 | 108,7 | 13,5 |  |
| 625 | 146,3 | 30,0 | 110,2 | 13,7 | 6 100 ± 180 |
| 635 | 148,4 | 30,5 | 111,8 | 13,9 |  |
| 645 | 150,5 | 31,0 | 113,5 | 14,1 |  |

Angle H

Table A.1 – Spherical coordinates for full headform size 445

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Reference plane

Angle V

Above

Angle H

Table A.2 – Spherical coordinates for full headform size 455

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement from front of mid-sagittal plane not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Angle V

Above

Reference plane

Angle H

Table A.3 – Spherical coordinates for full headform size 465

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Reference plane

Angle V

Above

Table A.5 – Spherical coordinates for full headform size 485

Angle H

Table A.4 – Spherical coordinates for full headform size 475

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,	Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane				not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,	Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane				not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Reference plane

Angle V

Above

Table A.5 – Spherical coordinates for full headform size 485

Angle H

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Reference plane

Angle V

Above

Table A.6 – Spherical coordinates for full headform size 495

Angle H

Reference plane

Angle V below

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Table A.7 – Spherical coordinates for full headform size 505

Angle H

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Angle V

Above

Table A.8 – Spherical coordinates for full headform size 515

Reference plane

Angle H

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Reference plane

Angle V

Above

Table A.9 – Spherical coordinates for full headform size 525

Angle H

Table A.10 – Spherical coordinates for full headform size 535

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V

Above

Reference plane

Angle V below

Table A.11 – Spherical coordinates for full headform size 545

Angle H

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle H

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Table A.12 – Spherical coordinates for full headform size 555

Angle H

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Table A.13 – Spherical coordinates for full headform size 565

Angle H

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Table A.14 – Spherical coordinates for full headform size 575

Angle H

Reference plane

Table A.15 – Spherical coordinates for full headform size 585

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle V below

Angle H

Angle V below

Reference plane

Angle V

Above

Table A.16 – Spherical coordinates for full headform size 595

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle H

Angle V below

Reference plane

Angle V

Above

Table A.17 – Spherical coordinates for full headform size 605

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle H

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Table A.18 – Spherical coordinates for full headform size 615

Angle H

Angle V below

Reference plane

Angle V

Above

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Table A.19 – Spherical coordinates for full headform size 625

Angle H

Reference plane

Reference plane

Angle V

Above

Table A.20 – Spherical coordinates for full headform size 635

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Angle H

V = Vertical angle above or below the reference plane	Angles in degrees, to be measured with an uncertainty of measurement not exceeding ± 0,2
H = Angle of vertical slice, measured in horizontal plane,		Radii in mm, with a tolerance of ± 0,5 % and measured with an uncertainty of measurement 
 from front of mid-sagittal plane					not exceeding 0,1 mm.
The jaw line shall be radiused along its length with a nominal 5 mm radius. The base of the neck shall be squared off perpendicular to the central vertical axis.

NOTE	The surface corresponding to the radii shown in italics lies below the jaw line.

Reference plane

Reference plane

Angle V

Above

Table A.21 – Spherical coordinates for full headform size 645

Table B.1
At and above the reference plane

| Angle V | Angle H | Equation to define radius, R | Angle H | Equation to define radius, R | Angle H | Equation to define radius, R |
| --- | --- | --- | --- | --- | --- | --- |
| 90 | 0 | 0,1618xC+9,2476 | 15 | 0,1621 xc + 9,080 4 | 30 | 0,1619xC+9,1657 |
| 80 |  | 0,160 1 x C + 8,973 7 |  | 0,162 5 x C + 7,543 2 |  | 0,1618xC+7,8886 |
| 70 |  | 0,159 6 x C + 8,724 6 |  | 0,159 9 x C + 8,507 5 |  | 0,160 4 x C + 8,273 5 |
| 60 |  | 0,159 x C + 9,842 |  | 0,159 4 x C + 9,607 3 |  | 0,159 2 xC + 9,752 5 |
| 50 |  | 0,1588xC+ 11,224 |  | 0,160 5 x C + 10,314 |  | 0,159 x C + 11,123 |
| 40 |  | 0,159 4 x C + 11,516 |  | 0,161 1 x C + 10,517 |  | 0,1598xC+11,007 |
| 30 |  | 0,160 5 x C + 10,344 |  | 0,161 x C + 9,885 5 |  | 0,1615xC+8,8126 |
| 20 |  | 0,1612xC+8,5764 |  | 0,1612xC+8,0269 |  | 0,163 8 x C + 5,160 1 |
| 10 |  | 0,1611 x C + 7,628 |  | 0,163 1 x C + 5,423 1 |  | 0,165 4 x C + 1,920 3 |
| 0 |  | 0,161 7 x C + 7,798 |  | 0,163 5 x C + 5,157 3 |  | 0,163 4 x C + 1,863 1 |
| 90 | 45 | 0,162 3 x C + 8,945 8 | 60 | 0,161 8 x C + 9,247 6 | 75 | 0,162 2 x C + 9,005 3 |
| 80 |  | 0,1613xC+8,2707 |  | 0,160 1 x C + 8,973 7 |  | 0,162 6 x C + 7,845 8 |
| 70 |  | 0,1622xC+7,3814 |  | 0,159 6 x C + 8,724 6 |  | 0,162 7 x C + 6,924 1 |
| 60 |  | 0,162 6 xC + 7,086 7 |  | 0,159 x C + 9,842 |  | 0,162 2 xC + 5,927 3 |
| 50 |  | 0,162 1 x C + 6,953 7 |  | 0,158 8 x C + 11,224 |  | 0,1618xC+4,1673 |
| 40 |  | 0,161 3 x C + 5,966 5 |  | 0,159 4 x C + 11,516 |  | 0,162 2 x C + 1,12 |
| 30 |  | 0,161 4 x C + 3,2511 |  | 0,160 5 x C + 10,344 |  | 0,163 5x C -3,177 6 |
| 20 |  | 0,163 3 x C - 1,134 8 |  | 0,161 2 x C + 8,576 4 |  | 0,165 x C - 7,873 |
| 10 |  | 0,165 3 x C - 5,346 5 |  | 0,161 1 x C + 7,628 |  | 0,165 2 xC-11,186 |
| 0 |  | 0,161 7 x C-4,831 6 |  | 0,161 7 x C + 7,798 |  | 0,1614 xC-10,437 |
| 90 | 90 | 0,162 x C + 9,125 8 | 105 | 0 ,162 1 xC + 9,093 3 | 120 | 0,162 2 x C + 9,004 6 |
| 80 |  | 0,161 4 x C + 8,89 |  | 0,161 1 x C + 9,399 1 |  | 0,1614xC+9,9318 |
| 70 |  | 0,161 6 x C + 7,5993 |  | 0,160 7 x C + 8,861 3 |  | 0,159 6 x C + 10,799 |
| 60 |  | 0,162 x C + 5,360 8 |  | 0,1607xC+7,3412 |  | 0,1606xC+9,3142 |
| 50 |  | 0,162 9 x C + 1,948 4 |  | 0,161 4 x C + 4,534 1 |  | 0,162 7 x C + 6,468 4 |
| 40 |  | 0,164 5 x C - 2,566 |  | 0,1628xC+0,5168 |  | 0,1639xC+3,3165 |
| 30 |  | 0,166 1 x C - 7,525 9 |  | 0,164 2 x C - 4,037 2 |  | 0,164 1 x C + 0,046 2 |
| 20 |  | 0,166 3 x C - 11,749 |  | 0,164 4 x C - 7,974 |  | 0,164 4 x C - 3,755 4 |
| 10 |  | 0,164 2 x C - 13,931 |  | 0,162 5 x C - 10,108 |  | 0,165 1 x C - 7,481 2 |
| 0 |  | 0,160 8 x C - 13,392 |  | 0,159 5 x C - 10,002 |  | 0,160 9 x C- 6,53 |
| 90 | 135 | 0,162 2 x C + 9,006 2 | 150 | 0,162 2 xc + 8,984 6 | 165 | 0,162 2 x C + 9,025 5 |
| 80 |  | 0,162 9 x C + 9,457 9 |  | 0,162 5 x C + 10,332 |  | 0,161 5 x C + 10,924 |
| 70 |  | 0,162 3 x C + 10,728 |  | 0,1634 x C + 11,251 |  | 0,162 5 x C + 11,945 |
| 60 |  | 0,161 6 x C + 11,292 |  | 0,163 4 x C + 12,112 |  | 0,163 2 x C + 12,437 |
| 50 |  | 0,161 3 x C + 10,589 |  | 0,162 6 x C + 12,622 |  | 0,163 x C + 12,498 |
| 40 |  | 0,161 9 x C + 8,529 1 |  | 0,161 8 x C + 12,194 |  | 0,1622xC+12,145 |
| 30 |  | 0,163 2 x C + 5,299 3 |  | 0,162 x C + 10,352 |  | 0,161 3 x C + 11,42 |
| 20 |  | 0,164 6 x C + 1,456 1 |  | 0,163 6 x C + 7,188 2 |  | 0,160 5 x C + 10,417 |
| 10 |  | 0,164 6 x C - 1,688 5 |  | 0,165 1 x C + 3,848 5 |  | 0,160 1 x C + 9,242 8 |
| 0 |  | 0,161 2 x C - 1,391 |  | 0,163 x C + 3,067 3 |  | 0,1601 x C + 7,912 5 |
| 90 | 180 | 0,1 62 x C + 9,082 1 |  |  |  |  |
| 80 |  | 0,164 3 x C + 9,491 6 |  |  |  |  |
| 70 |  | 0,163 4 x C + 11,462 |  |  |  |  |
| 60 |  | 0,162 4 x C + 12,789 |  |  |  |  |
| 50 |  | 0,1621 x C + 12,914 |  |  |  |  |
| 40 |  | 0,162 2 x C + 12,172 |  |  |  |  |
| 30 |  | 0,162 2 x C + 11,166 |  |  |  |  |
| 20 |  | 0,1616xC+ 10,277 |  |  |  |  |
| 10 |  | 0,161 1 xC+9,3042 |  |  |  |  |
| 0 |  | 0,1626 xC + 7,230 4 |  |  |  |  |

Table B.2
Below the reference plane

| Angle V | Angle H | Equation to define radius, R | Angle H | Equation to define radius, R | Angle H | Equation to define radius, R |
| --- | --- | --- | --- | --- | --- | --- |
| 10 | 0 | 0,163 7 x C + 8,204 4 | 15 | 0,162 4 x C + 5,7791 | 30 | 0,150 6 x C + 9,327 |
| 20 |  | 0,171 5 x C + 8,597 3 |  | 0,162 8 x C + 7,657 4 |  | 0,154 6 x C + 9,502 1 |
| 30 |  | 0,186 1 x C + 9,328 1 |  | 0,169 4 x C + 10,843 |  | 0,161 xc + 10,056 |
| 40 |  | 0,210 4 x C + 10,544 |  | 0,184 6 x C + 11,485 |  | 0,1774xC+ 10,713 |
| 46 |  | 0,232 xc + 11,629 |  | 0,208 2 x C + 13,186 |  | 0,1861 xc + 11,391 |
| 50 |  | 0,209 4 x C + 18,822 |  | 0,193 4 x C + 27,957 |  | 0,187 8 x C + 11,531 |
| 52 |  | 0,201 6 x C + 19,465 |  | 0,184 8 x C + 28,943 |  | 0,1935xC+ 12,717 |
| 55 |  | 0,191 8 x C + 19,923 |  | 0,173 7 x C + 30,031 |  | 0,189 4 x C + 13,21 |
| 60 |  | 0,179 9 x C + 19,532 |  | 0,161 7 x C + 29,455 |  | 0,184 6 x C + 13,635 |
| 65 |  | 0,175 4 x C + 26,334 |  | 0,147 5 x C + 42,113 |  | 0,196 7 x C + 14,539 |
| 10 | 45 | 0,134 5 x C + 8,733 7 | 60 | 0,122 6 x C + 8,277 2 | 75 | 0,119 6 x C + 7,381 5 |
| 20 |  | 0,138 8 x C + 8,251 1 |  | 0,124 9 x C + 8,082 9 |  | 0,120 9 x C + 6,710 9 |
| 30 |  | 0,142 2 x C + 9,036 8 |  | 0,130 9 x C + 8,458 2 |  | 0,124 6 x C + 8,789 5 |
| 40 |  | 0,154 6 x C + 10,016 |  | 0,142 3 x C + 8,435 2 |  | 0,132 1 x C + 7,042 1 |
| 46 |  | 0,165 9 x C + 10,65 |  | 0,153 x C + 9,018 1 |  | 0,138 4 x C + 8,055 4 |
| 50 |  | 0,1738 xC + 10,78 |  | 0,162 1 x C + 10,12 |  | 0,144 1 x C + 10,522 |
| 52 |  | 0,178 x C + 10,447 |  | 0,167 5 x C + 10,799 |  | 0,1481 x C + 11,641 |
| 55 |  | 0,170 2 x C + 14,751 |  | 0,165 3 x C + 11,864 |  | 0,157 1 x C + 11,423 |
| 60 |  | 0,168 5 x C + 14,694 |  | 0,170 9 x C + 14,974 |  | 0,176 5 x C + 12,349 |
| 65 |  | 0,197 8 x C + 15,457 |  | 0,203 9 x C + 16,436 |  | 0,210 2 x C + 13,41 |
| 10 | 90 | 0,120 7 x C + 6,902 2 | 105 | 0,123 5 x C + 7,635 5 | 120 | 0,128 8 x C + 8,271 8 |
| 20 |  | 0,116 9 x C + 6,043 |  | 0,1197xC+7,0857 |  | 0,1261 x C+ 6,754 3 |
| 30 |  | 0,116 4 x C + 6,526 7 |  | 0,120 3 x C + 6,225 7 |  | 0,124 5 x C + 7,259 1 |
| 40 |  | 0,122 6 x C + 7,913 5 |  | 0,126 6 x C + 6,626 6 |  | 0,127 5 x C + 8,666 9 |
| 46 |  | 0,132 3 x C + 8,252 5 |  | 0,136 2 x C + 6,930 3 |  | 0,135 7 x C + 8,860 4 |
| 50 |  | 0,141 8 x C + 8,534 4 |  | 0,1461 x C + 7,2003 |  | 0,145 x C + 8,9154 |
| 52 |  | 0,147 5 x C + 8,800 7 |  | 0,152 2 x C + 7,401 3 |  | 0,151 x C + 9,025 2 |
| 55 |  | 0,157 6 x C + 9,453 3 |  | 0,163 2 x C + 7,838 1 |  | 0,162 X C + 9,401 3 |
| 60 |  | 0,179 6 x C + 11,317 |  | 0,187 3 x C + 9,042 5 |  | 0,186 2 x C + 10,804 |
| 65 |  | 0,212 5 x C + 13,609 |  | 0,221 8 x C + 10,794 |  | 0,220 3 xC + 13,024 |
| 10 | 135 | 0,138 4 x C + 8,449 9 | 150 | 0,145 8 x C + 8,803 4 | 165 | 0,151xC+9,0546 |
| 20 |  | 0,1328 x C + 7,806 |  | 0,139 3 x C + 8,430 1 |  | 0,144 6 x C + 8,252 |
| 30 |  | 0,132 5 x C + 7,377 6 |  | 0,138 4 x C + 8,037 1 |  | 0,141 5 x C + 8,247 5 |
| 40 |  | 0,135 3 x C + 7,93 76 |  | 0,139 x C + 8,460 1 |  | 0,140 8 x C + 8,658 6 |
| 46 |  | 0,1411 xC+8,5164 |  | 0,1429 x C + 9,181 6 |  | 0,144 7 x C + 9,1792 |
| 50 |  | 0,148 5 x C + 9,111 8 |  | 0,149 x C + 9,932 8 |  | 0,151 2 x C + 9,83 |
| 52 |  | 0,153 6 x C + 9,514 2 |  | 0,153 7x C + 10,41 |  | 0,156 1 x C + 10,288 |
| 55 |  | 0, 163 5 x C + 10,286 |  | 0,1632xC+ 11,271 |  | 0,166 1 x C + 11,164 |
| 60 |  | 0,187 1 x C + 12,058 |  | 0,187xC+ 13,127 |  | 0,190 6 x C + 13,106 |
| 65 |  | 0,222 1 x C + 14,23 |  | 0,222 X C + 15,467 |  | 0,226 2 X C + 15,31 |
| 10 | 180 | 0 ,152 3 x C + 8,866 7 |  |  |  |  |
| 20 |  | 0,146 x C + 8,137 6 |  |  |  |  |
| 30 |  | 0,139 1 x C + 8,870 4 |  |  |  |  |
| 40 |  | 0,137 2 x C + 9,511 5 |  |  |  |  |
| 46 |  | 0,142 9 x C + 9,733 1 |  |  |  |  |
| 50 |  | 0, 151 2 x C + 10,064 |  |  |  |  |
| 52 |  | 0,157 x C + 10,35 |  |  |  |  |
| 55 |  | 0, 168 1 x C + 10,984 |  |  |  |  |
| 60 |  | 0,193 7 x C + 12,646 |  |  |  |  |
| 65 |  | 0,229 2 x C + 14,831 |  |  |  |  |
| NOTE: The equations shown in italics define the surface below the jaw line. |  |  |  |  |  |  |

Annex 7

Oblique impact test method of measuring rotational acceleration

1.		 Scope

The test method is designed to measure the oblique impact rotational kinematics against an anvil.

2.  		Headform

2.1. 	General

The head form shall not exhibit any resonant frequencies below 2 000 Hz.

2.2. 	Shape

The shape of the head form shall conform to the specifications in the paragraph 7.3.3.

2.3. 		Mass, Centrum of Gravity (CoG) and Moment of Inertia (MOI)

Table 1
Properties of the headforms

The headform inertia matrix of reference for the homologation is according to Table 1 (principal directions only, with regards to the centre of gravity):

| Headform denomination | Circumference [mm) | Mass [Kg) | lxx [Kg cm"] (± 5%) | lyy [Kgcm") (± 5%) | lzz [Kg cm") (± 5%) |
| --- | --- | --- | --- | --- | --- |
| A | 495· | 3.1 (± 0.10) | 142.2 | 166.6 | 95.0 |
| C | 515' | 36 (± 0.10) | 172.6 | 203.3 | 113.2 |
| E | 535· | 4.1 (± 0.12) | 202.9 | 238.6 | 141.3 |
| J | 575· | 4 7 (± 0.14) | 264.0 | 318.3 | 793 .1 |
| M | 605' | 5 6 (± 0.16) | 337.4 | 402.7 | 252.7 |
| 0 | 625' | 6.1 (± 0.18) | 383.6 | 461.1 | 293.5 |

Tolerances according to UN 960:2006

Note:  X axis => rear to nose   -   Y axis => ear to ear    -   Z axis => vertical

2.4. 	Outer surface specification

The coefficient of friction (µ) shall be 0.3 ± 0.05 between the outer surface of the head form and the common fabric used in the comfort padding of the helmet.

2.5.	Chin strap force controller

"Tightened as for normal use" means that the helmet must be tightened before each test after having applied below the chin a rigid cylinder 10 mm diameter at least 30 mm long that will be removed before the test. According paragraph 7.3.1.3.

2.6.	Instrumentation for measuring the head kinematics during impact

The instrumentation shall be calibrated to measure the linear and angular acceleration with an uncertainty not exceeding 2 per cent.  For measuring linear acceleration, the instrumentation shall be calibrated to measure within a range from 50 g to 300 g with a duration up to 30 ms.

For measuring angular acceleration, the instrumentation shall be calibrated to measure within a range from 1 000 rad/s2 to 25 000 rad/s2 with a duration up to 30 ms.

For measuring angular velocity, the instrumentation shall be calibrated to measure within a range from 5 rad/s to 70 rad/s with a duration up to 30 ms.

Headforms shall be fitted with an assembly of instruments containing either a set of three linear accelerometers and three angular rate sensors, located at their centre of gravity, or a set of nine linear accelerometers.

The assembly shall enable the measurement at the centre of gravity of the three components of the linear acceleration (𝑎𝑥, 𝑎𝑦, 𝑎𝑧) and the angular rate (𝜔𝑥, 𝜔𝑦, 𝜔𝑧) over time.

In case of use of set of three linear accelerometers and three angular rate sensors, the accelerometers shall be capable of withstanding a maximum acceleration of 2000 g without damage. The acceleration data shall be sampled at a minimum frequency of 10000 Hz and filtered in accordance with the latest edition of ISO 6487 (CFC 1000).

The angular rate sensors shall have a measurement capacity of 8000 deg/s, between 0 and 2000 Hz. The angular velocity data shall be sampled at a minimum frequency of 10000 Hz and filtered in accordance with the latest edition of ISO 6487 (CFC 180).

In case of use of a nine-accelerometer system the acceleration, data shall be sampled at a minimum frequency of 20000 Hz and filtered in accordance with the latest edition of ISO 6487 (CFC 1000). The distance between the accelerometers placed on each axis shall be at least 25 mm.

If angular rate sensors, three in total, are used they shall be placed on each anatomical axis (X, Y and Z).

Any objects attached to the head form shall be included in the total mass and moment of Inertia of the head form.

The accelerometer shall withstand a maximum acceleration of 2000 g without damage. The angular rate sensors, if used, shall withstand a maximum rotational velocity of 200 rad/s.

2.7.	Head form coefficient of friction calibration test

The head shall be positioned so that the head form bottom plan is horizontal. The head form Z-axis shall point in the positive vertical axis. A 30mm flexible band shall be used as shown in Figure 1. The flexible band shall consist of a nylon band covered with a cotton surface. The flexible band shall show a minimum elastic modulus of 4 N/mm. The quality of the pure cotton fabric, regular, not printed, shall have a density of 125 gr/m2 ± 25gr.

The flexible band shall then be positioned to cover one quarter of the headform. At one end a mass of 2 Kg shall be attached, and at the other end a force gauge shall be used. A number of n. 3 pulling cycles shall be completed and then it will be measured the average maximum pulling force on the following n. 5 cycles. This force shall be between 25-27 N.

Figure 1
Test set up to measure the coefficient of friction

Reference plane

3. 	Test method

3.1.  	Principle

The helmet is placed on a headform of appropriate size in accordance with the requirements of annex 5. The helmet shall be positioned in accordance to the HPI (head positioning index) provided by the manufacturer, if it is not available, the helmet shall be tipped towards the rear so that the front edge of the helmet in the median plane is displaced by 25 mm. The helmet shall then be allowed to fall with a specified speed on to a rigidly mounted anvil.

3.2.  	Apparatus

3.2.1. 	Base

The base (C in Figure 2) shall be solid and made of steel or a combination of steel and concrete. The base shall have a mass of at least 500 kg. At least the uppermost 25 mm shall consist of steel, which shall be firmly attached to the concrete if present. No part of the base and anvil assembly shall have a resonant frequency liable to affect the measurements.

3.2.2. 	Anvil

The anvil (A) shall be made from a solid steel cylinder with the diameter (d) of 130 mm (Figure 2). The cylinder shall then be cut with an angle (α) of 45 degrees as shown in Figure 2. The angle (α) of the anvil shall be defined from the horizontal plane (see Figure 2). The height of the base (h) shall be 30 mm ± 2 mm.

The point of first contact between the helmet and the anvil shall be at least 10 mm below the upper edge of the anvil.

Abrasive paper, with a grit designation P80 according to ISO 6344-1, shall be securely fixed on the top of the entire anvil surface. The abrasive paper shall be replaced after significant damage (up to 3 tests).

The anvil shall not move more than 2 mm in the X-direction when dropping the 58cm head form including at least 1kg helmet, at a vertical (Z) velocity of 6 m/s.

Figure 2
test apparatus

3.2.3. 	Guidance system and helmet carrier

The guidance system shall provide for the positioning of any initial head form angle and impact point on the helmet vertically above the anvil, within a radius of 10 mm. The guidance system shall ensure that the head form/helmet assembly falls onto the anvil with an impact speed of not less than 95 per cent of that which would theoretically be obtained for a free fall. The guidance system shall be attached to the helmet carrier that keeps the helmet in position during the raise and drop of the head form/helmet assembly.

The helmet carrier shall not affect the head form/helmet assembly during the impact with the anvil and 30 ms after the first contact with the anvil.

3.3.  	Measuring the impact speed

The head form/helmet assembly speed shall be measured with an uncertainty of ± 0.01 m/s at a distance not more than 60 mm prior to impact.

3.4. 	Procedure

Position the assembly so as to present the specified head form angle and impact point over the anvil, then raise to the required drop height and release. The impact speed shall be 8.0 (+ 0.15/- 0.0) m/s. Cable(s), if attached, shall not interfere with the helmet motion.

3.5.  		Impact sites

Impacts shall be performed on two helmets in correspondence of the sites as detailed: helmet sample one is used for front lateral right (45°), rear (180°) and lateral left (270°), while helmet sample 2 is used for front (0°) and rear-lateral right (135°). Only one impact per site shall be performed.

Figure 3
Impact layouts for the oblique test: SIDE VIEW

Rear lateral right
(135º)

Front lateral right
(45º)

Lateral left (270º)

Front (0º)

Rear (180º)

Figure 4
Impact layouts for the oblique test: TOP VIEW Impacts at points

Rear lateral right
(135º)

Rear (180º)

Front lateral right
(45º)

Front (0º)

Lateral left (270º)

Annex 8

Test machines headform - drop assembly

Figure 1a

Figure 1b	
Example of a suitable test apparatus for projections and surface friction (method A)

Release mechanism

Carriage

Straps

Guide wires

Net enclosure

Anvil

Instrumentation

Base

Helmet

Headform

Sturdy frame

Soft cushion

Figure 1 c
Example of a suitable test apparatus for projections and surface friction (method B)

Figure 2
Dynamic test of retention system

Figure 3
Retention (detaching) test apparatus

Figure 4
Apparatus for testing slippage of the chin strap

## Taut position	Slack position

Figure 5
Apparatus for testing abrasion of the chin strap

Annex 9

Testing of the angle of opening of the visor

The secant line MN is the straight line joining the points of the upper and lower edges of the visor contained in the median vertical plane of the helmet.

Annex 10

Abrasion test procedure

1.	Description of the test equipment

The sand spray test equipment consists essentially of that illustrated in Figure 1.	The gravity tube consists of three separate rigid polyvinylchloride tubes (PVC hard) of the same diameter, with two polyamide sieves mounted in between.	The sieves should have a mesh size of 1.6 mm ± 0.1 mm. The speed of the turntable shall be 250 + 10 rpm.

2.	Abrasive material

Natural quartz sand of a grain size of 0.50/0.7 mm, with no oversize, obtained by sieving on wire sieves complying with ISO 565 with a mesh size of 0.50 mm and 0.7 mm. The sand may be used up to 10 times.

3.	Test procedure

Three kilograms of 0.50/0.7 mm grain size quartz sand is allowed to drop through a gravity tube from a height of 1,650 mm ± 15mm onto the sample to be tested. The test piece and, if necessary, a control-piece are mounted on a turntable, the axis of which is at a 45° ±3° angle to the direction of the sand.

The test pieces are mounted on the turntable in such a way that the area to be measured does not extend beyond the turntable. Whilst the turntable is rotating, 3 kg of sand are allowed to spray over the test pieces.

Figure 1
Sand spray equipment

1.	Parts of gravity tube

2.	Container with discharge jet as figure 2, containing at least 3 kg sand

3.	Upper sieve

4.	Lower sieve

5.	Test piece

6.	Test piece holder (turnable)

Annex 11

Methods of measuring light diffusion and light transmission coefficient

1.	Method (a)

1.1.	Equipment

This assembly collects all the unscattered light originating from the visor up to an angle of 0.72 degree (using diaphragm BL) and all scattered light between the angles 1.5 degrees and 2 degrees in relation to the optical axis using diaphragm BR. The angular area is important in the case of night riding, where a range in the immediate proximity of headlights has to be observed.  The following dimensions are an information for the possible realization:

L	High-pressure xenon lamp (for example XBO 75 W)

H1	Spherical concave mirror:	focal length 150 mm; diameter 40 mm

H2	Spherical concave mirror:	focal length 300 mm; diameter 40 mm

H3	Spherical concave mirror:	focal length 300 mm; diameter 70 mm

A	Achromatic lens:	focal length 200 mm; diameter 30 m

BR	Annular diaphragm:	diameter of outer circle 21.00 mm; diameter of inner circle 15.75 mm

BL	Circular diaphragm:	diameter of aperture 7.5 mm

M	Silicon detector corrected according to curve V (λ) with diffusing screen MS

IB1	Iris-diaphragm to adjust diameter of field of observation, diameter 40 mm

IB2	Iris-diaphragm to eliminate edge effects from IB1

LB	Circular diaphragm, diameter of aperture 1 mm

P, P'	Positions of visor.

Spherical mirror H1 forms an image of light source L at diaphragm LB which is in the focal plane of H2. The concave mirror H3 forms an image of diaphragm LB in the plane of diaphragms BL and BR. The achromatic lens A is positioned immediately behind the diaphragm so that a reduced image of the test sample in position P appears on diffusing screen MS. The image of iris-diaphragm IB1 is simultaneously formed on IB2.

1.2.	Measurement

The visor is positioned in the parallel beam to position P, then diaphragm BL is set in place. The flux T1L falling onto the detector corresponds to the undiffused light transmitted by the sample.	Diaphragm BL is then replaced by annular diaphragm BR; flux T1R falling onto the detector corresponds to the total diffused light originating from the visor and from the apparatus. The visor is then placed at position P'.	Flux T2R falling onto the detector corresponds to the diffused light coming from the apparatus only. The visor is then brought out of the light beam (e.g. between P and P'). The flux TOL falling on the detector with the diaphragm BL in place corresponds to the total light.

1.3.	Optical qualities; definitions

1.3.1.	Luminous transmittance:

τ = T1L/TOL x 100

1.3.2.	Light diffusion before abrasion DB: DB = 597 x (T1R - T2R)/T1L

1.3.3.	Light diffusion after abrasion:

DA = 597 x (T1R - T2R)/T1L

2.	Method (b)

2.1.	Equipment (See figure 1)

The beam of a collimator K of semi-divergence γ/2 = 17.4 x 10-4 rd is limited by a diaphragm D1 with an opening of 12 mm against which the sample holder is placed.

An achromatic convergent lens L2 corrected for spherical irregularities links the diaphragm D1 with the receiver R, the diameter of the lens L2 being such that it does not restrict the light diffused by the sample in a cone with a top half angle of β/2 = 14°.

An annular diaphragm D2 with extended angles αo/2 = 1°

and αmax/2 = 12° is placed in a focal image plane of the lens L2

(see figure 2).

The non-transparent central part of the diaphragm is necessary to eliminate the light arriving directly from the light source. It must be possible to move the central part of the diaphragm away from the light beam in such a manner that it returns exactly to its original position.

The distance between the lens L2 and the diaphragm D1, and the focal length F2 1 of the lens L2 are to be chosen so that the image of D1 completely covers the receiver R.

For an initial incident flux of 1,000 units, the absolute precision of each reading shall be better than 1 unit.

2.2.	Measurements

The following reading shall be taken:

| Reading (T) | With sample | With central part of D2 | Quantity represented |
| --- | --- | --- | --- |
| T1 | no | no | Incident flux in initial reading |
| T2 | yes (before abrasion) | no | Flux transmitted by the new material |
| T30 | no | yes | Incident light flux with central part of D2 |
| T31 | yes (before abrasion) | yes | Flux diffused by the new material |
| T4 | yes (after abrasion) | yes | Flux diffused by the abraded material |

2.3.	Optical quantities definitions

2.3.1.	The luminous transmittance is given by:

(T2/T1)	x	100

2.3.2.	The light diffusion before abrasion is given by:

DB = (T31 - T30*)	x	100/T2 ; T30*=T30x(T2/T1)

2.3.3.	The light diffusion after abrasion is given by: DA = (T4 – T30*) x 100/T2

Note:	Markings DA and DB correspond to paragraph 1.3. of this annex

Figure 1:
Test equipment

Figure 2:
Annular diaphragm D2

3.		Method (c)

3.1.		Equipment

The test arrangement is shown in figure 3.

Note 1: The measurement principle is identical to the method (a), but the diameter of the measuring is smaller

(approximately 2.5 mm) and the test arrangement is simplified.

The beam of the laser (L) is expanded using the two lenses L1 and L2 and is directed towards the measuring point of the ocular (P). Ocular (P) is positioned in such a way what it can rotate around the axis of the beam.

The deviation of the beam is a function of the prismatic refractive power at the measuring point.

The annular or circular diaphragm, whichever is chosen, is at a distance of (400 " 2) mm from the centre of the ocular. The lens A then produces the image of the centre of the ocular on the photoreceptor S.

The part of the test arrangement, comprising the diaphragms, the lens and the receptor is designed to rotate about the vertical axis through the centre of the ocular.

The ocular and the detector part of the apparatus has to pivot in order to compensate for any prismatic refractive power of the ocular.

Note 2: For oculars without corrective effect, it is not necessary, in most cases, for the ocular and the detector part to pivot.

3.2.	Procedure

3.2.1.	Calibration of the apparatus

Set up the apparatus, the essential features of which are shown in figure 3, without the ocular in place. Put the annular diaphragm BR in place.	Rotate the detector part of the apparatus (consisting of a photoreceptor S, a lens A and the annular diaphragm BR) horizontally about P so as to align the light beam from the beam expander (consisting of a lens L1, with a typical focal length of 10 mm, a lens L2 with a typical focal length of

30 mm and a circular diaphragm B with a pinhole of sufficient size so as to provide a uniform beam) with the centre of the annular diaphragm BR. Measure the flux Φ1R falling onto the photoreceptor S, corresponding to the total non-diffused light. Replace the annular diaphragm BR by the circular diaphragm BL.

Measure the flux Φ1L falling onto the photoreceptor, corresponding to the total non-diffused light.

Obtain the reduced luminance factor for the apparatus, Ia* , for the solid angle ω using the following equation:

where Φ1R	is the luminous flux without the visor in the parallel beam and with the annular diaphragm BR in place

Φ1L	is the luminous flux without the visor in the parallel beam and with circular diaphragm BL in place

ω	is the solid angle defined by the annular diaphragm BR

3.2.2.		Testing of the visor

Place the visor in the parallel beam at position P as shown in figure 3. Repeat paragraph 3.2.1. with the visor in place, and with the visor rotated about the axis of the beam to a position such that the prismatic deviation by the visor is horizontal. Rotate the detector part of the apparatus so that the light beam falls on the centre of BR.	Obtain the reduced luminance factor for the apparatus including the visor, Ig* , for the solid angle ω using the following equation:

where Φ2R	is the luminous flux with the visor in the parallel beam and with the annular diaphragm BR in place

Φ2L	is the luminous flux without the visor in the parallel beam and with circular diaphragm BL in place

ω	is the solid angle defined by the annular diaphragm BR

Then calculate the reduced luminance factor I* of the ocular using the following equation:

I*	= I*g – I*a

Figure 3	
Arrangement of apparatus for measurement of light diffusion - Method (c)

| L | = | Laser with wavelength of (600 " 70) Note: Class 2 laser recommended. | nm. |  |
| --- | --- | --- | --- | --- |
|  |  | < 1mW. Diameter of beam between 0.6 and 1 mm |  |  |
| L1 | = | 10 mm nominal focal length lens |  |  |
| L2 B | = = | 30 mm nominal focal length lens Circular diaphragm - (a hole of 0.1 mm approx produces a uniform |  |  |
|  |  | light beam) |  |  |
| P | = | Visor sample |  |  |
| BR | = | Annular diaphragm, the diameter of the external circle being |  |  |
|  |  | 28.0 " 0.1) mm and the inner circle (21.0 " 0.1) mm. See note 2 |  |  |
|  |  | below. |  |  |
| BL | = | Circular diaphragm of 10 mm nominal diameter |  |  |
| A | = | Lens, 200 mm nominal focal length and 30 mm nominal diameter |  |  |
| S | = | Photoreceptor |  |  |

The distance between the annular/circular diaphragm and the centre of the ocular shall be (400 " 2) mm.

Note 1:	The focal lengths of the lenses are only given as a guide.	Other focal lengths may be used, for example, if a wider beam is desired or a smaller image of the sample is to be formed on the receptor.

Note 2:	The diameters of the annular diaphragm circles shall be measured to an uncertainty not exceeding 0.01 mm in order that the solid angle ω may be determined accurately; any deviation from the nominal diameters shall be taken into account by calculation.

Annex 12

Type approval scheme (flow chart)

(1) 	To be carried out at the same technical service or the same accredited independent laboratory.

(2)	Visit of the manufacturer for inspection and random sampling by the authority or technical service:

(a)	If there is no ISO 9001* or an equivalent standard: 1 time each 8 months up to 12 months depending on the results of the inspection

(b)	If there is an ISO 9001* or an equivalent standard: 1 time every 2 years, depending on the results of the inspection.

(3)	Tests in accordance to paragraph 10.5 and/or 10.6 on samples taken out of the production:

(a)	If there is no ISO 9001*: of the authority or technical service during the visit of footnote 2 a) of the manufacturer between the visits of footnote 2 (a)

(b)	 If there is an ISO 9001 1: taken by the manufacturer, procedure checked during visit of footnote 2 (b).

Annex 13

Definitions

The luminous transmittance Tv is defined as:

The relative visual attenuation quotient Q is defined as:

Q=TsignTv

where:

τv	is the luminous transmittance of the visor relative to the standard illuminant D65

τsign	is the luminous transmittance of the visor relative to the spectral power distribution of the traffic signal light and it is given by the following equation:

where:

SAλ (λ) 	is the spectral distribution of radiation of CIE standard illuminant A (or 3200 K light source for blue signal light). See: ISO/CIE 10526, "CIE standard colorimetric illuminants.

SD65λ  (λ) 	is the spectral distribution of radiation of CIE standard illuminant D65.	See: ISO/CIE 10526, "CIE standard colorimetric illuminants";

V(λ)		is the spectral visibility function for daylight vision. See: ISO/CIE 10527, "CIE standard colorimetric observers";

τS (λ)		is the spectral transmittance of the traffic signal lens;

# τV (λ)		is the spectral transmittance of the visor. 
The spectral value of the product of the spectral distributions 
(SAλ (λ) ⋅ SD65λ (λ)) of the illuminant, the spectral visibility function V(λ) of the eye and the spectral transmittance τS (λ) of the traffic light signal lenses are given in annex B.

# .

Annex 14

Product of the energy distribution of standard illumination D65 as specified in ISO 11664-2 and the spectral visibility function of the average human eye for daylight vision as specified in ISO 11664-1

Table D.1

Product of the energy distribution of Standard Illuminant D65 and the spectral visibility function of the average human eye for daylight vision

| Wavelength λ nm | SD65(λ) V (λ) | Wave length λ nm | SD65(λ) V(λ) | Wave length λ nm | SD65(A) V (λ) |
| --- | --- | --- | --- | --- | --- |
| 380 | 0,0001 | 515 | 3,0589 | 650 | 0,4052 |
| 385 | 0,0002 | 520 | 3,5203 | 655 | 0,3093 |
| 390 | 0,0003 | 525 | 3,9873 | 660 | 0,2315 |
| 395 | 0,0007 | 530 | 4,3922 | 665 | 0,1714 |
| 400 | 0,0016 | 535 | 4,5905 | 670 | 0,1246 |
| 405 | 0,0026 | 540 | 4,7128 | 675 | 0,0881 |
| 410 | 0,0052 | 545 | 4,8343 | 680 | 0,0630 |
| 415 | 0,0095 | 550 | 4,8981 | 685 | 0,0417 |
| 420 | 0,0177 | 555 | 4,8272 | 690 | 0,0271 |
| 425 | 0,0311 | 560 | 4,7078 | 695 | 0,0191 |
| 430 | 0,0476 | 565 | 4,5455 | 700 | 0,0139 |
| 435 | 0,0763 | 570 | 4,3393 | 705 | 0,0101 |
| 440 | 0,1141 | 575 | 4,1607 | 710 | 0,0074 |
| 445 | 0,1564 | 580 | 3,9431 | 715 | 0,0048 |
| 450 | 0,2104 | 585 | 3,5626 | 720 | 0,0031 |
| 455 | 0,2667 | 590 | 3,1766 | 725 | 0,0023 |
| 460 | 0,3345 | 595 | 2,9377 | 730 | 0,0017 |
| 465 | 0,4068 | 600 | 2,6873 | 735 | 0,0012 |
| 470 | 0,4945 | 605 | 2,4084 | 740 | 0,0009 |
| 475 | 0,6148 | 610 | 2,1324 | 745 | 0,0006 |
| 480 | 0,7625 | 615 | 1,8506 | 750 | 0,0004 |
| 485 | 0,9001 | 620 | 1,5810 | 755 | 0,0002 |
| 490 | 1,0710 | 625 | 1,2985 | 760 | 0,0001 |
| 495 | 1,3347 | 630 | 1,0443 | 765 | 0,0001 |
| 500 | 1,6713 | 635 | 0,8573 | 770 | 0,0001 |
| 505 | 2,0925 | 640 | 0,6931 | 775 | 0,0001 |
| 510 | 2,5657 | 645 | 0,5353 | 780 | 0,0000 |
|  |  |  |  | Sum | 100,0000 |

Spectral distribution of radiation in incandescent signal lights weighted by the sensitivity of the human eye V(λ)

Table H.1

Spectral distribution of radiation in signal lights weighted by the sensitivity of the human eye V(λ)

| Wave length | Red | Yellow | Green | Blue |
| --- | --- | --- | --- | --- |
| λ (nm) | E Red (λ) ·V(λ) | E vellow(λ) ·V(λ) | E Green(λ) ·V(λ) | E Blue(λ) ·V(λ) |
| 380 | 0,000 | 0,000 | 0,000 | 0,000 |
| 385 | 0,000 | 0,000 | 0,000 | 0,000 |
| 390 | 0,000 | 0,000 | 0,000 | 0,000 |
| 395 | 0,000 | 0,000 | 0,000 | 0,000 |
| 400 | 0,000 | 0,000 | 0,000 | 0,010 |
| 405 | 0,000 | 0,000 | 0,000 | 0,010 |
| 410 | 0,000 | 0,000 | 0,000 | 0,030 |
| 415 | 0,000 | 0,000 | 0,000 | 0,060 |
| 420 | 0,000 | 0,000 | 0,000 | 0,120 |
| 425 | 0,000 | 0,000 | 0,000 | 0,250 |
| 430 | 0,000 | 0,000 | 0,000 | 0,440 |
| 435 | 0,000 | 0,000 | 0,010 | 0,680 |
| 440 | 0,000 | 0,000 | 0,020 | 0,970 |
| 445 | 0,000 | 0,000 | 0,030 | 1,260 |
| 450 | 0,000 | 0,000 | 0,050 | 1,600 |
| 455 | 0,000 | 0,000 | 0,080 | 1,950 |
| 460 | 0,000 | 0,000 | 0,120 | 2,350 |
| 465 | 0,000 | 0,000 | 0,180 | 2,760 |
| 470 | 0,000 | 0,000 | 0,270 | 3,230 |
| 475 | 0,000 | 0,010 | 0,380 | 3,720 |
| 480 | 0,000 | 0,010 | 0,540 | 4, 240 |
| 485 | 0,000 | 0,020 | 0,740 | 4,650 |
| 490 | 0,000 | 0,040 | 1,020 | 5,080 |
| 495 | 0,000 | 0,070 | 1,410 | 5,510 |
| 500 | 0,010 | 0,120 | 1,910 | 5,870 |
| sos | 0,010 | 0, 200 | 2,610 | 6,450 |
| 510 | 0,010 | 0,320 | 3,430 | 6,800 |
| 515 | 0,010 | 0,490 | 4,370 | 6,660 |
| 520 | 0,010 | 0,760 | 5,320 | 5,950 |
| 525 | 0,020 | 1,160 | 6,130 | 5,150 |

| Wavelength | Red | Yellow | Green | Blue |
| --- | --- | --- | --- | --- |
| λ (nm) | E Red(λ) ·V(λ) | E Yellow (λ) ·V(λ) | E Green (λ) ·V(λ) | E B1ue (λ) ·V(λ) |
| 530 | 0,020 | 1,700 | 6,860 | 3,960 |
| 535 | 0,020 | 2,350 | 7,370 | 3,370 |
| 540 | 0,020 | 3,060 | 7,700 | 2,650 |
| 545 | 0,020 | 3,710 | 7,750 | 2,320 |
| 550 | 0,020 | 4,260 | 7,340 | 1,940 |
| 555 | 0,020 | 4,730 | 6,460 | 1,460 |
| 560 | 0,030 | 5,050 | 5,480 | 0,970 |
| 565 | 0,040 | 5,270 | 4,790 | 0,660 |
| 570 | 0,080 | 5,440 | 4,340 | 0,360 |
| 575 | 0,230 | 5,470 | 3,770 | 0,280 |
| 580 | 0,670 | 5,430 | 3,040 | 0,200 |
| 585 | 1,640 | 5,320 | 2,400 | 0,220 |
| 590 | 3,320 | 5,160 | 1,790 | 0,240 |
| 595 | 5,400 | 4,940 | 1,050 | 0,230 |
| 600 | 7,320 | 4,670 | 0,400 | 0,230 |
| 605 | 8,750 | 4,380 | 0,120 | 0,180 |
| 610 | 9,350 | 4,040 | 0,050 | 0,130 |
| 615 | 9,320 | 3,640 | 0,060 | 0,100 |
| 620 | 8,950 | 3,270 | 0,090 | 0,060 |
| 625 | 8,080 | 2,840 | 0,110 | 0,070 |
| 630 | 7,070 | 2,420 | 0,100 | 0,070 |
| 635 | 6,100 | 2,030 | 0,070 | 0,160 |
| 640 | 5,150 | 1,700 | 0,040 | 0,210 |
| 645 | 4,230 | 1,390 | 0,020 | 0,430 |
| 650 | 3,410 | 1,110 | 0,020 | 0,540 |
| 655 | 2,690 | 0,870 | 0,010 | 0,420 |
| 660 | 2,090 | 0,670 | 0,000 | 0,320 |
| 665 | 1,570 | 0,510 | 0,000 | 0,210 |
| 670 | 1,150 | 0,370 | 0,000 | 0,140 |
| 675 | 0,850 | 0,280 | 0,000 | 0,260 |
| 680 | 0,640 | 0,210 | 0,000 | 0,300 |
| 685 | 0,470 | 0,150 | 0,000 | 0,320 |
| 690 | 0,330 | 0,100 | 0,000 | 0,300 |
| 695 | 0,240 | 0,070 | 0,000 | 0,230 |
| 700 | 0,180 | 0,060 | 0,010 | 0,180 |
| 705 | 0,130 | 0,040 | 0,020 | 0,130 |
| 710 | 0,090 | 0,030 | 0,020 | 0,100 |
| 715 | 0,070 | 0,020 | 0,020 | 0,070 |
| 720 | 0,050 | 0,010 | 0,020 | 0,050 |

| λ (nm) | E Red(λ) ·V(λ) | E Yellow(λ) ·V(λ) | E Green(λ) ·V(λ) | E B1ue(λ) ·V(λ) |
| --- | --- | --- | --- | --- |
| 725 | 0,030 | 0,010 | 0,020 | 0,030 |
| 730 | 0,020 | 0,010 | 0,010 | 0,030 |
| 735 | 0,020 | 0,010 | 0,010 | 0,020 |
| 740 | 0,010 | 0,000 | 0,010 | 0,010 |
| 745 | 0,010 | 0,000 | 0,010 | 0,010 |
| 750 | 0,010 | 0,000 | 0,000 | 0,010 |
| 755 | 0,010 | 0,000 | 0,000 | 0,010 |
| 760 | 0,010 | 0,000 | 0,000 | 0,010 |
| 765 | 0,000 | 0,000 | 0,000 | 0,000 |
| 770 | 0,000 | 0,000 | 0,000 | 0,000 |
| 775 | 0,000 | 0,000 | 0,000 | 0,000 |
| 780 | 0,000 | 0,000 | 0,000 | 0,000 |
| Sum | 100,000 | 100,000 | 100,000 | 100,000 |

Spectral distribution of radiation in LED signal lights weighted by the sensitivity of the human eye V(λ)

Table I.1
Spectral distribution of radiation in LED signal lights weighted by the sensitivity of the human eye V(λ)

| Wavelength | Red LED | Yell ow LED | Gr eenLED | Blue LED |
| --- | --- | --- | --- | --- |
| λ (nm) | E'Red(λ) ·V(λ) | E'Yellow(λ) ·V(λ) | E'Green(λ) ·V(λ) | E'Blue(λ) ·V(λ) |
| 380 | 0,000 | 0,000 | 0,000 | 0,000 |
| 385 | 0,000 | 0,000 | 0,000 | 0,000 |
| 390 | 0,000 | 0,000 | 0,000 | 0,000 |
| 395 | 0,000 | 0,000 | 0,000 | 0,000 |
| 400 | 0,000 | 0,000 | 0,000 | 0,000 |
| 405 | 0,000 | 0,000 | 0,000 | 0,000 |
| 410 | 0,000 | 0,000 | 0,000 | 0,000 |
| 415 | 0,000 | 0,000 | 0,000 | 0,000 |
| 420 | 0,000 | 0,000 | 0,000 | 0,000 |
| 425 | 0,000 | 0,000 | 0,000 | 0,010 |
| 430 | 0,000 | 0,000 | 0,000 | 0,050 |
| 435 | 0,000 | 0,000 | 0,000 | 0,170 |
| 440 | 0,000 | 0,000 | 0,010 | 0,550 |
| 445 | 0,000 | 0,000 | 0,010 | 1,650 |
| 450 | 0,000 | 0,000 | 0,020 | 4,470 |
| 455 | 0,000 | 0,000 | 0,040 | 9,600 |
| 460 | 0,000 | 0,000 | 0,090 | 14,170 |
| 465 | 0,000 | 0,000 | 0,190 | 13,990 |
| 470 | 0,000 | 0,000 | 0,450 | 11,180 |
| 475 | 0,000 | 0,000 | 1,010 | 9,070 |
| 480 | 0,000 | 0,000 | 2,130 | 7,370 |
| 485 | 0,000 | 0,000 | 4,000 | 5,470 |
| 490 | 0,000 | 0,000 | 6,530 | 4,210 |
| 495 | 0,000 | 0,000 | 9,380 | 3,380 |
| 500 | 0,000 | 0,000 | 11,340 | 2,690 |
| 505 | 0,000 | 0,000 | 11,820 | 2,160 |
| 510 | 0,000 | 0,000 | 11,150 | 1,760 |
| 515 | 0,000 | 0,000 | 9,840 | 1,410 |
| 520 | 0,000 | 0,010 | 8,220 | 1,140 |

| Wavelength | Red LED | Yellow LED | Green LED | Blue LED |
| --- | --- | --- | --- | --- |
| λ (nm) | E'Red(λ) · V(λ) | E'vellow(λ) · V(λ) | E'Green(λ) · V(λ) | E'Blue(λ) · V(λ) |
| 525 | 0,000 | 0,010 | 6,5 50 | 0,900 |
| 530 | 0,000 | 0,020 | 4,890 | 0,690 |
| 535 | 0,000 | 0,030 | 3,570 | 0,570 |
| 540 | 0,000 | 0,050 | 2,630 | 0,480 |
| 545 | 0,000 | 0,120 | 1,870 | 0,410 |
| 550 | 0,000 | 0,240 | 1, 290 | 0,330 |
| 555 | 0,010 | 0,500 | 0,930 | 0,270 |
| 560 | 0,020 | 1,000 | 0,630 | 0, 220 |
| 565 | 0,040 | 1,850 | 0,430 | 0, 220 |
| 570 | 0,070 | 3,390 | 0,300 | 0,200 |
| 575 | 0,110 | 6,080 | 0,210 | 0,170 |
| 580 | 0,210 | 11,180 | 0,140 | 0,140 |
| 585 | 0,400 | 20,100 | 0,090 | 0,110 |
| 590 | 0,690 | 26,720 | 0,070 | 0,140 |
| 595 | 1,110 | 18,530 | 0,050 | 0,120 |
| 600 | 1,710 | 6,910 | 0,030 | 0,090 |
| 605 | 2,520 | 2, 200 | 0,020 | 0,070 |
| 610 | 3,640 | 0,700 | 0,020 | 0,090 |
| 615 | 5,350 | 0, 230 | 0,010 | 0,050 |
| 620 | 7,990 | 0,080 | 0,010 | 0,040 |
| 625 | 12,220 | 0,030 | 0,010 | 0,030 |
| 630 | 17,410 | 0,010 | 0,010 | 0,040 |
| 635 | 19,030 | 0,010 | 0,010 | 0,040 |
| 640 | 14,200 | 0,000 | 0,000 | 0,020 |
| 645 | 7,800 | 0,000 | 0,000 | 0,020 |
| 650 | 3,380 | 0,000 | 0,000 | 0,010 |
| 655 | 1,320 | 0,000 | 0,000 | 0,010 |
| 660 | 0,490 | 0,000 | 0,000 | 0,010 |
| 665 | 0,180 | 0,000 | 0,000 | 0,010 |
| 670 | 0,060 | 0,000 | 0,000 | 0,000 |
| 675 | 0,030 | 0,000 | 0,000 | 0,000 |
| 680 | 0,010 | 0,000 | 0,000 | 0,000 |
| 685 | 0,000 | 0,000 | 0,000 | 0,000 |
| 690 | 0,000 | 0,000 | 0,000 | 0,000 |
| 695 | 0,000 | 0,000 | 0,000 | 0,000 |
| 700 | 0,000 | 0,000 | 0,000 | 0,000 |
| 705 | 0,000 | 0,000 | 0,000 | 0,000 |
| 710 | 0,000 | 0,000 | 0,000 | 0,000 |

| Wavelength | Red LED | Yellow LED | Green LED | Blue LED |
| --- | --- | --- | --- | --- |
| λ (nm) | E' Red(λ) ·V(λ) | E' vellow(λ) ·V(λ) | E' Green(λ) ·V(λ) | E' Blue(λ) ·V(λ) |
| 715 | 0,000 | 0,000 | 0,000 | 0,000 |
| 720 | 0,000 | 0,000 | 0,000 | 0,000 |
| 725 | 0,000 | 0,000 | 0,000 | 0,000 |
| 730 | 0,000 | 0,000 | 0,000 | 0,000 |
| 735 | 0,000 | 0,000 | 0,000 | 0,000 |
| 740 | 0,000 | 0,000 | 0,000 | 0,000 |
| 745 | 0,000 | 0,000 | 0,000 | 0,000 |
| 750 | 0,000 | 0,000 | 0,000 | 0,000 |
| 755 | 0,000 | 0,000 | 0,000 | 0,000 |
| 760 | 0,000 | 0,000 | 0,000 | 0,000 |
| 765 | 0,000 | 0,000 | 0,000 | 0,000 |
| 770 | 0,000 | 0,000 | 0,000 | 0,000 |
| 775 | 0,000 | 0,000 | 0,000 | 0,000 |
| 780 | 0,000 | 0,000 | 0,000 | 0,000 |
| Sum | 100,000 | 100,000 | 100,000 | 100,000 |

Annex 15

Test of refractive powers

1.		Spherical and astigmatic refractive powers

1.1.1.	Apparatus

1.1.2.	Telescope

A telescope with an aperture nominally 20 mm and a magnification between 10 and 30, fitted with an adjustable eyepiece incorporating a reticular.

1.1.3.	Illuminated target

A target, consisting of a black plate incorporating the cut-out pattern shown in figure 1, behind which is located a light source of adjustable luminance with a condenser, if necessary, to focus the magnified image of the light source on the telescope objective.

The large annulus of the target has an outer diameter of 23 ± 0.1 mm with an annular aperture of 0.6 ± 0.1 mm.	The small annulus has a inner diameter of 11.0 ± 0.1 mm with annular aperture of 0.6 ± 0.1 mm. The central aperture has a diameter of 0.6 ± 0.1 mm. The bars are nominally 20 mm long and 2 mm wide with a nominal 2 mm separation.

Figure 1

Telescope target

1.1.4.	Filter

A filter with its maximum transmittance in the green part of the spectrum may be used to reduce chromatic aberrations.

1.1.5.	Calibration lenses

Lenses with positive and negative spherical refractive powers of 0.06 m-1, 0.12 m-1 and 0.25 m-1 (tolerance ± 0.01 m-1).

1.2.	Arrangement and calibration of apparatus

The telescope and illuminated target are placed on the same optical axis 4.60 ± 0.02 m apart.

The observer focuses the reticule and the target and aligns the telescope to obtain a clear image of the pattern.	This setting is regarded as the zero point of the focusing scale of the telescope.

The focusing adjustment of the telescope is calibrated with the calibration lenses (paragraph 1.1.4.) so that a power of 0.01 m-1 may be measured.	Any other calibration method may be used.

1.3.	Procedure

The visor is mounted in front of the telescope as worn and measurements shall be taken at the sign points as specified in paragraph 6.15.3.8.

1.3.1.	Spherical and astigmatic refractive powers

1.3.1.1.	Visors without astigmatic refractive power

The telescope is adjusted until the image of the target is perfectly resolved.

The spherical power of the visor is then read from the scale of the telescope.

1.3.1.2.	Visor with astigmatic refractive power

The target, on the visor, is rotated in order to align the principal meridians of the visor with the bars on the target. The telescope is focused firstly on one set of bars (measurement D1) and then on the perpendicular bars (measurement D2). The spherical power is the mean,  D1 + D22  ,  the astigmatic refractive power is the absolute difference, | D1 - D2 | , of the two measurements.

2.		Determination of the difference in prismatic refractive power

2.1.	Apparatus

The arrangement of the reference method is shown in figure 2.

2.2.1.	Procedure

The diaphragm LB1, illuminated by the light source, is adjusted in such a way that it produces an image on the plane B when the visor (P) is not in position. The visor is placed in front of the lens L2 so that the axis of the visor is parallel to the optical axis of the test assembly.

Adjustable tilt visors are positioned with their ocular regions normal to the optical axis of the equipment.

Measure the vertical and horizontal distance between the two displaced images arising from the two ocular areas of the visor.

These distance in cm are divided by 2 to give the horizontal and vertical prismatic difference in cm/m.

If the light paths which correspond to the two eye regions cross, the prismatic refractive power is "base in" and if the light paths do not cross, it is "base out".

Figure 2
Arrangement apparatus for measurement of prismatic difference

La =	light source, for example, small filaments lamp, laser with wavelength of 600 " 70 nm, etc.

J =	interface filter, with peak transmittance in the green part of the spectrum (required only if a filament lamp is used as the light source).

L1 =	achromatic lens focal length between 20 and 50 mm. LB1	= diaphragm, diameter of aperture 1 mm  nominal

P =	visor

LB2 =	diaphragm as shown in detail A

L2 =	achromatic lens, 1,000 mm nominal focal length and 75 mm nominal diameter

B =	image plane

Annex 16

Test for mist-retardant visor

1.	Apparatus

Apparatus to determine the change in the non-diffused transmittance value, as shown in figure 1.

The nominal diameter of the parallel beam is 10 mm. The size of the beam divider, reflector R and lens L3 shall be selected in such a way that diffused light is captured up to an angle of 0.75°. If a lens L3 with a nominal focal length f3 = 400 mm is used, the nominal diameter of a diaphragm is 10 mm. The plane of the diaphragm must lie within the focal plane of the lens L3.

The following focal lengths fi of the lens Li are nominal examples and will not affect the test results:

f1 = 10 mm and f2 = 100 mm

The light source shall be a laser with a wavelength of 600 ± 70 nm. The volume of air above the water bath is at least 4 litres. The seating ring has a nominal diameter of 35 mm and a nominal height of 24 mm is then measured to the highest point of the seating ring. A soft rubber ring, 3 mm thick and 3 mm wide (nominal dimensions), is inserted between the sample and the seating ring.

The water bath container also contains a ventilator to circulate the air. In addition, there must also be a device to stabilize the temperature on the water bath.

2.	Samples

At least 3 samples of the same type are to be tested. Before the test, the samples are conditioned for one hour in distilled water (at least 5 cm3 water per cm2 sample surface area) at 23 ± 5 °C, then dabbed dry and then conditioned in air for at least 12 hours at 23 ± 5 °C and 50 per cent nominal relative humidity.

3.	Procedure and evaluation

The ambient temperature during the measurement is 23 ± 5 °C.

The temperature of the water bath is set at 50 ± 0.5 °C. The air above the water bath is circulated using a ventilator, so that it becomes saturated with water vapor. During this time, the measurement opening is to be covered. The ventilator is switched off before the measurement.

To measure the change in the value of the transmittance τr the sample is placed on the seating ring and the time determined until the square of τr has dropped to less than 80 per cent of the initial value of the sample without fogging (time without fogging).

τ

=

2	Φb

r

Φu

where:

Φb	is the luminous flux when there is fogging on the sample

Φu	is the luminous flux before fogging

Initial fogging of maximum 0.5 s duration shall not be taken into consideration in the evaluation.

Note 1: Since the light beam passes through the samples twice, this measurement defines Tr2

Note 2: The period until the start of the fogging can usually be determined visually. However, with some types of coating the formulation of the surface water causes diffusion to increase more slowly so that visual evaluation is difficult. The detection apparatus described in paragraph 1.1. should then be used.

Figure 1:
Test apparatus for mist-retardant visor

Annex 17

High speed particle test for visors

1.	Scope

Test for visor resistance to high-speed particles

2. 	Apparatus

2.1.	Headform

Appropriate headform, as defined in 7.3.3.

2.2.	Propulsion equipment

The apparatus shall be capable of imparting known speeds of up to 195 m/s to a 6 mm nominal diameter steel ball of 0,86 g minimum mass.

Note 1: The apparatus consists fundamentally of a barrel or tube of sufficient length to ensure a reproducible exit speed of the steel ball, with a breech or loading mechanism ensuring that the ball is in a given position in relation to the tube or barrel end, and of a spring or compressed gas to provide propulsion.

The apparatus also includes a means of calibrating or measuring the exit speed of the ball; because of the speed and distances involved, a timing indicator, recording in multiples of not greater than 10 µs is required.

The measurement of speed should be made as near as possible to the point of impact. The end of the barrel or tube should be protected against ricochets.

The area surrounding the test specimen, the head-form and the barrel or tube should be enclosed.

Note 2: The tube length should be chosen to ensure that the required speed for the ball is achieved.

Note 3: For the time measurement, a method using an electronic timer operated by photoelectric cells through amplifiers has been found suitable.

The distance between the sensing elements should not exceed 150 mm.

3.	Procedure

Resistance to high speed particles

Place the eye-protector to be tested on the headform in the position corresponding to normal use and with the tension of the headband, if fitted, adjusted according to the manufacturer's instructions.

Insert a sheet of carbon paper on top of a sheet of white paper, between the eye-protector and the head-form. Position the eye-protector/headform assembly in front of the propulsion equipment, the point of impact being not more than 250 mm from the exit end of the speed sensing equipment.

Project the steel ball at 60 m/s. The points of impact are (L1 and L2).

(a)	left eye frontal;

(b)	right eye frontal;

Two samples shall be conditioned in air at 50 °C for 2 h and four two additional samples shall be conditioned in air at -10 °C for 2 h;

The impact of the steel ball on the goggles shall take place within 30 s after the removal of the sample from the corresponding atmosphere;

The test shall be made at an ambient temperature of (23 ± 5) °C;

New specimens shall be used for this test and each specimen shall only be subjected to two impacts.

Annex 18

Test for photochromic, liquid crystal visors

1.	Scope

To define the maximum and the minimum light transmittance of a visor capable of two different levels, as photochromic, liquid crystal or equivalent visors.

2.	Apparatus

2.1.	Light source(s) to approximate the spectral distribution of solar radiation for air mass m = 2 for testing

Testing shall be done with a Xenon high-pressure lamp with filters chosen so that the specified illuminance of (50 000 ± 5 000) lx and the irradiance values (with permitted tolerances) given in the following table are reached.

| Wavelength range nm | Irradiance W·m-2 | Tolerance W·m-2 |
| --- | --- | --- |
| 300 – 340 | < 2,5 | - |
| 340 – 380 | 5,6 | ±1,5 |
| 380 – 420 | 12,0 | ±3,0 |
| 420 – 460 | 20,0 | ±3,0 |
| 460 – 500 | 26,0 | ±2,6 |

2.1.1.	Radiation source using one lamp

Use an ozone free high-pressure xenon arc lamp, a heat absorbing filter and a cut-on filter as specified in the following table:

Spectral transmittance of the combination of the heat absorbing filter and the cut-on filter for the measurement of photochromic lenses.

This transmittance curve can be achieved using, for example, a clear white crown glass, e.g. B 270 with a thickness of 5 mm and a heat absorbing filter, e.g. a Schott KG 2 of 3 mm thickness or a Pittsburg 2043 of 2 mm thickness.

2.1.2.	Radiation source using two lamps

The use of two ozone free high-pressure xenon arc lamps approximates as closely as possible the spectral distribution of solar radiation for an air mass of m = 2.

The radiation of the two lamps is superimposed with a semi-transparent mirror. If a different filtering is used in front of the two lamps, the solar spectrum can be approximated more closely than with one lamp.

The principle may be extended by the use of more than two lamps to even better approximate the solar spectrum in the relevant spectral ranges.

## 2.1.3.	Conditioning for luminous transmittance in the faded state

Unless the manufacturer specifies a different procedure to reach the faded state in the information supplied with the product, photochromic visors shall be conditioned by the following procedure:

(a)	Store filters in the dark at (65 ± 5) °C for (2 ± 0,2) h.

(b)	Store filters in the dark at (23 ± 5) °C for at least 12 h.

(c)	Expose filters to (15 000 ± 1 500) lx at (23 ± 1) °C for 15 min using a source similar to the one described

(d)	Store filters in the dark at (23 ± 5) °C for at least 60 min.

*	In accordance with the programme of work of the Inland Transport Committee for 2018–2019 (ECE/TRANS/274, para. 123 and ECE/TRANS/2018/21/Add.1, Cluster 3.1), the World Forum will develop, harmonize and update UN regulations to enhance the performance of vehicles. The present document is submitted in conformity with that mandate.

Protective helmets for wear in competitions may have to comply with stricter provisions.

See also the diagram in annex 3.

The distinguishing numbers of the Contracting Parties to the 1958 Agreement are reproduced in Annex 3 to the Consolidated Resolution on the Construction of Vehicles (R.E.3), document ECE/TRANS/WP.29/78/Rev. 6, Annex 3- www.unece.org/trans/main/wp29/wp29wgs/wp29gen/wp29resolutions.html.

The distinguishing numbers of the Contracting Parties to the 1958 Agreement are reproduced in Annex 3 to the Consolidated Resolution on the Construction of Vehicles (R.E.3), document ECE/TRANS/WP.29/78/Rev.6, Annex 3 - www.unece.org/trans/main/wp29/wp29wgs/wp29gen/wp29resolutions.html.

Helmets of sizes not listed in paragraph 7.3.3.2. shall be tested with the next smaller headform listed. Helmets of size 62 or larger shall be tested with the headform "O".

During the test along the longitudinal axis, the contact point between the helmet and one of the two plates must be the "B" impact point

Unsatisfactory results mean values exceeding 1.1 L, where L is the limit value prescribed for each approval test.

1	Distinguishing number of the country which has granted/extended/refused/withdrawn an approval (see approval provisions in the Regulation).

2	Strike out what does not apply

1	Distinguishing number of the country which has granted/extended/refused/withdrawn an approval (see approval provisions in the Regulation).

2	Strike out what does not apply

1 	For L2 a focal diameter of about 80 mm is recommended

1 		Or an equivalent standard, i.e. one that delivers the same or better levels of quality