INF. 22

ECONOMIC COMMISSION FOR EUROPE

INLAND TRANSPORT COMMITTEE

Working Party on the Transport of Dangerous Goods

(71st Session, Geneva, 5-9 November 2001)

Proposal to refer to EN standards in chapter 6.8 of the ADR

Transmitted by the European Committee for Standardisation (CEN)

CEN proposes to refer to two standards EN 12252: 2000 and EN 12493:2001 in 6.8.2.6 as follows:

| DOC. Reference | Title of Document | Applicable sections |
| --- | --- | --- |
| EN 12252:2000 | Equipping of LPG road tankers | 6.8.3.2 |
| EN 12493 (except Annex C) | Design and manufacture of welded steel tanks for LPG road tankers | 6.8.2.1; 6.8.2.4.1(with the exclusion of the leakproofness test); 6.8.2.5.1 and 6.8.3.5.1 |

Annex C of EN12493 gives the design conditions for countries that accept for national transport design conditions different from those in ADR. In order to avoid any confusion with regard to the validity of that Annex (though informative) for the design of tanks for international transport, it is proposed to exclude it from the reference.

### A synopsis of the assessments made by the CEN consultant for these two standards was presented in INF.27E at the November 2000 session of WP15.

### At that meeting, it was requested from CEN to provide together with the final proposal for adoption a comparison between the minimum thickness for pressure calculated according to the requirements of the standard and according to the requirements of ADR.

### The comparison is shown in attachment for LPG tanks of various diameters and at various pressures. The last column indicates the variations. Negative figures are in favour of the thickness calculated by the standard; positive figures are in favour of the thickness calculated by the ADR. The maximum variation is 3.7% versus the “ADR thickness”.

### For low pressures, the variations are due to the linear formula (without corrections for “other steels”) adopted in the standard (D/500 + 1.5 mm) for the calculation of the “minimum thickness against damage”compared to the “step” formula in ADR (6mm >1.8m; 5mm<1.8m). For those reasons, the minimum thickness required by the standard is in many cases higher than that required by ADR.

Attachment to CEN informal document to WP15-Nov.2001

| Determination of minimum wall thickness according to EN 12493 and to chapter 6.8 |
| --- |
| Material | Material characteristics | ADR limitations | Std limitations |  |  | Ratio |
| Grade | Re | Rm | A |  | Rex0.75 | Rmx0.5 | Re/1.5 | Rm/2.4 | ADR | Std |  |
| Annex L | N/mm² | N/mm² | % | Re/Rm | N/mm² | N/mm² | N/mm² | N/mm² | N/mm² |  |
| P235GH* | 235 | 360 | 25 | 0.65 | 176 | 180 | 157 | 150 | 176 | 150 | 1.18 |
| P265GH* | 265 | 410 | 23 | 0.65 | 199 | 205 | 177 | 171 | 199 | 171 | 1.16 |
| P295GH | 295 | 460 | 22 | 0.64 | 221 | 230 | 197 | 192 | 221 | 192 | 1.15 |
| P355GH | 355 | 510 | 21 | 0.70 | 266 | 255 | 237 | 213 | 255 | 213 | 1.20 |
| P275N* | 275 | 390 | 24 | 0.71 | 206 | 195 | 183 | 163 | 195 | 163 | 1.20 |
| P355N | 355 | 490 | 22 | 0.72 | 266 | 245 | 237 | 204 | 245 | 204 | 1.20 |
| P460N | 460 | 570 | 17 | 0.81 | 345 | 285 | 307 | 238 | 285 | 238 | 1.20 |
| S 235* | 235 | 360 | 26 | 0.65 | 176 | 180 | 157 | 150 | 176 | 150 | 1.18 |
| S 275* | 275 | 430 | 22 | 0.64 | 206 | 215 | 183 | 179 | 206 | 179 | 1.15 |
| S 355J2G3 | 355 | 510 | 22 | 0.70 | 266 | 255 | 237 | 213 | 255 | 213 | 1.20 |
| *=mild steel |  |  |  |  |  |  |  |  |  |  |
| case 1a: Di=2300; De=2330 mm; test pressure 25 bar (with thermal insulation) |
| Material |  |  | e mini | e mini | e mini | e mini | e (mm) | e (mm) | Diff. |  |  |
| Grade | ADR | Std | pressure | pressure | 6.8.2.1.18 | D.3.1 | final | final | e |  |  |
| Annex L | N/mm² | ADR | STD | ADR | STD | ADR | STD | % |  |  |
| P235GH* | 176 | 150 | 16.31 | 16.07 | 6.0 | 6.16 | 16.3 | 16.1 | 1.5% |  |  |
| P265GH* | 199 | 171 | 14.47 | 14.12 | 6.0 | 6.16 | 14.5 | 14.1 | 2.4% |  |  |
| P295GH | 221 | 192 | 12.99 | 12.59 | 6.0 | 6.16 | 13.0 | 12.6 | 3.1% |  |  |
| P355GH | 255 | 213 | 11.27 | 11.37 | 5.7 | 6.16 | 11.3 | 11.4 | -0.8% |  |  |
| P275N* | 195 | 163 | 14.74 | 14.84 | 6.0 | 6.16 | 14.7 | 14.8 | -0.7% |  |  |
| P355N | 245 | 204 | 11.73 | 11.83 | 5.7 | 6.16 | 11.7 | 11.8 | -0.8% |  |  |
| P460N | 285 | 238 | 10.09 | 10.17 | 6.1 | 6.16 | 10.1 | 10.2 | -0.9% |  |  |
| S 235* | 176 | 150 | 16.31 | 16.07 | 6.0 | 6.16 | 16.3 | 16.1 | 1.5% |  |  |
| S 275* | 206 | 179 | 13.94 | 13.47 | 6.0 | 6.16 | 13.9 | 13.5 | 3.4% |  |  |
| S 355J2G3 | 255 | 213 | 11.27 | 11.37 | 5.6 | 6.16 | 11.3 | 11.4 | -0.8% |  |  |

*=mild steel

| case 3a: Di=1700 mm; De=1720 mm; test pressure 25 bar (with thermal insulation) |
| --- |
| Material |  |  | e mini | e mini | e mini | e mini | e (mm) | e (mm) | Diff. |  |  |
| Grade | ADR | Std | pressure | pressure | 6.8.2.1.18 | D.3.1 | final | final | e |  |  |
| Annex L | N/mm² | ADR | STD | ADR | STD | ADR | STD | % |  |  |
| P235GH* | 176 | 150 | 12.06 | 11.86 | 5.0 | 4.94 | 12.1 | 11.9 | 1.6% |  |  |
| P265GH* | 199 | 171 | 10.69 | 10.42 | 5.0 | 4.94 | 10.7 | 10.4 | 2.5% |  |  |
| P295GH | 221 | 192 | 9.60 | 9.30 | 5.0 | 4.94 | 9.6 | 9.3 | 3.2% |  |  |
| P355GH | 255 | 213 | 8.33 | 8.39 | 4.8 | 4.94 | 8.3 | 8.4 | -0.7% |  |  |
| P275N* | 195 | 163 | 10.90 | 10.96 | 5.0 | 4.94 | 10.9 | 11.0 | -0.5% |  |  |
| P355N | 245 | 204 | 8.67 | 8.73 | 4.8 | 4.94 | 8.7 | 8.7 | -0.7% |  |  |
| P460N | 285 | 238 | 7.46 | 7.51 | 5.1 | 4.94 | 7.5 | 7.5 | -0.7% |  |  |
| S 235* | 176 | 150 | 12.06 | 11.86 | 5.0 | 4.94 | 12.1 | 11.9 | 1.6% |  |  |
| S 275* | 206 | 179 | 10.30 | 9.94 | 5.0 | 4.94 | 10.3 | 9.9 | 3.5% |  |  |
| S 355J2G3 | 255 | 213 | 8.33 | 8.39 | 4.6 | 4.94 | 8.3 | 8.4 | -0.7% |  |  |

| case 1d: Di=2300; De=2330 mm; test pressure 12 bar (with thermal insulation) |
| --- |
| Material |  |  | e mini | e mini | e mini | e mini | e (mm) | e (mm) | Diff. |  |  |
| Grade | ADR | Std | pressure | pressure | 6.8.2.1.18 | D.3.1 | final | final | e |  |  |
| Annex L | N/mm² | ADR | STD | ADR | STD | ADR | STD | % |  |  |
| P235GH | 176 | 150 | 7.83 | 7.74 | 6.0 | 6.16 | 7.8 | 7.7 | 1.1% |  |  |
| P265GH | 199 | 171 | 6.94 | 6.80 | 6.0 | 6.16 | 6.9 | 6.8 | 2.1% |  |  |
| P295GH | 221 | 192 | 6.24 | 6.06 | 6.0 | 6.16 | 6.3 | 6.1 | 4.2% |  |  |
| P355GH | 255 | 213 | 5.41 | 5.47 | 5.7 | 6.16 | 5.7 | 6.1 | -6.8% |  |  |
| P275N | 195 | 163 | 7.08 | 7.15 | 6.0 | 6.16 | 7.1 | 7.1 | -1.0% |  |  |
| P355N | 245 | 204 | 5.63 | 5.69 | 5.7 | 6.16 | 5.7 | 6.1 | -7.3% |  |  |
| P460N | 285 | 238 | 4.84 | 4.89 | 6.1 | 6.16 | 6.1 | 6.1 | 0.1% |  |  |
| S 235J2G3 | 176 | 150 | 7.83 | 7.74 | 6.0 | 6.16 | 7.8 | 7.7 | 1.1% |  |  |
| S 275J2G3 | 206 | 179 | 6.69 | 6.48 | 6.0 | 6.16 | 6.7 | 6.5 | 3.1% |  |  |
| S 355J2G3 | 255 | 213 | 5.41 | 5.47 | 5.6 | 6.16 | 5.6 | 6.1 | -10.2% |  |  |
| case 3d: Di=1700 mm; De=1720 mm; test pressure 12 bar (with thermal insulation) |
| Material |  |  | e mini | e mini | e mini | e mini | e (mm) | e (mm) | Diff. |  |  |
| Grade | ADR | Std | pressure | pressure | 6.8.2.1.18 | D.3.1 | final | final | e |  |  |
| Annex L | N/mm² | ADR | STD | ADR | STD | ADR | STD | % |  |  |
| P235GH | 176 | 150 | 5.79 | 5.71 | 5.0 | 4.94 | 5.8 | 5.7 | 1.3% |  |  |
| P265GH | 199 | 171 | 5.13 | 5.02 | 5.0 | 4.94 | 5.1 | 5.0 | 2.2% |  |  |
| P295GH | 221 | 192 | 4.61 | 4.48 | 5.0 | 4.94 | 5.0 | 4.9 | 0.4% | ** |  |
| P355GH | 255 | 213 | 4.00 | 4.04 | 4.8 | 4.94 | 4.8 | 4.9 | -3.4% | ** |  |
| P275N | 195 | 163 | 5.23 | 5.28 | 5.0 | 4.94 | 5.2 | 5.3 | -0.9% |  |  |
| P355N | 245 | 204 | 4.16 | 4.20 | 4.8 | 4.94 | 4.8 | 4.9 | -3.8% | ** |  |
| P460N | 285 | 238 | 3.58 | 3.61 | 5.1 | 4.94 | 5.1 | 4.9 | 3.1% | ** |  |
| S 235J2G3 | 176 | 150 | 5.79 | 5.71 | 5.0 | 4.94 | 5.8 | 5.7 | 1.3% |  |  |
| S 275J2G3 | 206 | 179 | 4.95 | 4.79 | 5.0 | 4.94 | 5.0 | 4.9 | 1.2% | ** |  |
| S 355J2G3 | 255 | 213 | 4.00 | 4.04 | 4.6 | 4.94 | 4.6 | 4.9 | -6.7% | ** |  |
|  |  |  |  |  |  |  |  |  | **=surge plates thickness=e |