UN/SCETDG/26/INF.38

# COMMITTEE OF EXPERTS ON THE TRANSPORT OF

# DANGEROUS GOODS AND ON THE GLOBALLY

# HARMONIZED SYSTEM OF CLASSIFICATION

# AND LABELLING OF CHEMICALS

Sub-Committee of Experts on the

Transport of Dangerous Goods

Twenty-sixth session

Geneva, 29 November-7 December 2004

Item 4 of the agenda

# NEW PROPOSALS OF AMENDMENT TO THE RECOMMENDATIONS

# ON THE TRANSPORT OF DANGEROUS GOODS

Aluminium witness screens used in Series 6(c) Testing

Availability of specified aluminium sheets

Transmitted by the expert from Australia

# SCOPE

This proposal aims to recommend:

- Amendments to Section 16.6.1.2.(g) of the Manual of Tests and Criteria (Forth revised edition) with regards to the specifications for aluminium witness screens.

# Introduction

1.	Section 16.6.1.2.(g) of the Manual of Tests and Criteria (Forth revised edition) specifies that witness screens used in series 6(c) [External Fire (Bonfire) Test] should be 1100-0 aluminium sheets of Brinell Hardness 23 with a tensile strength of 90MPa. This specification is not in common use and as a result compliant aluminium sheets cannot be sourced for tests conducted in Australia. It appears this material is only available on special order from Norway and with a minimum order quantity of 4m3.

2.	It is unrealistic to expect testing authorities to use a material that is not, in reality, available. As a result series 6(c) testing in Australia is being conducted using aluminium sheets that are of a softer material. As an example 2mm thick 1150 Aluminium sheets have been used. These are a close match to the specification.

# Proposal

3.	It is recommended that section 16.6.1.2.(g) be modified either:

i.	Replace 1100-0 aluminium sheets of Brinell Hardness 23 with a viable specification; or

ii.	Permit the use of a specified viable alternative.

4.	Australia recommends the adoption of a viable alternative employing a matrix that relates thickness of the material to the Brinell hardness in order to provide a range of options that will give the same result as employing the 1100-0 aluminium sheets of Brinell Hardness 23 specified. Using materials that are close to the 1100-0 but do not provide the same susceptibility to indentation and penetration means tests will not be consistent and confidence cannot be maintained in the results. A realistic specification must be adopted in order that all tests are conducted on a consistent basis.

___________