| Transmitted by the expert from CLEPA | Informal Document No. GRE-62-07 (62nd GRE, 6 - 9 October 2009, agenda item 15(h)) |
| --- | --- |

26 August 2009

Proposal for Corrigendum 2 to Supplement 3 to Regulation No. 104

(Retro-reflective markings for heavy and long vehicles and their trailers)

The modification to the Amendment 3 to Regulation No. 104 is marked in bold characters.

# PROPOSAL

Paragraph 8, amend to read:

"8.	Bonding strength (in the case of adhesive materials of Class C)

8.1.	The adhesion of retro-reflective materials shall be determined after 24 hours curing time by utilising a 90 degree peel on a tensile strength testing machine.

8.2.	The retro-reflective materials shall not be easily removable without damaging the material.

8.3.	The retro-reflective materials shall need a force of at least 10 N per 25 mm width at a constant speed of 300 mm per minute to be removed from their substrate."

## B.	JUSTIFICATION

This requirement should only apply to Conspicuity Markings as defined in paragraph 2.7.17. of Regulation No. 48 (Installation of lighting and light-signalling devices).

Class D and E materials, as defined in paragraphs 5.4.3.2. and 5.4.3.3., are not safety devices. Those materials are typically used for advertisement purposes following national regulations (see also paragraph 2.7.16.4. of Regulation No. 48).

- - - - -