IGPG-01-06

Japan prepares some comments for the DRAFT AGENDA of plastic glazing informal meeting.

Please see the following:

1. We would like to add tests of I, II, and III indicated below to “the Update of the test procedures”.

I “Wiper abrasion test”

II “Chipping test and solvent test after that”

III “Chemical resistance test after scratch is made”

These (I, II, and III) were proposed from Japan at the pre-meeting (06 October 2010 at the OICA offices in Paris).

The reason for this proposal is indicated in the presentation which Japan made at the pre-meeting (06 October 2010 at the OICA offices in Paris), as follows:

(1) Windscreen is wiped by wiper blade. --> For good visibility, abrasion resistance needs to be secured.

(2) On windscreen, window washer (solvent) is used. --> For good visibility, solvent resistance needs to be secured.

(3) Windscreen is hit by stones rolled up by the vehicle in front. --> For good visibility, scratch resistance needs to be secured. However, there is no concrete knowledge on the test methods and judgment criteria for test results. (There is no know-how.)

For this reason, we would like to have them discussed and studied specifically in this informal group.

And in these tests, we hope that the Informal Group clarifies performance differences between plastic glazing and sheet glass by conducting comparison tests.

By clarifying performance differences, we would like to get evidences that the use of plastic glazing has no safety problem.

2. In the previous discussions, arguments have become ambiguous and indefinite (to clarify the reason that there is no safety problem) with comments like "there is a track record although there is no data", "the basis is clear", "it is satisfactory also for windshields since there is a track record of SD glass", etc.

For this reason, we would like to have a table showing each test results.

3. Based on the table, the Informal Group needs to eliminate concerns of each country before starting further

discussions at GRSG meetings.

- - - - -